# uv	Appendix 1: The forcefield description

### Parameters

The force field is described in Tables 1 to 8.

| Substance | Atom/Ion label | Charge /e (formula 7) | Mass /au | ε /(kcal/mol) (formula 6) | σ /Å (formula 6) | number per molecule |
| --- | --- | --- | --- | --- | --- | --- |
| CDC | C | -0.04037 ... -0.04758 [Tarmo] | 12.0107 [webelements] | 0.105067 [Walther] | 3.851 [Walther] | 62 … 72 |
|  | H | +0.157 [Tarmo] | 1.00794 [webelements] | 0.0150 [AMBER] | 2.599642 [AMBER] | 16...20 |
| EMI | N1, N2 | +0.15 [Lopes] | 14.0067 [webelements] | 0.169886 [Lopes] | 3.25 [Lopes] | 2 |
|  | Ca1 | -0.11 [Lopes] | 12.0107 [webelements] | 0.069953 [Lopes] | 3.55 [Lopes] | 1 |
|  | Ca2, Ca3 | -0.13 [Lopes] | 12.0107 [webelements] | 0.069953 [Lopes] | 3.55 [Lopes] | 2 |
|  | Cm, Ce1 | -0.17 [Lopes] | 12.0107 [webelements] | 0.065955 [Lopes] | 3.5 [Lopes] | 2 |
|  | Ce2 | -0.05 [Lopes] | 12.0107 [webelements] | 0.065955 [Lopes] | 3.5 [Lopes] | 1 |
|  | Ha1, Ha2, Ha3 | +0.21 [Lopes] | 1.00794 [webelements] | 0.029980 [Lopes] | 2.42 [Lopes] | 3 |
|  | Hm1, Hm2, Hm3, He1, He2, | +0.13 [Lopes] | 1.00794 [webelements] | 0.02998 [Lopes] | 2.5 [Lopes] | 5 |
|  | He3, He4, He5 | +0.06 [Lopes] | 1.00794 [webelements] | 0.02998 [Lopes] | 2.5 [Lopes] | 3 |
| BF4 | B | +1.1504 [Lopes] | 10. 811 [webelements] | 0.094941 [Lopes] | 3.5814 [Lopes] | 1 |
|  | F | -0.5376 [Lopes] | 18.9984 [webelements] | 0.060953 [Lopes] | 3.1181 [Lopes] | 4 |

Table 1: Forcefield parameters of single atoms

| Formula | Atom label 1 | Atom label 2 | E0 /(kcal/mol) | r0 / Å | k / Å-1 | number per molecule |
| --- | --- | --- | --- | --- | --- | --- |
| 2 | C | C | 114.459847 [Walther] | 1.418 [Walther] | 2.1867 [Walther] | 85...89 |

Table 2: Carbon bond parameters (Morse potential, formula 2)

| Atom label 1 | Atom label 2 | k / kcal/mol | r0 / Å | number per molecule |
| --- | --- | --- | --- | --- |
| Ca1 | N1, N2 | 476.736410 [Lopes] | 1.315 [Lopes] | 2 |
| Ca2, Ca3 | N1, N2 | 426.817617 [Lopes] | 1.378 [Lopes] | 2 |
| Ca2 | Ca3 | 519.728671 [Lopes] | 1.341 [Lopes] | 1 |
| N1, N2 | Cm, Ce1 | 336.772714 [Lopes] | 1.466 [Lopes] | 2 |
| Ce1 | Ce2 | 267.746250 [Lopes] | 1.529 [Lopes] | 1 |
| B | F | 289.815611 [Lopes] | 1.39 [Lopes] | 4 |

Table 3: Ionic Liquid bond parameters (formula 1).

| Substance | Atom label 1 | Atom label 2 | r0 / Å | number per molecule |
| --- | --- | --- | --- | --- |
| CDC | C | H | 1.08 [AMBER] | 16...20 |
| EMI | Ca1, Ca2, Ca3 | Ha1, Ha2, Ha3 | 1.08 [Lopes] | 3 |
|  | Cm, Ce1, Ce2 | Hm1...Hm3,He1...He5 | 1.53 [Lopes] | 8 |

Table 4: Geometric constraints

| Atom label 1 | Atom label 2 | Atom label 3 | k / kcal/mol | φ0 / deg | number per molecule |
| --- | --- | --- | --- | --- | --- |
| C | C | C | 134.369025 [Walther] | 120.0 [Walther] | 154...158 |
| C | C | H | 35.000000 [AMBER] | 120.0 [AMBER] | 32...40 |
| Ca3, Ca2 | N1, N2 | Ca1 | 69.886309 | 108.0 | 2 |
| Ca3, Ca2 | N1, N2 | Ce1, Cm | 69.886309 | 125.6 | 2 |
| Ca1 | N1, N2 | Ce1, Cm | 69.886309 | 126.4 | 2 |
| N1, N2 | Ca1 | Ha1 | 34.943155 | 125.1 | 2 |
| N1 | Ca1 | N2 | 69.886309 | 109.8 | 1 |
| N1, N2 | Ca3, Ca2 | Ca2, Ca3 | 69.886309 | 107.1 | 2 |
| N1, N2 | Ca3, Ca2 | Ha3, Ha2 | 34.943155 | 122.0 | 2 |
| Ca2, Ca3 | Ca3, Ca2 | Ha3, Ha2 | 34.943155 | 130.9 | 2 |
| N1 | Ce1 | He1, He2 | 74.806535 | 110.7 | 2 |
| N2 | Cm | Hm1, Hm2, Hm3 | 74.806535 | 110.7 | 3 |
| Ce1 | Ce2 | He3, He4, He5 | 74.806535 | 110.7 | 3 |
| Ce2 | Ce1 | He1, He2 | 74.806535 | 110.7 | 2 |
| N1 | Ce1 | Ce2 | 99.933123 | 112.70 | 1 |
| He1 | Ce1 | He2 | 65.945352 | 107.8 | 1 |
| He3, He4, He5 | Ce2 | He4, He5, He3, | 65.945352 | 107.8 | 3 |
| Hm1, Hm2, Hm3 | Cm | Hm2, Hm3, Hm1 | 65.945352 | 107.8 | 3 |
| F | B | F | 49.966562 | 109.5 | 6 |

Table 5: Forcefield valence angle potential parameters (formula 3)

| Atom label 1 | Atom label 2 | Atom label 3 | Atom label 4 | A /(kcal/mol) | δ /deg | m | Number per molecule |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C, H | C | C | C, H | 3.0 [Walther] | 180 | 2 | 345…398 |

Table 6: Forcefield dihedral parameters for carbon (formula 4)

| Atom label 1 | Atom label 2 | Atom label 3 | Atom label 4 | A1 /(kcal/mol) | A2 /(kcal/mol) | A3 /(kcal/mol) | Number per molecule |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ca3, Ce1 | N1 | Ca1 | N2, Ha1 | 0 | 4.647941 | 0 | 4 |
| Ca2, Cm | N2 | Ca1 | N1, Ha1 | 0 | 4.647941 | 0 | 4 |
| N2,Ha2 | Ca2 | Ca3 | N1, Ha3 | 0 | 10.743288 | 0 | 4 |
| Ca1, Ce1 | N1 | Ca3 | Ca2, Ha3 | 0 | 2.997516 | 0 | 4 |
| Ca1, Cm | N2 | Ca2 | Ca3, Ha2 | 0 | 2.997516 | 0 | 4 |
| Ca3 | N1 | Ce1 | He1, He2 | 0 | 0.131365 | 0 | 2 |
| Ca2 | N2 | Cm | Hm1, Hm2, Hm3 | 0 | 0.131365 | 0 | 3 |
| Ca1 | N1 | Ce1 | He1, He2 | 0 | 0 | 0 | 2 |
| Ca1 | N2 | Cm | Hm1, Hm2, Hm3 | 0 | 0 | 0 | 3 |
| Ca3 | N1 | Ce1 | Ce2 | -1.375752 | 1.058087 | 0.209468 | 1 |
| Ca1 | N1 | Ce1 | Ce2 | -0.771472 | 0 | 0 | 1 |
| N1 | Ce1 | Ce2 | He3, He4, He5 | 0 | 0 | 0 | 3 |
| He1, He2 | Ce1 | Ce2 | He3, He4, He5 | 0 | 0 | 0.317904 | 6 |
| Ce1 | N1 | Ha1, Ca3 | Ca3, Ha1 | 0 | 1.999140 | 0 | 2 |
| Cm | N2 | Ca1, Ca2 | Ca2, Ca1 | 0 | 1.999140 | 0 | 2 |
| Ha1 | Ca1 | N1, N2 | N2, N1 | 0 | 2.197382 | 0 | 2 |
| Ha2 | Ca2 | N2, Ca3 | Ca3, N2 | 0 | 2.197382 | 0 | 2 |
| Ha3 | Ca3 | N1, Ca2 | Ca2, N1 | 0 | 2.197382 | 0 | 2 |

Table 7: Forcefield dihedral parameters for EMI (formula 5)

### Formulas

Harmonic bond potential:

(1)

Morse potential:

(2)

In the bond potential formulas, U is the potential energy of the bond, r is the interatomic distance and r0, k and E0 are bond parameters.

Harmonic angle potential:

(3)

„cos“ dihedral potential:	U(φ)=A[1+cos(mφ -δ)]	(4)

„cos3“ dihedral potential:	U(φ)=(1/2)A1(1+cos(φ)) + (1/2)A2(1-cos(2φ)) + (1/2)A3(1+cos(3φ))	(5)

Lennard-Jones potential: 		(6)

Coulomb potential:		(7)

Lorentz-Berthelot combining rules:	, 	(8)

The intermolecular potential consists of Lennard-Jones potentials (6) combined using Lorentz-Berthelot combining rules (8) and Coulomb potentials (7).

### References

- [Walther] –  http://dx.doi.org/10.1021/jp011344u

- [AMBER] – http://dx.doi.org/10.1021/ja00124a002

- [Lopes] – J. N. C. Lopes, J. Deschamps, A. A. H. Pádua, J. Phys. Chem. B, 108, 2038–2047, (2004); http://dx.doi.org/10.1021/jp0362133

- [webelements] http://webelements.com

- [Tarmo] – Tarmo Tamm, private communication