(

A Linked Manipulator with IPMC Joints for Soft- and Micromanipulation

Maarja Kruusmaa, Andres Hunt, Andres Punning, Mart Anton, Alvo Aabloo

Abstract—These instructions give you guidelines for preparing papers for IEEE conferences. Use this document as a template if you are using Microsoft Word 6.0 or later. Otherwise, use this document as an instruction set. Instructions about final paper and figure submissions in this document are for IEEE journals; please use this document as a “template” to prepare your manuscript. For submission guidelines, follow instructions on paper submission system as well as the Conference website. Do not delete the blank line immediately above the abstract; it sets the footnote at the bottom of this column.

# INTRODUCTION

E

lectroactive polymer materials  are materials that change their shape and size when electrically stimulated. This paper represents a manipulator design using a specific type of electroactive polymers, called ionomeric polymer metal composites (IPMC) [oguro]. These materials bend when  electric voltage is applied.

Fig. 1 shows a typical response of the IPMC material to electric stimulation. In Fig. 1 (B) the strip of the IPMC sheet is fixed between the electric contacts from above. When low voltage is applied to the contacts the material bends in response to the stimulation as it is shown in Fig. 1 (A) and Fig. 1 (C). The direction of bending depends on the polarity of the applied voltage.

An IPMC consists of a thin ion-exchange polymer membrane covered with a thin metal layer from both sides. The metal layers serve as surface electrodes. The ion-exchange membrane contains and excess of free cations. When voltage is applied to the surface electrodes through the clamps, the cation migration in the electric field causes the expanding of the membrane from one side and this is observed as the bending of the material. The actual electrochemical processes inside the membrane are much more complicated though and not yet thoroughly understood. The reader is referred to [nemat-nasser] for a detailed discussion.

IPMC materials work at low  voltages (up to 5V), have high actuation length (for example bending radius of 1 cm), they are soft and flexible but at the same time have low output force (few mN). Compared to many other types of electroactive polymer materials IPMC are also rather mature, with custom-made materials commercially available for purchase [eamex].

IPMC materials can also work as sensors, when they are mechanically bent they generate voltage between the metal surfaces (few mV) and are proposed to be used as accelerometers or vibration sensors.

Fig. 1.The IPMC material under electric stimulation

Pilt ära vahetada!

## State-of-the-art of IPMCs for robotics

IPMC materials propose an appealing alternative in robotics design. Devices using the conventional technology of electromechanical devices need rigid links to connect the rotating joints, gears and bearings and they are therefore unavoidably complex, rigid and noisy.

IPMC materials offer almost complementary alternatives to the electromechanical devices. They are lightweight, soft and flexible, easy to miniaturize, and permit distributed actuation and sensing. The behavior of the EAP materials in the electric field somewhat resembles the performance of biological muscles, therefore EAP materials are considered to be good candidates for building biomimetic devices [cohe, breazeal]. However, compared to the technology of electromechanical devices, EAPs have many drawbacks typical to developing technologies such as low output force or small strain (depending on the material used), high energy consumption and lack of well-established control methods.

To demonstrate their suitability for robotic applications many proof-of-concept prototype devices have been created, such as an active catheter system [3[,  micromanipulators [5], a miniature robotic arm [6], a micropump [7], a facetype actuator [8], a wiper for an asteroid rover [9], prototype walking robot [] or a ray-like underwater robot [10].

## IPMC materials for soft manipulators

Due to the softness and flexibility but small output force  IPMC materials seem to be a natural choice for soft- and micromanipulation. However, there are several fundamental problems still to be solved before these devices could be put in a practical use. First of all, although the material properties of IPMCs are steadily improving, their long-terms stability, efficiency and reliability is still not sufficient for commercial applications. Second, appropriate control methods and mechanical design of these manipulators are still to be developed.

So far, IPMC manipulator design and their control is addressed by several authors who also mention soft manipulation as a suitable application area.  In [laser] a higher number of degrees of freedom of IPMC manipulator is achieved by laser ablation of the metal coating of the IPMC strip. After metal plating a pattern is cut on both sides of the membrane. By patterning, the thin metal layer is removed and insulations between segments of the electrodes are achieved [46, 48]. There have also been attempts to couple laser patterned sensor and actuator segments on a single piece of a patterned polymer backbone [49, 50].

Zheng et al. have developed a combined IPMC/PVDF sensing actuator and demonstrated its applicability for open-loop micro-injection of living Drosophila embryos.

The applicability of these manipulators depends on more fundamental issues, namely, how well the issues of IPMC modeling and control are solved.

Control of IPMC manipulators is usually investigated in the cantilever beam configuration, fixing one end of a thin IPMC strip between electric contacts and controlling the displacement or the blocking force of the tip [malllavarapu, etc..]. Typically these methods are accurate only at small flexures, for example, when measuring the output force of a cantilever IPMC actuator against a fixed load cell.

Control of IPMC devices has also been addressed in various papers, none of the results are though, particularly successful. For example the walking robot with IPMC linear actuators with the feedback from off-board camera has been reported to walk 6 steps [asaka]. In our own previous work we have managed to balance and inverted pendulum with an IPMC actuator for 10 seconds. These results are not particularly impressive from the control perspective and rather confirm that the control of IPMC devices is still to a large extent and unsolved problem.

In this paper we propose a design concept of a linked manipulator with IPMC rotating joints and passive links. We argue that this design reduces the control complexity of an IPMC manipulator and increases the precision of the device.

This design concept is derived from our previous work in material modeling. In the following section we briefly describe the results of our past work that has motivated our desing. After that, we describe the manipulator design. Section IV is devoted to validation of the manipulator’s performance. We demonstrate that the control of the linked manipulator can be implemented using conventional inverse kinematics of robot manipulators. The open loop control experiments also show that the precision of this manipulator increases considerably compared to a IPMC cantilever beam manipulator. Also the workspace of the manipulator is enlarged from an 1D circular trajectory to a 2D workspace. We also show that the reaction time of the manipulator increases. We finish this paper with few remarks about the implications and limitations of this work.

# previous work and desing considerations

This section gives a brief overview of our previous work on modeling of IPMC cantilever beams. The conclusions of these studies have motivated the design choice of our linked IPMC manipulator.

## The distributed model of an IPMC manipulator

IPMC materials are usually described as lumped models with uniform properties. These models are rather simple and convenient for control but do not describe the response of the IPMC actuators to electric stimulation very accurately. Instead, we have proposed a distributed model of an IPMC manipulator as shown in Fig. 1 [punni tiss]. The resistors Ra and Rb represent the conductivity of the surface metal coating and the resistors Rc,Rx and C are properties of the polymer ion-exchange membrane.

Fig.1. A distributed model of IPMC

The circuit shown in Fig. 1 is well known in circuit theory and, in fact, represents a lossy transmission line. Looking at the IPMC manipulator is such a way also explains why real-time control of IPMC manipulators is so challenging.  The control signals traveling along the transmission line get delayed and distorted. The longer is the line or the worth is the surface conductivity Ra and Rb, the harder in the behaviour of the actuator to describe. If the transmission line is non-uniform, the closed-form solutions are available only in rare circumstances, the solutions are usually numerical approximations and not necessarily suitable for real-time control.

## Optimal design of IPMC cantilever beam manipulators

In [mart] we have presented the electromechanical model of the cantilever beam IPMC actuator where the actuator is described as subject to bending caused by external force and electrically induced bending moment. The electrically induced bending moment can vary along the surface.

We have also investigated a case where the Young’s modulus of the beam is not constant, which makes it possible to analyze cases where part of the IPMC actuator is replaced with a passive rigid elongation. We have studied the optimal design of an elongated IPMC manipulator in terms of output force, efficiency and work done by unit area of an IPMC actuator.

The theoretical analysis confirmed by experiments has lead to the following conclusions. First, the output force of the actuator is proportional to the width of the IPMC sheet.

Second, when optimizing work done by the active part of the actuator per unit area, it appears that part of the IPMC actuator can be replaced with a rigid elongation and the actuator still has an equal performance.

| (a) | (b) |
| --- | --- |

Third, the position-force relationship of a short IPMC actuator with an elongation is linear while for an equally long IPMC sheet it is not. From a control point of view, this indicates that an elongated actuator should be better suited for precision control.

Also, to estimate the shape of the long sheet is more difficult. Fig. xxx shows the static equilibrium states of the two actuators and shows that in the static equilibrium state the shape of the sheet differs. In case of a long sheet the difference is big. In case of a short sheet with a passive elongation the difference is barely noticeable. When considering moving sheets the shape of the sheet is an input parameter that we need to know in order to calculate the output force. In case of a short sheet with elongation the shape of the sheet does not vary so much and can be easily estimated. In case of the long sheet estimation of the shape is more difficult.

## Position-input voltage relationship of IPMC actuators.

In connection of the RC transmission line modeling of the IPMC actuators we have intensively investigated the relationship between the driving voltage and flexure of the cantilever beam actuator. In general, the transmission line causes the input signal to get delayed and progressively weaker when traveling towards the tip and such a behavior is usually hard to describe, analytical solutions exist only for special cases and the solutions are not suitable for real time control.  However, our simulations show that for certain short length the relationship between input voltage and deflection angle is linear Kas see väide on kuskil tõestatud?.  So if short pieces of IPMC are considered, there is a chance that the behaviour can be described by a simple formula suitable for real-time control.

# manipulator design

## Design considerations

The design of our IPMC manipulator is motivated by our previous work in materials modeling. The results that have affected our design considerations are the following:

- An IPMC material can be described as a lossy RC-line. The longer is the actuator, the longer is the line. The longer is the line, the more the signals get distorted and delayed and the harder the actuator is to model and consequently, to control.

- An IPMC cantilever actuator can be partially replaced with a passive elongation without the loss of efficiency.

- The output force of the actuator does not depend on the length of the IPMC sheet but on the width. When more output force is required, the IPMC actuator should be wider, not longer.

- If a long strip of an IPMC is replaced with a short IPMC and a passive elongation with an equal efficiency, the mechanical model of the actuator gets simplified. The force-position relationship gets linear and the actuator has no shape memory.

- At a certain short length of the IPMC delay line, the relationship between voltage and deflection angle of the actuator is linear.

These conclusions quite well guide the choices of manipulator that would be better controllable but still efficient.

First of all, we conclude that a soft IPMC manipulator as it is usually described and analyzed so far by various authors [] can be replaced by a short IPMC piece with a rigid elongation. That would increase the controllability of the manipulator. If the IPMC part is very short with respect to the elongation, the manipulator can be described and analyzed as consisting of a passive rigid link and an active rotating joint. (see Fig. x)

When more degrees of freedom are required these joints and links can be liked together to form a chain. Occasionally, this configuration is exactly a classical serial robot manipulator with very well established models and control methods. We can thus reduce the very complicated problem of IPMC manipulator control to the conventional serial robot manipulator control.

At the same time, this design has several advantages compared to traditional robot manipulators where the joints are driven by electric motors. First, this design is mechanically simpler, as it only requires sheets of different materials to be connected together and each joint to be separately powered. Therefore the manipulator is easier to miniaturize. However, it should be also mentioned, that on the other hand, the mechanical design gets more complicated when compared to an IPMC manipulator made of the single strip of an IPMC sheet (such as in Fig. 1).

Second, the manipulator is inherently compliant due to the elastic joints. These would make the manipulator more suitable for soft object and micro manipulator than the conventional electromechanical robotic manipulators where the compliance is achieved with a sophisticated mechanical design.

An important issue in robot manipulation is force control. However, the output force of the IPMC is very little (ca 10 mN). In practice, it is quite difficult to find an application where this force is too large. Internal friction and intertia are small. Therefore the output force is proportional to inut voltage.  Rather it seems that the force should be maximized depending on the application at hand. It would thus make more sense to specify the maximal required force and then design the manipulator knowing that the maximal force is proportional to the width of the IPMC joint. In practice, the lack of force control or in general, imprecision of control, is also somewhat compensated by the inherent compliance of the IPMC material.

# validation of the manipulator design

We designed a manipulator prototype based on the considerations descried above.  The prototype device is depicted in Fig. xxx. In this section we validate the robot design to justify our design considerations. We aim at answering the following questions:

Fig.xxx. Manipulator prorotype

- Does this manipulator design increase the precision with respect to the conventional manipulator made of a single strip of an IPMC material?

- can the input voltage and curvature relationship of a short IPMC joint be described by a linear approximation as suggested by our previous theoretical results?

- How much does the new design increase the reachable workspace compared to a manipulator made of a single strip of an IPMC material?

- Does the new design of the manipulator increase the reaction time compared to the manipulator made of a single long IPMC sheet?

In these experiments we do not measure the efficiency, output force and the force position relationship of the manipulator as this is thoroughly investigated and experimentally validated in [mart] for the elongated IPMC mechanical models.

## Materials and Methods

The experiments consist of the following phases:

- First, a single IPMC joint with a rigid elongation is characterized to find the relationship between the driving voltage and curvature.

- The manipulator is built and tested. The previously gained voltage-curvature relationship is used to control the joints. The precision of the manipulator is measured and verified against a single IPMC strip with an equal length.

- The surface resistance of the manipulator joint is measured to investigate how it reflects the curvature of the joint.

In the following we briefly describe the experimental setup for each of the experiments, more technical details are available in [hunt bakatöö].

Fig. xxx shows the general experimental design. The manipulator is driven with LabView7 DAQ board and driven from separate energy source through a current amplifier. The motion of the actuator is recorded with an overview camera. For the single IPMC joint calibration the angle of the elongated strip is recorded against an illuminated white background. To measure the position of the manipulator, LEDs are mounted at manipulator joints.

Autoaku maha võtta, 6703 on õige ei ole õige!

The IPMC material used in these experiments is Musclesheet™, provided by BioMimetics Inc. Musclesheet™ consists of a 0.2…0.5 mm thick proprietary ionomer, similar to Nafion, covered with platinum electrodes. The materials were doped with Li+ or Na+ counter-ions prior to the experiments and the experiments were conducted in deionised water to keep the environmental conditions constant. The passive links are made of plastic.

## Characterization of a manipulator segment

The joints of the manipulator where separately characterized using the setup in Fig. xxx.

The purpose of the calibration was to find the relationship between the driving voltage and the angle of the IPMC joint. Moreover, we were also interested if we can find a certain optimal length of the IPMC joint where the function of the curvature from the input voltage is linear as suggested by out previous theoretical work.

Lüli kalibreerimise graafik siia.

Some results of the joint calibration are found in Fig. xxxx. They show that the assumption of linearity holds only in some cases. When we found the optimal length of the joint so that the function is linear in one direction, the linearity does not hold when the segment bends in the opposite direction. This is most probably caused by that the resistance and stiffness of the surface electrode is not equal on both sides and therefore also the behaviour of the actuator differs when bent in opposite directions. We thus failed to find a single universal function that would universally characterize all joints and the joints had to be characterized separately by simple curve-fitting.

## Manipulator control

The purpose of the experiments with the manipulator was to show that the linked manipulator with IPMC joints can be reduced to a simple serial link robotic manipulator and be controlled using simple methods of inverse kinematics.

To determine the position of the manipulator LEDs were mounted to both of the joints and the tip of the manipulator. The joint and tip positions where then extracted from a camera image. As an indirect measurement method this does not affect the performance of the manipulator and we also made sure that the errors caused by image processing are negligible.

The precision of the manipulator was then measured by choosing 400 random points from the workspace of the manipulator and driving the tip of the manipulator to reach these goal points. The manipulator was driven by LabView 7 calculating the joint angles with inverse kinematics equations. In case of a planar manipulator with 2 joints these equations reduce to simple trigonometric equations:

Siia valem

where the driving voltage corresponding to angles 1 and  2 where found from the previous curve fitting experiments.

The charts in Fig. xx and Fig. xx show the experimental distribution of absolute and relative errors respectively.

Alumine joonis ära võtta square root of a Chi-square distribution

## Comparative experiments with a single IPMC strip

To compare the performance of the linked manipulator with the conventional single strip IPMC manipulator, comparative experiments where conducted. Our hypothesis was that the linked configuration of the manipulator would simplify the manipulator control and increase precision. For that purpose we used a single IPMC strip (such as in Fig. 1) with the length equal to the length of the linked manipulator . We characterized the strip by curve fitting as we did for the joints of the linked manipulator. Next, we chose random points on the working trajectory of the manipulator, as we did for the linked manipulator and measured the precision of the open-loop control. The results are represented in Fig. xxx

Siia pika lihase täpsuse graafik

Kas saad 2 joont anda samal graafikul?

The results show that the precision of the linked manipulator increases 314% with respect to the single strip IPMC manipulator.

## Reaction time

The IPMC manipulator represents a lossy transmission line, so it would be feasible to expect that as the length of the IPMC strip increases the response time of the actuator increases as well as the signals take time to spread until the tip. We thus hypothesized that the linked manipulator is faster as the IPMC joints are short and electrically decoupled from each other.

We therefore conducted comparative experiments with the linked manipulator and an IPMC sheet of an equal length. The voltage was applied to both  devices and the time required to obtain the maximal flexure was recorded.

## Reachable Workspace

Siia pilt kuidas tööpiirkond suureneb

# conclusions

## This paper presented a linked IPMC manipulator with IPMC joints. We have shown that such a design of an IPMC manipulator increases the precision and the workspace of the manipulator compared to a conventional single strip IPMC manipulator commonly investigated in the literature of smart materials. At the same time the linked manipulator is at least equally efficient and the output force equally large. Due to the IPMC joints the manipulator is inherently soft and compliant. Compared to a single strip manipulator it gets mechanically more complex but compared to a conventional electromechanical manipulator driven my DC motor powered joints it is considerably simpler and therefore easier to miniaturize. We therefore propose that this manipulator is well suited for soft object and micro manipulation.

The main contribution of this paper is to show that the IPMC manipulator control, very vaguely understood so far, can be reduced to simple well-established methods of inverse kinematics. Although serial chain manipulators are a standard measure in robotics and from robotics perspective this solution might look trivial, it is not so far considered for electroactive polymer manipulators. Also the rationale for this design is not “to build the manipulators like it is always done” but is motivated from out theoretical work in materials modeling. This work theoretically shows that the behavior of a short IPMC manipulator is more linear and that part of the IPMC actuator can be replaced by an passive elongation without the loss in efficiency. Our experimental results confirmed these assumptions.

This design can be improved or modified for example by adding more links to even more increase the workspace, to change the orientation of joints to make the manipulator to work in 3D instead of 2D or by adding an extra soft link to the tip of the manipulator for extra soft manipulation. It can be also improved by applying closed loop control, either by using feedback from ad off-board camera or from the self-sensitive IPMC joints.

References

- G. O. Young, “Synthetic structure of industrial plastics (Book style with paper title and editor),” 	in Plastics, 2nd ed. vol. 3, J. Peters, Ed.  New York: McGraw-Hill, 1964, pp. 15–64.

- W.-K. Chen, Linear Networks and Systems (Book style).	Belmont, CA: Wadsworth, 1993, pp. 123–135.

- H. Poor, An Introduction to Signal Detection and Estimation.   New York: Springer-Verlag, 1985, ch. 4.

- B. Smith, “An approach to graphs of linear forms (Unpublished work style),” unpublished.

- E. H. Miller, “A note on reflector arrays (Periodical style—Accepted for publication),” IEEE Trans. Antennas Propagat., to be published.

- J. Wang, “Fundamentals of erbium-doped fiber amplifiers arrays (Periodical style—Submitted for publication),” IEEE J. Quantum Electron., submitted for publication.

- C. J. Kaufman, Rocky Mountain Research Lab., Boulder, CO, private communication, May 1995.

- Y. Yorozu, M. Hirano, K. Oka, and Y. Tagawa, “Electron spectroscopy studies on magneto-optical media and plastic substrate interfaces(Translation Journals style),” IEEE Transl. J. Magn.Jpn., vol. 2, Aug. 1987, pp. 740–741 [Dig. 9th Annu. Conf. Magnetics Japan, 1982, p. 301].

- M. Young, The Techincal Writers Handbook.  Mill Valley, CA: University Science, 1989.

- J. U. Duncombe, “Infrared navigation—Part I: An assessment of feasibility (Periodical style),” IEEE Trans. Electron Devices, vol. ED-11, pp. 34–39, Jan. 1959.

- S. Chen, B. Mulgrew, and P. M. Grant, “A clustering technique for digital communications channel equalization using radial basis function networks,” IEEE Trans. Neural Networks, vol. 4, pp. 570–578, July 1993.

- R. W. Lucky, “Automatic equalization for digital communication,” Bell Syst. Tech. J., vol. 44, no. 4, pp. 547–588, Apr. 1965.

- S. P. Bingulac, “On the compatibility of adaptive controllers (Published Conference Proceedings style),” in Proc. 4th Annu. Allerton Conf. Circuits and Systems Theory, New York, 1994, pp. 8–16.

- G. R. Faulhaber, “Design of service systems with priority reservation,” in Conf. Rec. 1995 IEEE Int. Conf. Communications, pp. 3–8.

- W. D. Doyle, “Magnetization reversal in films with biaxial anisotropy,” in 1987 Proc. INTERMAG Conf., pp. 2.2-1–2.2-6.

- G. W. Juette and L. E. Zeffanella, “Radio noise currents n short sections on bundle conductors (Presented Conference Paper style),” presented at the IEEE Summer power Meeting, Dallas, TX, June 22–27, 1990, Paper 90 SM 690-0 PWRS.

- J. G. Kreifeldt, “An analysis of surface-detected EMG as an amplitude-modulated noise,” presented at the 1989 Int. Conf. Medicine and Biological Engineering, Chicago, IL.

- J. Williams, “Narrow-band analyzer (Thesis or Dissertation style),” Ph.D. dissertation, Dept. Elect. Eng., Harvard Univ., Cambridge, MA, 1993.

- N. Kawasaki, “Parametric study of thermal and chemical nonequilibrium nozzle flow,” M.S. thesis, Dept. Electron. Eng., Osaka Univ., Osaka, Japan, 1993.

- J. P. Wilkinson, “Nonlinear resonant circuit devices (Patent style),” U.S. Patent 3 624 12, July 16, 1990.

- IEEE Criteria for Class IE Electric Systems (Standards style), IEEE Standard 308, 1969.

- Letter Symbols for Quantities, ANSI Standard Y10.5-1968.

- R. E. Haskell and C. T. Case, “Transient signal propagation in lossless isotropic plasmas (Report style),” USAF Cambridge Res. Lab., Cambridge, MA Rep. ARCRL-66-234 (II), 1994, vol. 2.

- E. E. Reber, R. L. Michell, and C. J. Carter, “Oxygen absorption in the Earth’s atmosphere,” Aerospace Corp., Los Angeles, CA, Tech. Rep. TR-0200 (420-46)-3, Nov. 1988.

- (Handbook style) Transmission Systems for Communications, 3rd ed., Western Electric Co., Winston-Salem, NC, 1985, pp. 44–60.	Motorola Semiconductor Data Manual, Motorola Semiconductor Products Inc., Phoenix, AZ, 1989.

- (Basic Book/Monograph Online Sources) J. K. Author. (year, month, day). Title (edition) [Type of medium]. Volume(issue).	 Available: http://www.(URL)

- J. Jones. (1991, May 10). Networks (2nd ed.) [Online]. Available: http://www.atm.com

- (Journal Online Sources style) K. Author. (year, month). Title. Journal [Type of medium]. Volume(issue), paging if given.	  Available: http://www.(URL)

- R. J. Vidmar. (1992, August). On the use of atmospheric plasmas as electromagnetic reflectors. IEEE Trans. Plasma Sci. [Online]. 21(3). pp. 876—880.   Available: http://www.halcyon.com/pub/journals/ 21ps03-vidmar

# Footnotes

Manuscript received October 9, 2001. (Write the date on which you submitted your paper for review.) This work was supported in part by the U.S. Department of Commerce under Grant BS123456 (sponsor and financial support acknowledgment goes here). Paper titles should be written in uppercase and lowercase letters, not all uppercase. Avoid writing long formulas with subscripts in the title; short formulas that identify the elements are fine (e.g., "Nd–Fe–B"). Do not write "(Invited)" in the title. Full names of authors are preferred in the author field, but are not required. Put a space between authors' initials.

F. A. Author is with the National Institute of Standards and Technology, Boulder, CO 80305 USA (corresponding author to provide phone: 303-555-5555; fax: 303-555-5555; e-mail: author@ boulder.nist.gov).

S. B. Author, Jr., was with Rice University, Houston, TX 77005 USA. He is now with the Department of Physics, Colorado State University, Fort Collins, CO 80523 USA (e-mail: author@lamar. colostate.edu).

T. C. Author is with the Electrical Engineering Department, University of Colorado, Boulder, CO 80309 USA, on leave from the National Research Institute for Metals, Tsukuba, Japan (e-mail: author@nrim.go.jp).