# A Distributed Model of Ionomeric Polymer Metal Composite (IPMC).

A. Punning, U. Johanson, M. Anton, A.Aabloo, M.Kruusmaa

Institute of Technology, Tartu University, Nooruse 1, Tartu 50411, Estonia

Corresponding author: Andres.Punning@ut.ee

Abstract.

This paper presents a novel model of an IPMC (Ionomeric polymer metal composite). An IPMC is modeled as a distributed RC transmission line. Unlike other electromechanical models of an IPMC, the distributed nature of our model permits modelling the non-uniform bending of the material. Instead of modeling the tip deflection or uniform deformation of the material, we model the changing curvature. The analytical model is shown to be consistent with the experimental results. We also demonstrate that this analytical model can be used to determine the optimal configuration of the sheet. From the described model we finally derive a more elaborate model that also considers the non-linear parameters of the sheet during bending.

1. Introduction.

IPMCs are materials that bend in electric field (Fig. 1). An IPMC actuator consists of a highly swollen polymer sheet, such as Nafion™, filled with water or ionic liquid and plated with metal on both sides. Applied voltage causes the migration of ions inside the polymer matrix which in turn causes the non-uniform distribution of the ions inside the polymer. As a result, the polymer sheet bends. The direction of bending depends on the polarity of the applied voltage. An overview of the working principle of IPMC actuators can be found e.g. in [1].

Fig. 1. An IMPC sheet in a bent configuration with the opposite driving voltage polarities (A and C) and an initial configuration with no electric stimulus applied (B).

IPMC actuators and sensors have many appealing properties from the implementation point of view. Being noiseless, soft and flexible, mechanically simple, lightweight and resilient they have potentially many applications in the areas of noise damping, haptics, smart textiles, biorobotics, medicine, space applications and elsewhere [2].

The state-of-the-art of the IPMC sensor and actuator technology is not thoroughly understood which makes it difficult to predict the behavior of this material and therefore limits the potential applications areas.

Several models are proposed so far to model the behavior of IPMC sensors and actuators. A systemized overview of the existing models can be found in [3]. The most accurate IPMC models are derived from first principles and comprise the modeling of underlying electrochemical phenomena coupled to the mechanical bending of the sheet [4, 5, 6]. While capturing the complex phenomena inside the IPMC actuator those models tend to be complex, computationally time consuming and require laborious parameter identification.

The empirical models describing the behavior of the actuator on a macro-level are derived experimentally by curve fitting [7, 8] or based on the description of some sort of an equivalent circuit [9, 10, 11]. To our knowledge, all the equivalent circuit models proposed so far are treated as lumped models. Kanno and Tadokoro have proposed a model in a form of an RC-line but by representing the circuit in a form of a first order transfer function they reduce it to a lumped model and define the relationship between tensile stress and input current. Also the model proposed by X. Bao et al. [12] is based on the assumption of uniform properties but it is recognized that the distributed model would provide a more accurate description. In [13] a distributed model is proposed, where the IPMC actuator is divided to segments, but each segment is assumed to be driven separately to achieve waving motion of the actuator and each segment is again treated as a lumped model subjected to uniform tensile forces.

The models proposed so far can model the tip displacement or output force of the tip but not the configuration of the entire actuator surface. The model proposed by us is different in the sense that it takes into consideration the fact that deformation of the IPMC material is non-uniform. Fig, 1 represents a typical behavior of the actuator where the bending curvature from the electric contacts along the sheet decreases.

The fact that the electric current through the polymer matrix of IPMC causes nonuniform distribution of voltage along the electrodes seems not to have been sufficiently covered in scientific literature. In this paper we propose modelling the IPMC actuator as a distributed RC line. This presentation permits identifing the electric current through the polymer matrix at every point of the IPMC sheet. As such, it corresponds more accurately to the real situation where the bending curvature of the actuator at each point is determined by the migration of ions at that particular location and variations in the ion concentration cause non-uniform bending.

We represent the model of an IPMC actuator in an analytical or simulated form based on the theory of RC transmission lines and show the solution in case of the step input voltage. By coupling the current through the polymer matrix to the mechanical bending of the actuator we derive the electromechanical model of an IPMC. We then proceed by representing the simulation results and thereafter demonstrate that these results are well consistent with the experimental data obtained from the experiments of four different types of IPMC.

2. Characterization of the actuator.

Generally the models of an IPMC described in the scientific literature do not characterize the shape of IPMC-based devices. These models usually describe the motion of the tip or the bending radius of the device assuming that the bending radius is constant. The equipment used to characterize the parameters are for instance laser position sensors or force gauges [14-17].

In order to describe the mechanical motion of the actuator, we developed a simple computer vision system. It consists of a fast CCD camera and a PC with image processing software. The National Instruments Vision was used for both frame grabbing and image processing. The direction of the camera is set transverse to the actuator and the experiment is illuminated from the background through a frosted glass. In perfect conditions the image of the actuator recorded in such a way consists of a single curved contrast line. It is easy to use image processing software to process the shape of the actuator during each particular frame. The separate frames of a noticeably bending actuator, recorded in such a way, are depicted in Fig. 2.

It is apparent from Fig. 2., that in the beginning of the input pulse (images 0...0.4s in Fig. 2.-A) the actuator performs a sharp motion close to the input contacts only, the free end remains almost straight.

A			B

Fig. 2. Overlay of a series of frames showing the response of an actuator to a 1s driving voltage pulse. A – actuation during the pulse; B – relaxation after the pulse. The numeric characters indicate the time instant of the frame.

Later (images 0.4...1.0s in Fig. 2.-A) the flexure of the actuator propagates gradually on, but the flexure at the region close to the contacts does not increase any more. During the relaxation (images 1.0...4.0s in Fig. 2.-B) the sharp decrease of the flexure takes place close to the input contacts again, whereas the remaining part of the actuator straightens slowly in few seconds.

The drop of voltages along the electrodes of the actuator can be recorded by attaching additional terminals onto its surface. The outline of the setup of the electrical measurements is depicted in Fig. 4.

Fig. 4. Setup of electrical measurements.

We measure the voltages on the surface of a working IPMC-based actuator or sensor by attaching a set of pairs of lightweight contacts to its surface using special lightweight clips, and connect them via thin wires to the measuring equipment. The voltages , ,  and  with respect to the ground are measured at the contacts C, D, E and F respectively, as well as the input voltage  at the contact A. The voltages between the two faces of the sample can be calculated as , and .

The measured voltages on an actuator, bending similarly to the one presented in Fig. 2, are represented as a 3D graph in Fig. 5.

Fig. 5. Voltages along a bending actuator.

It is apparent in Fig. 5. that even in the middle of the sample the voltage does not reach a substantial value. The voltage at the free end differs from the voltage in the middle only slightly.

In order to describe the bending movement of the actuator, the image of the bending sheet is divided into segments assumed to have a constant curvature. The principle of determining the angles is shown in Fig 4. (angles  - ). The angles of the segments are calculated from each frame of the video. The changing flexure of the actuator, electrically characterized in Fig. 5. is depicted in Fig. 6. It can be observed that the bending of the sheet is faster and stronger close to the input contacts, getting progressively weaker as well as delayed towards the free end of the sheet.

Fig. 6. Mechanical response of an actuator to a step input voltage. The “Position” axis stands for the relative coordinate starting from the input contacts.

It is apparent that the the two graphs – the graph of spreading voltages along the surface and the graph of bending angles along the surface are strikingly similar

### 3. A distributed electromechanical model of IPMCs.

The fact that the electrical perturbation as well as the change of the flexure spreading along the actuator at finite speed; and the described similarity between the two graphs Fig. 5. and Fig. 6. were the motivations to develop a distributed model of an IPMC.

The basis of the model is the distributed model of an IPMC proposed by Kanno et al. in 1996 [9]. Originally Kanno divided a piece of an IPMC into ten similar segments and modelled the relation between the input current and tip displacement. Dividing the same piece into an infinite number of infinitesimally short similar segments, gives an RC transmission line. The resulting distributed RC line represented by a series of equivalent circuits with discrete elements is depicted in Fig. 6. The transient behavior of electrical signals, for instance voltage, electric current, charge, etc. along this kind of lines can be described with PDE-s implementing the proper boundary conditions.

Fig. 6. The distributed RC line describing IPMC, represented by a series equivalent circuits with discrete elements.

Several authors have modelled the mechanical behavior of IPMC as the bending of a bilayer beam [Mitu_viidet]. The foundation of the theory of mechanical bending of bilayer actuators was established by Timoshenko in 1925 with his analysis of bi-metal thermostats [Timoshenko] and elaborated by several authors [Suhir, jt.]. The described models of thermostats assume that the bi-metal strip is uniformly heated and the bending moment, causing the buckling of the strip, is uniform. Simlarily in the models of IPMC the electrical equivalent circuit is supposed to be a lumped and the voltage along the actuator is supposed to be constant.

In principle, there exists a yet another analogy between the bi-metal thermostat and the IPMC - the transient propagation of energy along the material. It is well-known, that a variety of mechanical, acoustic, or thermal systems exhibit characteristics very similar to those of electric filters or distributed lines and therefore can be treated by the same mathematical methods [Weber]. This similarity was put up already by Georg Simon Ohm. He reasoned by establishing an analogy between the Fourier's theory of heat flow and that of electricity. In his scheme the temperature and the voltage correspond as do the heat flow and the electrical current [RemarkablePhysicists]. According to this theory, the voltage along a lossless RC line behaves alike the temperature along a thermally insulated rod. The lossy RC line is the counterpart of the problem of heat flow along a thermally non-insulated homogeneous rod.

Following this theory we see a conspicuous similarity between the bi-metal thermostat and the IPMC actuator. The IPMC actuator in a cantilever configuration - a bending strip having the input contacts at one tip - is the counterpart of a bi-metal strip thermostat, attached to a heat exchanger with one tip only. The distinguished analogy between the two devices lies in the fact that the same PDE - the heat equation [PolyaninHandbook] - describes the heat flow along the metal rod of the thermostat as well as the propagation of voltage along the transmission-line-like structure of IPMC. The amount of bending of the bi-metal rod at each spot along its length depends on the instant temperature at that spot; the amount of bending of IPMC depends on the charge carried over at that spot, i.e. in principle on the instant voltage at that spot. The actual transient behavior of the particular device depends on the specific parameters of that device - heat conductance, thermal capacitance length, etc. in the case of bi-metal thermostat, and electrical conductance, electrical capacitance, length etc. in the case of IPMC. The behavior of both devices is affected by their mechanical parameters: dimensions, mass, moment of inertia, flexural rigidity, modulus of elasticity, etc.

Siia veel midagi!

The distributed model of IPMC represented by an infinite series equivalent circuits with discrete elements of infinitesimally short single units is given in Fig. 7. The conductivity of the electrodes of IPMC is represented by the series of resistances of the opposite electrodes  and , connecting the single units. Each single unit contains the electrical parameters determining the propagation of voltage along the transmission line and the elements for calculating the mechanical behavior of the actuator within the limits of that unit.

There are two fundamental causes of the electric current between the electrodes of an IPMC through the polymer matrix:

- The current caused by ionic conductivity. Relocating ions constitute the pseudocapacitance of the double-layer which forms at the interface between the ion exchange membrane and the metal electrode [18]. As described hereinabove, the resulting irregular density of hydratized ions is the cause of bending of the IPMC. The resulting deformation of the IPMC is proportional to the total amount of relocated ions. In the equivalent circuit the pseudocapacitance is depicted as shunt capacitors  between the electrodes in each single unit. The conductivity  denotes the summarized transversal ionic conductivity of the electrodes and the ionomer.

- The current caused by electrochemical electrode reactions, for example electrolysis of the solvent. The electrode reactions appear only if the voltage between the electrodes exceeds some certain critical level, depending on the materials used. The presence of the electrode reactions wastes energy and affects the propagation of voltage, but does not have direct effect on the deformation of the IPMC. In the equivalent circuit the electrode reactions are depicted as shunt resistors  between the electrodes in each single unit.

The electric charge  determines the mechanical flexure  within the limits of the single unit. As the electric charge can be expressed as the derivative of the current with respect of the time, the total electric charge  carried over within each single unit is calculated as a integral of the current . Figuratively, each single unit of the RC transmission line contains a block composed of ammeter, measuring current  through the capacitance , an integrator in order to determine the charge moved over in the limits of that unit, and a function  describing the bending effect of the charge, moving to the electrode. In the simplest case the flexure is proportional to the charge and the block  contains , where  is is the coefficient for bending effect of the charge.

Fig. 7. The distributed model of IPMC.

### 4. The equations describing the distributed model of IPMC

The step response of a system is the output of the system when a unit step function is used as the input and is a common analysis tool used to determine certain metrics about a system. The step response of the distributed line depicted in Fig. 6. is solvable in an analytical form. On the other hand it is easy to verify the theoretical model by applying the step voltage to the input of the IPMC actuators, describing their electromechanical response and measuring the transient behavior of the electrical parameters.

In this section we give the equations describing the transient behavior of the voltage  for the distributed line of a finite length  depicted in Fig. 6. when a voltage step is applied to its input. The derivation of the PDE and the procedure of applying the inital and boundary conditions is described in detail in [RcgwLine]. We give only the short overview and the relevant equations in the current paper.

First, we transfer the line depicted in Fig. 6. into the Cauer form [CircFiltHandbook] by replacing the two resistances  and  by their sum . The resulting line is depicted in Fig. 8.

Fig. 8. The Cauer canonical form of the line depicted in Fig. 6.

As shown in Fig. 9 , the parameters  and  are the resistance of the conductive layer and the capacitance of the dielectric per unit length of the line, respectively. The loss parameters  and  are the transversal conductivities per unit length along the line. For visual clarity in Fig. 9 the parameters ,,, and , all defined per unit length along the coordinate , are represented as the discrete elements of a single cell of the line. The voltage checkpoints and the selected positive directions of the currents are indicated by the arrows. We assume that all these parameters are uniform and time-invariant. The voltages and the currents are assumed to be functions of the coordinate along the line and the time, i.e. , , , , and .

Fig. 9. The meaning of the line parameters, voltages and currents for the distributed line.

In the next subchapters we give separately the equations describing the behavior of voltage, charge, water carried over and bending radius.

4.1. Equations for voltage

The variation of current along the coordinate  is equal to the sum current through the chains “” and “”:

,

where .

The variation of voltage along the coordinate  is equal to the voltage drop on resistance :

.

The current  charging the capacitance  is given by

.

Voltages in the chain  add up to the line voltage:

.

Now we have 4 equations with 4 unknown variables: , ,  and . After some math we get the PDE describing the transient behavior of the voltage  along the line in the form

.

This equation can be easily solved by a method called the separation of variables. The general solution of the PDE  for is

,

where and  are arbitrary constants, whose values are determined from the boundary conditions.

It is obvious that after a long time under constant input voltage the transients fade out and a steady, time-independent voltage distribution, denoted by , forms on the line. As it can be inferred form Fig. 8 and Fig. 9., in the steady limit case the current through the capacitance  is ceased, , and the voltages  and  are equalized, . The steady current through the distributed resistive network, formed by  and , still remains. This results in a diminishing voltage along the line.The equation describing the steady voltage distribution is

.

By applying the condition of the input voltage  at , , and the open end condition,  or , to its general solution  we find that

.

The initial/boundary conditions can be applied to the equation  using the method of Fourier series. This procedure is thoroughly described in [RcgwLine]. In the current paper we give the analytical solutions for the two distinct cases of practical importance:

- the step voltage of amplitude is applied to the input of the initially discharged line;

- the shorted input to the line that has been under the input of voltage of amplitude  until the steady distribution is formed.

The initial and boundary conditions for the two cases are given in the Table1.

Table1.

|  | a) | b) | condition |
| --- | --- | --- | --- |
| initial voltage distribution |  |  |  |
| input voltage at |  |  |  |
| steady voltage distribution |  |  |  |

In general, the voltage-step response of the distributed lines of length  depicted in Fig. 8. can be expressed as

,

where

,

and where , , , and  are the eigenfunctions, eigenvalues, Fourier coefficients, and the steady voltage distribution respectively. All these quantities depend on the initial/boundary conditions. Applying the boundary conditions for our two cases, we get that the solutions for voltage are:

- ;

- ,

where

.

4.2. Equations for charge, currents, and hydraulic pressure

As described hereinabove, the mechanical flexure of the actuator  is determined by the transitory charge  of the capacitance . The charge  can be derived from the equation . Since the charge  of the capacitance  and the voltage  relate as ; and the charge  relates to the current  as , we can write

.

Solving  for  gives

,

where  is the constant of integration. From the boundary conditions we find that equals to the distribution of charge corresponding to the steady state voltage . The steady state charge  can be found from . When the voltage transients have been faded out,  and

,

where  is defined by  and for our two cases can be found from Table1.

The distribution of electric current between the opposite electrodes can be derived from . By means of the bending movement of IPMC it can be devided into two parts. The current producing movement  is derived from  as

.

is the useless waste of energy, but it also determines the distribution of voltage. The expression of  follows from  or  as

.

The total input current  of the sample is determined by all currents over the full length of the distributed line:

The bending movement of IPMC is produced by the hydraulic pressure caused by the moving hydratized charge. In the simplest case the amount of water carried over by the migrating cations is proportional to the charge:

,

where  is the coefficient of hydratization of the cations.

Several authors have described the slow back-relaxation of the IPMC actuators after the quick response to the applied voltage [Bao, Mõni_veel]. This phenomenon is explained with the water leakage resulting from a high-pressure layer near the cathode toward to the anode through channels in the polymer backbone. The research of the effect of relaxation and developing the equation for the hydraulic pressure considering the back-relaxation, suitable for the distributed model of IPMC is the subject of our future work.

4.3. Equations for bending radius

The derivation of the relation between the curvature of the swollen polymer matrix and the charge carried over is described in [Berry]. The equations are derived to similarily to that employed by Timoshenko in his work on bi-metallic strips [Timoshenko]. Actually [Berry] describes the method of determining the coefficient of moisture swelling of polymers by their bending curvature. In our model of IPMC we use the result conversely - determine the bending curvature from the nonuniform concentration profile of water.

Fig. 10. Self-induced bending of a polymer strip caused by the water concentration profile  through the polymer layer.

Assuming that the polymer is isotropic and swells in volume V proportionally to a uniform water concentration , we may write

,

where  is a hygroscopic strain analogous to a thermal expansion strain of the bi-metal thermostats, and  is a linear swelling parameter equal to one-third of the volumetric swelling factor:

A nonuniform concentration profile of water through the thickness (z-coordinate) of the strip will produce elongation, bending and internal stress. With the assumption that plane cross-sections remain plane, the stress  is given by

,

where  denotes ,  and  are Young’s modulus and Poisson ratio of the polymer layer,  is the strain at midplane , and  is the radius of curvature. Since the polymer layer is under no external forces, we can write

Ma ei mäleta praegu kust see 12 sinna tuleb!

where for convinience we introduced the dimensionless coordinate .

Assuming that concentration profile of water through the thickness (z-coordinate) of the strip is linear: , the equation  simplifies to

Siin on mul nüüd mingi segadus. Kardan et K ja k tähistavad mitut asja! Kas tuleb artikli algusse teha tabelina valemites kasutatavate suuruste nomenklatuur?

5. Estimation of the parameters.

The values of the resistances of the both surface electrodes can be measured using a four-probe system. This method eliminates inexactnesses caused by the inconsistent current density and the resistances of the contacts [4].

The values of the parameters ,  and  can be determined using impedance spectroscopy with voltage step pulses as follows. A small piece of the IPMC material is wholly fixed between contact clamps made of gold. In this configuration the resistance of the electrodes does not influence the results. The typical response of electric current corresponding to a long-lasting step voltage input is depicted in Fig. 8. Electric current peaks sharply at the very first moment (instant A). After charging the whole pseudocapacitor, electric current remains at a stable level (instant B).

Fig. 8. Response of the electric current to a rectangular voltage pulse.

This behaviour of current can be explained by analysing the equivalent circuit illustrated in Fig. 9. At the very first moment, when the capacitor  is totally discharged, the current flows through the parallel resistances  and  (instant A). When the capacitance  is totally charged, the current flows through resistance  only (instant B). The capacitance can be found from the decay of the electric current.

Fig. 9. Estimation of the resistances  and .

7. Verification of the model

The experiments show that the electromechanical responses of the different types of IPMCs are different. Some materials bend faster, some slower; some have almost constant bending radius, some bend non-uniformly. In order to demonstrate the validity of the distributed model of IPMC in the case of different materials, we compare the results of the experiments carried out with two fundamentally different IPMC materials manufactured in Tartu University Institute of Technology and the simulations of the distributed model of the IPMC using the estimated parameters. We give the parameters of the samples of both materials measured using the methodology described in Chapter 5, and present the graphs of voltage and bending movement as described in Chapter 2. Simultaneously we simulate the same graphs by the equations given in Chapter 4. using the measured parameters and compare the measured and simultaed behaviors of the samples.

The IPMCs represented in the current paper are:

- Sample1 - an IPMC covered with platinum electrodes using the method of electroless deposition;

- Sample2 - an IPMC covered with gold electrodes using the direct assembly method.

The parameters of the samples measured using the methodology described in Chapter 5 are given in the table below:

| sample | dimensions (mm) | thickness of ionomer (μm) |  |  |  |  |  | cations |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1. | 10 x 35 | 250 | 9 | 5 | 1 | 0.0005 | 0.02 | Li+ |
| 2. | 10 x 35 | 180 | 0.5 | 0.5 | 0.015 | 0.0001 | 0.02 | Li+ |

Sample1 is made of 0.25 mm thick Nafion membrane and covered with platinum electrodes using the method of electroless deposition. It is a water-containing IPMC, intended to work in a wet environment. The cations introduced to the ionomer were Li+. This material is thick, hence more stiff than the other material. The thicker material contains potentially more cations, thus it has relatively big pseudocapacitance. The resistance of the electrodes of this sample is rather high, but still good enough to ensure conductivity. The nonuniform behavior of this sample is considerable due to the high resistance of the electrodes. The value of the conductivity  (see Fig. 7.) is relatively high. When the applied voltage is lower than the voltage required for the electrolysis of water, the value of is very low - in the range of about . When the applied voltage is close to the voltage required for the electrolysis of water, the conductivity  gains sharply up to about .

The experimental results of the electrical measurements and the electromechanical response of the Sample1 are depicted in Fig. 5. and Fig. 6. respectively.

The simulations of the Sample1 are given in Fig. 10. The graphs demonstrate that voltage increases rapidly close to the input contacts and more slowly further away from the input contacts (Fig. 9.-A). The electric current between the electrodes peaks sharply near the input contacts during the first few milliseconds of the input pulse, and then decreases rapidly to almost zero towards the free end of the sample.

It is not possible to measure directly the distribution of electric current through the sheet. This data can be only derived from the simulations, see . The distribution of current depicted in Fig. 9.-B produces the bending motion of the sample depicted in Fig. 9.-C. The graph exhibits that the actuator performs a sharp movement only close to the input contacts. The noticeably weaker change of the curvature of the free end appears after a short delay. The behavior of the voltage and the flexure are rather similar to the parameters obtained by the measurements of a real actuator and presented in Fig. 5. and Fig. 6. respectively.

A				B				C

Fig. 10. Simulations of Sample1. A – voltage, B – current, C – charge. The “Position” axis stands for the relative coordinate starting from the input contacts.

Sample1 exhibits insistent back-relaxation. As seen from Fig. 6, already in a half second after the beginning of the input pulse. As we have no model for relaxation yet, we give here only the graphs.....

The Sample2 is an ionic liquid containing IPMC made of 0.18 mm thick Nafion membrane. It is covered by a thin layer of RuO2 powder and gold foil electrodes glued to the ionomer with the dilution of nafion. This material is intended to work in air. The conductivity of the surface of the gold electrodes of that material is very high, however the poor conductivity of the RuO2 layer between the gold foil and the ionomer creates high value of . The large surface area of the RuO2 powder supposedly creates large pseudocapacitance of the IPMC material. The ionic liquid used was .... and the cations introduced to the polymer were Li+ .

Due to the pure conductivity of the RuO2 layer between the gold electrode and the ionomer the ionic current inside the ionomer cannot grow fast. For that reason the voltage drop along the electrodes is imperceptible and the IPMC has nearly a constant bending radius as depicted in simulations in Fig. 14. As electric current between the electrodes cannot grow, this IPMC is slow. It gains its maximal flexure in minutes.

Fig. 11. Measured mechanical response of Sample2.

Sample2 performs a slow bending movement with almost uniform bending radius over its full length. During the 8 sec input voltage pulse it almost reaches the steady state. During the pulse the voltage along the sample is near to the uniform distribution, so that the drop of voltage occurs on the conductivity W.

The simulations of the charge, carried over , calculated according to   in the course of applied voltage and in the course of relaxation after the shorting of the input contacts are depicted in Fig. 12.

The distribution of current between the opposite electrodes is depicted in Fig. 12-B. While in the case of the nonuniform bending of Sample1 the current peaked only for a very short time near the contacts only, see Fig. 11-B, the current of Sample 2 remains almost uniform along its full length for a long time, producing uniform bending.

A				B				C

Fig. 12. Simulations of Sample2. A - charge during the step voltage input; B - current during voltage input;  C - charge during relaxation.

5. Conclusions and future work

The presented distributed one-dimensional model of an IPMC consists of a number of lumped models coupling them with a spacial parameter – a generally uneven distribution of voltage caused by the resistance of the electrodes. It shows a good correlation with the experimental data obtained from the measurements conducted with the different IPMC materials. Its advantages with respect to the previous models are:

- it permits modeling the non-uniform flexure of the IPMC actuator in spatial and time domain.

- it permits modeling large flexure of the actuator or sensor.

- it takes into account the real measurable parameters of the material – resistance of the electrodes and capacitance and with respect to the previously developed models does not reduce it to a uniform lumped model;

- it is scalable, i.e. the length of the actuator is one of the parameters of the model;

- the values of the measurable parameteres - the capacitance of the material, the resistance of the electrodes and the length; - may vary in a large scale.

The model described in the current paper gives the analytical solution for the free bending of the IPMC actuators only. It does not take into account the mechanical parameters of IPMC membranes, for example the viscoelasticity of polymer membranes, the blocking force produced by the IPMC actuator, inertia, etc. Presumably the combination of the electrical distributed model and the theory of mechanics of multilayer elastic thin films would give a result, capable to express the force produced by arbitrary segment of the actuator.

IPMC materials are also known to have sensor properties, When the material is mechanically deformed, it generates a weak voltage between the faces of the IPMC sheet due to the change of the concentration of ions. According to (2) voltage at output contacts depends on time and distance between the bending area and the output. If the deformation is continuous or distributed, the values of  should be superpositioned. Verification of the proposed model for IPMC sensors is a subject of our future work.

8. Acknowledgements

This work has been supported by Estonian Ministry of Education, European Science Foundation, Estonian Science Foundation grants No. 6765, 6785 and 6763 and by Estonian Information Technology Foundation.

References

- M. Shahinpoor, “Ionic polymer-conductor composites as biomimetic sensors, robotic actuators and artificial muscles – a review”, Electrochimica Acta 48 (2003), pp. 2343-2353

- M. Shahinpoor, K. J .Kim, “Ionic polymer–metal composites: IV. Industrial and medical applications”, In Smart Materials and Structures, No. 14, Institute of Physics Publishing, 2005, pp. 197-214.

- C. S. Kothera, “Characterization, Modeling, and Control of the Nonlinear Actuation Response of Ionic Polymer Transducers”, Ph.D. dissertation, Dept. of Mechanical Engineering, Virginia Tech, 2005.

- S. Nemat-Nasser, C. W. Thomas, Ionomeric polymer–metal composites, in: Y. Bar-Cohen (Ed.), Electroactive Polymer (EAP) Actuators as Artifical Muscles. Reality, Potential, and Challenges, SPIE Press, Washington, 2001

- K. Asaka, K. Oguro, „Bending of Polyelectrolyte Membrane-Platinum Composites by Electric Stimuli. Part II, Response Kinetics”, J. Electroanal. Chem, Vol. 480, pp.186-198, 2000

- S. Tadokoro, T. Takamori, K. Oguro, “Modeling IPMC for Design of Actuation Mechanism” in: Y. Bar-Cohen (Ed.), Electroactive Polymer (EAP) Actuators as Artifical Muscles. Reality, Potential, and Challenges, SPIE Press, Washington, 2001

- K. Mallavarapu, D. Leo, “Feedback Control of the bending response of ionic polymer actuators,” Journal of Intelligent Material Systems and Structures, vol. 12, no. 3, pp. 143–155, 2001

- R. Kanno, S. Tadokoro, M. Hattori, T. Takamori, K. Oguro, „Modeling of ICPF Actuator, Modeling of Electrical Characteristics” Proc. In IEEE 21st Intl Conf. On Industrial Electronics, Control, and Instrumentation, Vol. 2, pp. 913-918, 1995

- R. Kanno, S. Tadokoro, T. Takamori, M. Hattori, K. Oguro, “Linear approximate dynamic model of an ICPF actuator”, Proc. IEEE Intern. Conf. on Robotics and Automation, Vol. 1, pp. 219-225, Minneapolis, Apr. 1996

- C. Bonomo, L. Fortuna, P. Giannone, S. Graziani and S. Strazzeri, „A nonlinear model for ionic polymer metal composites as actuators”, Smart Mater. Struct. 16 1-12, 2007

- K. Newbury, D. Leo, „Linear Electro-mechanical Model of Ionic Polymer Trans-ducers – Part I: Model Development”, Journal of Intelligent Material Systems and Structures, vol. 14, no. 6, pp. 333–342, 2003

- X. Bao, Y. Bar-Cohen, S. Lih, “Measurements and Macro Models of Ionomeric Polymer-Metal Composites (IPMC),” EAPAD Conference 2002, Proc. SPIE 4695, pp. 286-293, 2002

- W. Yim, M. B. Trabia, J. M. Renno, “Dynamic Modeling of Segmented Ionic Polymer Metal Composite (IPMC) Actuator,” Proc. IEEE/RSJ Int. Conf. on Intelligent Robots and Systems, 2006

- K. Jung, J. Nam, and H. Choi, “Investigations on actuation characteristics of IPMC artificial muscle actuator,” Sensors and Actuators A: Physical, Vol. 107, No. 2, 2003, pp. 183–192.

- D. Bandopadhya, D. Bhogadi, B. Bhattacharya, A. Dutta, “Active vibration suppression of a flexible link using ionic polymer metal composite, IEEE Conference on Robotics, Automation and Mechatronics, Bangkok, 2006.

- R. C. Richardson, M. C. Levesley, M. D. Brown, J. A. Hawkes, K. Watterson, P. G. Walker, “Control of ionic polymer metal composites,” IEEE/ASME Transactions on Mecatronics, Vol. 8, No. 2, 2003, pp.245–253.

- J.-D. Nam, J. H. Lee, J. H. Lee, H. Choe, K. J. Kim, and Y. S. Tak, “Water uptake and migration effects of electroactive IPMC (ion-exchange polymer metal composite) actuator,” Sensors and Actuators A: Physical, Vol. 118, 2005, pp. 98–106.

- K. Sadeghipour, R. Salomon, S. Neogi, “Development of a novel electrochemically active membrane and “smart” material based vibration sensor/ damper,” Smart Materials and Structures, Vol. 1, pp. 172–179, 1992.

- V. B. Rao, Delay analysis of the distributed RC line, Proceedings of the 32nd ACM/IEEE conference on Design automation, p.370-375, June 12-16, 1995

- V. Szekely, "Distributed RC Networks," in " The circuits and filters handbook. 2nd ed." Wai Kai Chen (ed) 2003

- B. Akle, S. Nawshin, D. Leo, “Reliability of high strain ionomeric polymer transducers fabricated using the direct assembly process”, Smart Mater. Struct. 16 (2007) S256–S261

- M. Shahinpoor and K. J. Kim, “Ionic polymer–metal composites: II. Manufacturing techniques,” Smart Mater. Struct. 12, 2003, pp. 65–79.

- A. Punning, M. Kruusmaa, A. Aabloo, “Surface resistance experiments with IPMC sensors and actuators”, Sensors and Actuators A: Physical, Vol. 133, Issue 1, 2007, pp 200-209

- E.N. Protonotarios, O. Wing, “Theory of nonuniform RC lines – part I: analytic properties and realizability conditions in the frequency domain,” IEEE Trans. Circuit Theory, vol. CT-14, 1967, pp. 2–12.

- E.N. Protonotarios, O. Wing, “Theory of nonuniform RC lines – part II: analytic properties in the time domain,” IEEE Trans. Circuit Theory, vol. CT-14, 1967, pp. 13–20.

- E.N. Protonotarios, O. Wing, “Computation of the step response of a general nonuniform RC distributed network,” IEEE Trans. Circuit Theory, vol. CT-14, 1967, pp. 219–221.