Molecular Dynamics simulations of EMI-BF4 in nanoporous carbon for electroactive polymer actuators.

Authors: Endel Soolo, Anti Liivat, Heiki Kasemägi, Daniel Brandell, Tarmo Tamm, Alvo Aabloo

# Abstract

# Introduction

Electroactive polymers (EAP) are materials which change their shape in response to electric stimulation, and are therefore useful as lightweight actuators in for example space industry [Bar-Cohen-1999, Bar-Cohen-2001] and medicine applications [Bar-Cohen-2001], or biomimetic robotics [Mart, Liu-2008]. EAPs can generally be divided into two basic categories: ionic and electronic EAPs. Ionic EAPs act by ion/ionpair relocation during actuation, similar to supercapacitors. They are better suited for miniature devices, since they can be operated under low voltage (1-10V) [eapbook]. However, most ionic EAPs offer only small force, display low electromechanical efficiency and have short lifetime compared to traditional electromechanical actuators. Several practical solutions have been proposed to improve the total actuator force; e.g., designing specific shapes [Wang] or bundling multiple actuators [Fernandez]. In order to increase the efficiency, however, it is vital to understand the details of the actuation process and the ion migration at atomistic level [eapbook].

Ionic EAP materials are composed of three basic components: a porous electrode material (often carbon), an ionic transfer media and a polymer binder which adds toughness and flexibility. Several types of micro-porous carbon composite materials have been used in supercapacitors, where charges accumulate in a double layer on a large surface area. It has been claimed [Hoefer] that Carbide Derived Carbon (CDC) capacitor capacitance is mainly determined by two components: electrostatic/double layer capacitance [Brett] and faradaic/pseudocapacitive components [Conway]. Pore diameters smaller than 1 nm result in even higher capacitance due to larger surface area and confinement effects [Huang]. CDCs are one of the best known nanoporous materials for ion storage, since the pore-size is uniform and can be fine-tuned in a wide range [Gogotsi]. Ionic liquids (ILs) are frequently used as ion transfer media. ILs, or molten salts, consist of charged particles without solvent. Due to their low vapor pressure, ILs avoid evaporation of the electrolyte when functioning in a dry environment. IL electrolytes can also improve the cycle lifetime of the material compared to water based electrolytes [biomedbook]. The EAP actuator comprise two electrode sheets of the above mentioned components laminated together, with an ion permeable membrane in between, impregnated with electrolyte.

Different kinds of ion storage, ion transport medium, binder and membrane materials offer countless possibilities to experiment with. For example, IL electrolytes in Nafion membranes have been tested with metal [Bennett], carbon nanotubes [Akle], CDC [Viljar] or RuO2 [Akle, Viljar] electrodes. CDC in a polytetrafluoroethylene (PTFE) matrix has also been used as electrodes, in combination with an IL electrolyte and an ion permeable paper membrane [Janno]. Asaka et al. [Asaka-2005, Asaka-2008] have studied carbon bucky gel actuators, where the electrodes contains carbon nanotubes in different ILs, supported by polyvinylidene fluoride (PVDF)-based binders [Asaka-2005]. The largest strain was achieved by using 1-ethyl-3-methylimidazolium tetrafluoroborate (EMI-BF4) as the IL [Asaka-2008]. Carbon nanotube sheets have also been demonstrated to work as actuators in water based electrolytes [Baughman-1999].

The EAP bending motion is caused either by electrode or membrane expansion at one side of the device and/or contraction at the other side, upon actuation. The mechanisms causing the expansions and contractions are still to a large degree unknown and debated [Kiyohara]. Suggestions include bond length changes due to repulsive Coulomb forces  accompanying double layer charging [Baughman-1999], insertion of counterions [Baughman-1995], electro-osmosis [Asaka-1995], electrostatic repulsion of the charged molecules in the material [Baughman-1999], decreased interfacial tension at the pore surfaces due to change in double-layer charges [Oren], etc.

A correlation has been found between increased accumulation of ions on the electrode surface (i.e., the capacity) and improved peak strain [Akle], but that result was seen to be dependent on electrolyte type [Janno]. Considering the large influence from the choice of IL or the type of carbon on the EAP performance [Janno, Viljar], the primary factor for strain ratio and maximum strain seems to be the ionic transport rather than changes in electronic configuration. When comparing EAPs with 1-ethyl-3-methylimidazolium trifluoromethanesulfonate  (EMI-TF)-based electrolyte with those with  tetraethyl ammonium tetrafluoroborate (TEA-BF4)-based electrolyte which has larger effective ion size due to ions moving in pairs, the EMI-Tf with its smaller ions can generate larger strains and has larger capacitance [Janno]. Increasing the ion mobility would, therefore, significantly help in  increasing both the strain ratio and the maximum strain of EAPs [biomedbook].

Several approaches can be used for optimizing ionic conductivity. It is general knowledge from the field of battery polymer electrolytes that changing the monomeric sequence [ref.req.], adding plasticizers [Dias] or nano-particle fillers [Ahmad] all have proven successful strategies. In this study, the charge on the electrodes is varied and the ionic transport studied with Molecular Dynamics (MD) simulation techniques. The usefulness of MD simulations is in the detailed view it renders of the ion movement processes, and it has been used to study polymer electrolytes [Heiki, Daniel, Anti, Borodin, etc].

For most electrolytes, ion mobility is directly related to the diffusion coefficient through the Einstein relation. However, this does not apply for ILs. Instead, the change of ionic orientation in an electric field can increase the ion mobility by several orders of magnitude compared with the values estimated from diffusion coefficient [Umecky].

# Methodology

The method of Molecular Dynamics (MD) is based on step-wise calculations of the forces acting on each atom within a fixed model. This force field is composed of bond stretchings, bond angle vibrations, dihedral angle torsion rotations, van der Waals forces, and electrostatic interactions. The net force acting on an atom from all other particles in the system, together with its current position and velocity are used to calculate its position at the next time-step. This generates trajectories of all the particles in the model. By continuously sampling the atomic coordinates, diffusion coefficients and other macroscopic characteristics can be estimated, while transport mechanisms also can be analyzed on a more subtle molecular level. [Rapaport]

In this work, the simulation results were generally analyzed by Radial Distribution Functions (RDFs) and Coordination Numbers (CNs), while Space Distribution functions [Liu-2004] were used to find the coordination sphere radii and the most frequent interaction sites for ions and molecules.

## Simulated systems

Experimentally, the IL content is determined from the saturation concentration of the electrode material. In an MD simulation, on the other hand, the amount of each component must be controlled directly. To gain insight in the dynamical behaviour of the actuator and the ion conduction mechanism, the charge stored in the CDC carbon was varied and the anion-cation ratio was also adjusted  to maintain the neutrality of the simulation cell. The carbon to IL (here: EMI-BF4; the molecular structure and atom labels used are  represented in Fig. 1) ratio was also varied, in the proximity of experimentally estimated values[Janno, Arulepp]. The polymer binder was not included in the simulation.

The components were inserted into four different MD simulation boxes according to Table 1, containing:

- Carbon in the form of curved graphene-like flakes with 24 to 27 cycles each, used as a model for CDC. This form was used, because fully amorphous carbon with no long-range structural order has the largest surface area of the CDC variety [Leis].

- 1-Ethyl-3-methyl-imidazolium (EMI+) cations

- Boron tetrafluoride (BF4-) anions

Table 1: Simulated systems

| System nr. | IL:Carbon mass ratio | Carbon | EMI+ cations | BF4- anions | Cell size | Density |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | mass-% | No. of flakes | Flake charge | mass-% | No. of cations | mass-% | No. of anions | (Å) | (g/cm3) |
| 1 | 1.89 | 34.6 | 24 | +2 | 32.6 | 165 | 32.8 | 213 | 41.12 | 1.34 |
| 2 | 1.89 | 34.6 | 24 | 0 | 36.7 | 186 | 28.7 | 186 | 41.47 | 1.31 |
| 3 | 1.89 | 34.6 | 24 | -2 | 40.9 | 207 | 24.5 | 159 | 41.75 | 1.28 |
| 4 | 1.13 | 47.0 | 24 | 0 | 29.8 | 111 | 23.3 | 111 | 42.38 | 1.33 |
| 5 | 1.13 | 46.9 | 24 | +2 | 18.5 | 69 | 34.6 | 165 | 50.0* | 0.81* |
| 6 | 1.13 | 47.0 | 24 | -2 | 41.1 | 153 | 11.9 | 57 | 50.0* | 0.81* |
| 7 | 1.55 | 39.2 | 48 | 0 | 34.1 | 305 | 26.7 | 305 | 50.0* | 1.32* |

## Construction of simulation cells

The nanoporous amorphous CDC carbon consists of graphene-like sheets without long-range ordering [Palmer]. Therefore, separate slightly curvedt graphene flakes were used to create a similar structure. The individual shapes of the flakes were initially created in planar form by putting together 6-member carbon rings with occasional 5-member rings (defects). The energy of the flakes was minimized by MD simulations in vacuo and the defects caused the flakes to curl up. The number of carbon rings in each flake was between 24 and 27, up to 3 of which were 5-sided. An example of the shape the carbon flakes take after simulation in vacuo is depicted in Fig. 2.

The amorphous structure of the simulated material was generated with Monte Carlo methods, using  in-house software [mcgen]. The carbon flakes, cations and anions were rotated in rigid body manner and sequentially inserted in random locations where the atoms would not coincide with each other until the required density was achieved. In cases where the process reached a standstill before the required density, another process was also used: all possible coordinates at regular intervals were tested and then the ions were inserted at each of the available locations without rotation.

The models were created in cubic simulation boxes measuring either 40×40×40 Å or 50×50×50 Å with periodic boundary conditions. The model with neutral carbons was created first. For charged carbons, the configuration of the carbon flakes was left the same, but their partial atomic charges were changed. To maintain the neutrality of the simulation cell,  some ions of  the same charge were removed and the  respectivecounterions inserted using the same methods as before. The cations are significantly larger than anions, so additional ion pairs were inserted or removed to keep the total mass of IL invariant of the charging of carbons (Table 1).

## Force fields

The force field used was a combination of quantum chemical  calculations with force fields found in literature. The partial charges  for carbon and hydrogen atoms were calculated for each charge (0, +2 or -2) and for each type of the carbon flake (with different number and location of defects) using PM6 [PM6] semi-empirical optimization method with open shells (UHF). The exact values are in appendix X . An example of the charges is represented in Fig. 3.

Parameters for bonded interactions between carbon atoms within the carbon flakes were taken from [Walther]. Hydrogen atoms were attached to the edges of the carbon flakes in order to saturate valences  using parameters from [AMBER].

The EMI-BF4 interactions were taken from Lopes et al. [Lopes]. Van der Waals forces between atoms with force fields originating from separate sources were calculated by using standard combination rules (1) for the Lennard-Jones potential (2) parameters of each atom pair (1 and 2 subscripts denote Lennard-Jones parameters of the atom types):

(1)

(2)

All force field parameters are presented in Appendix 1.

## Simulation details

Each system was first equilibrated by a 2 ns long MD simulation using the NVT ensemble in the original 40 Å cubic cell to relieve internal stresses left from the generation. Then a 10 ns long simulation followed with NPT ensemble, using Nose-Hoover barostat with the pressure of 1 atm and  relaxation time of  0.3 ps. Some additional simulations were done with 50 Å initial box. In those cases the NPT simulation was omitted and only the results from NVT simulations were compared with the results from simulations done with the smaller box in order  to determine that the box was large enough already and no additional effects would appear when it is increased.

The simulations used a Verlet leap-frog algorithm with 1 fs timestep. Temperature was kept at 293 K by a Nose-Hoover thermostat with 0.1 ps relaxation time. Ewald summation with 10-5 precision was used for all electrostatic interactions. The cubic symmetry of the simulation cell was retained in all simulations.

## Analysis methods

# Results

System description

The effect of IL:Carbon ratio

The effect of the electric field

Other effects

# Conclusion

# References

- [Bar-Cohen-1999] Y. Bar-Cohen, S. P. Leary, M. Shahinpoor, J. S. Harrison, J. G. Smith, Proc. SPIE, 3669, 57 (1999); doi:10.1117/12.349708  http://dx.doi.org/10.1117/12.349708

- [Bar-Cohen-2001] Y. Bar-Cohen, Proc SPIE Int Soc Opt Eng, 4329, 1-6, (2001); http://dx.doi.org/10.1117/12.432639

- [Mart] M. Anton, A. Punning, A. Aabloo, M. Listak, M. Kruusmaa, Towards Autonomous Robotic Systems (TAROS 2004), University of Essex, 1-7, (2004); http://www.essex.ac.uk/csee/research/publications/technicalreports/2004/csm415/Anton_etal.pdf

- [Liu-2008] Y. Liu, L. Shi, L. Liu, Z. Zhang, J. Leng, Proc. SPIE, 6927, 69271A, (2008); http://dx.doi.org/10.1117/12.775946

- [Spigna] N. Di Spigna, P. Chakraborti, P. Yang, T. Ghosh, P. Franzon, Proc. SPIE, 7287, 72871K, (2009); http://dx.doi.org/10.1117/12.816009

- [eapbook] Y. Bar-Cohen (editor), Electroactive Polymer (EAP) Actuators as Artificial Muscles: Reality, Potential, and Challenges, Second Edition (SPIE Press Book), ISBN: 9780819452979

- [Wang] H. Wang, C. Li, ICMTMA'09. International Conference on Measuring Technology and Mechatronics Automation, 1, 73-76, (2009); http://dx.doi.org/10.1109/ICMTMA.2009.114

- [Fernandez] D. Fernández, L. Moreno, J. Baselga, Proc SPIE Int Soc Opt Eng, 5759, 361, (2005);  http://dx.doi.org/10.1117/12.599108

- [Akle] B. J. Akle, M. D. Bennett, D. J. Leo, K. B. Wiles, J. E. Mcgrath, J. Mater. Sci., 42, 7031-41, (2007); http://dx.doi.org/10.1007/s10853-006-0632-4x`

- [Hoefer] M. Hoefer, P. R. Bandaru, Appl. Phys. Lett. 95, 183108 (2009); http://dx.doi.org/10.1063/1.3258353

- [Brett] C. M. A. Brett, A. M. O. Brett, Electrochemistry: Principles, Methods, and Applications (Oxford University, Oxford, 1993).

- [Conway] B. E. Conway, J. Electrochem. Soc. 138, 1539 (1991).

- [Huang] J. Huang, B. G. Sumpter, V. Meunier, Chemistry - A European Journal, 14, 6614 (2008); http://dx.doi.org/10.1002/chem.200800639

- [Gogotsi] Y. Gogotsi, A. Nikitin, H. Ye, W. Zhou, J. E. Fischer, B. Yi, H. C. Foley, M. W. Barsoum, Nature Materials, 2, 591 (2003); http://dx.doi.org/10.1038/nmat957

- [biomedbook] F. Carpi (editor), E. Smela (editor), Biomedical Applications of Electroactive Polymer Actuators, Wiley 2009, ISBN: 978-0-470-77305-5

- [Bennett] M. D. Bennett, D. J. Leo, Sensors and Actuators A, 115, 79 (2004); http://dx.doi.org/10.1016/j.sna.2004.03.043

- [Viljar] V. Palmre, D. Brandell, U. Mäeorg, J. Torop, O. Volobujeva, A. Punning, U. Johanson, M. Kruusmaa, A. Aabloo, Smart Mater. Struct. 18, 095028 (2009); http://dx.doi.org/10.1088/0964-1726/18/9/095028

- [Janno] J. Torop, M. Arulepp, J. Leis, A. Punning, U. Johanson, V. Palmre, A. Aabloo, Materials, 3, 9 (2010); http://dx.doi.org/10.3390/ma3010009

- [Asaka-2005] T. Fukushima, K. Asaka, A. Kosaka, T. Aida, Angew. Chem. Int. Ed. 44, 2410-2413, (2005); http://dx.doi.org/10.1002/anie.200462318

- [Asaka-2008] K. Asaka, K. Mukai, I. Takeuchi, K. Kiyohara, T. Sugino, N. Terasawa, K. Hata, Proc. SPIE, 7037, 703710 (2008); http://dx.doi.org/10.1117/12.794503

- [Baughman-1999] R. H. Baughman, C. Cui, A. A. Zakhidov, Z. Iqbal, J. N. Barisci, G. M. Spinks, G. G. Wallace, A. Mazzoldi, D. De Rossi, A. G. Rinzler, O. Jaschinski, S. Roth, M. Kertesz, Science, 284, 1340 (1999); http://dx.doi.org/10.1126/science.284.5418.1340

- [Kiyohara] K. Kiyohara, T. Sugino, I. Takeuchi, K. Mukai, K. Asaka, J. Appl. Phys. 105, 063506 (2009)

- [Asaka-1995] K. Asaka, K. Oguro, Y. Nishimura, M. Mizuhata, H. Takenaka, Polym. J., 27, 436 (1995); http://dx.doi.org/10.1295/polymj.27.436

- [Oren] Y. Oren, I. Glatt, A. Livnat, O. Kafari, and A. Soffer, J. Electroanal. Chem. Interfacial Electrochem. 187, 59 (1985); http://dx.doi.org/10.1016/0368-1874(85)85575-1

- [Dias] F. B. Dias, L. Plomp, Journal of Power Sources, 88, 169 (2000); http://dx.doi.org/10.1016/S0378-7753(99)00529-7

- [Ahmad] S. Ahmad, S.A. Agnihotry, Current Applied Physics, 9, 108 (2009); http://dx.doi.org/10.1016/j.cap.2007.12.003

- [Heiki] H. Kasemägi, M. Klintenberg, A. Aabloo, J. O. Thomas, Solid State Ionics, Volume 147, Issues 3-4, April 2002, Pages 367-375, http://dx.doi.org/10.1016/S0167-2738(02)00013-9

- [Umecky] T. Umecky, Y. Saito, H. Matsumoto, J. Phys. Chem. B, 113, 8466 (2009); http://dx.doi.org/10.1021/jp9043946

- [Han] Z. J. Han, R. Morrow, B. K. Tay, D. McKenzie, Appl. Phys. Lett. 94, 043118 (2009); http://dx.doi.org/10.1063/1.3077605

- [Yushin] G. N. Yushin, E. N. Hoffman, A. Nikitin, H. Ye, M. W. Barsoum, Y. Gogotsi, Carbon, 43, 2075 (2005); http://dx.doi.org/10.1016/j.carbon.2005.03.014

- [mcgen] E. Soolo, J. Karo, H. Kasemägi, M. Kruusmaa, A. Aabloo, Proc. SPIE, 6168, 61682A (2006); http://dx.doi.org/10.1117/12.658664

- [dlpoly] W. Smith, T. Forester, The DL_POLY Project,TCS Division, Daresbury Laboratory, Daresbury, Warrington, WA44AD, England

- [Hentscke] R. Hentschke, B. L. Schürmann, J. P. Rabe, J. Chem. Phys. 96, 6213 (1992)

- [Okada] O. Okada, K. Oka, S. Kuwajima, K. Tanabe, Molecular Simulation, 21, 325-342, (1999); http://dx.doi.org/10.1080/08927029908022072

- [Lopes] J. N. C. Lopes, J. Deschamps, A. A. H. Pádua, J. Phys. Chem. B, 108, 2038–2047, (2004); http://dx.doi.org/10.1021/jp0362133

- [webelements] http://webelements.com

- [Palmer] J.C. Palmer, A. Llobet, S.-H. Yeon, J.E. Fischer, Y. Shi, Y. Gogotsi, K.E. Gubbins, Carbon, 48, 1116 (2010); http://dx.doi.org/10.1016/j.carbon.2009.11.033

- [Rapaport] D. C. Rapaport, The Art of Molecular Dynamics Simulation, Second Edition, Cambridge University Press, 2004.

- [Niu] S. Niu, Z. Cao, S. Li, T. Yan, J. Phys. Chem. B, 114, 877 (2010); http://dx.doi.org/10.1021/jp909486z

- [Daniel] D. Brandell, H. Kasemägi, A. Aabloo, Electrochimica Acta, 55, 1333 (2010); http://dx.doi.org/10.1016/j.electacta.2009.04.070

- [Liu-2004] Z. Liu, S. Huang, W. Wang, J. Phys. Chem. B, 108, 12978 (2004); http://dx.doi.org/10.1021/jp048369o

- [Newkome] G. R. Newkome (Editor), Advances in dendritic macromolecules, vol. 5, 2002; ISBN: 0-7623-0839-7

- [Floris] F. M. Floris, J. M. Martínez, J. Tomasi, The Journal of Chemical Physics, 116, 5460 (2002); http://dx.doi.org/10.1063/1.1453957

- [Arulepp] M. Arulepp, J. Leis, M. Lätt, F. Miller, K. Rumma, E. Lust, A.F. Burke, Journal of Power Sources, 162, 1460 (2006); http://dx.doi.org/10.1016/j.jpowsour.2006.08.014

- [Janno-personal] Janno Torop, personal communication

- [Leis] J. Leis, A. Perkson, M. Arulepp, M. Kaarik, G. Svensson, Carbon 39, 2043 (2001)

- [PM6]  J. J. P. Stewart, J. Mol. Mod., 13, 1173-1213 (2007); http://dx.doi.org/10.1007/s00894-007-0233-4

# Comments

Ca1 ja Ce2 viivad mõtted pigem vastavalt kaltsiumi ja tseeriumi aatomitele, kas sellele oleks lahendus asendades Ca2 -> Ca2 ?

„Larger“  viitab ruumalale, edasi on jutt massist.  Võiks olla kooskõlas.

Kas jäi nii, et jõuväli ja optimaalne C-C kaugus laengust ei olenenud ?

page 167

# Text boxes

Figure 3: Partial charges of carbon flake type #7 with flake charge -2.

Figure 2: The shape of carbon flake type #2.

Figure 1: Atom labels used for the ionic liquid EMI-BF4