Molecular Dynamics simulations of EMI-BF4 in nanoporous carbon for electroactive polymer actuators.

Authors: Endel Soolo, Anti Liivat, Heiki Kasemägi, Daniel Brandell, Tarmo Tamm, Alvo Aabloo

# Abstract

# Introduction

Electroactive polymers (EAP) are materials which change their shape in response to electric stimulation, and are therefore useful as lightweight actuators in for example space industry [Bar-Cohen-1999, Bar-Cohen-2001] and medicine applications [Bar-Cohen-2001], or biomimetic robotics [Mart, Liu-2008]. EAPs can generally be divided into two basic categories: ionic and electronic EAPs. Ionic EAPs act by ion/ionpair relocation during actuation, similar to supercapacitors. They are better suited for miniature devices, since they can be operated under low voltage (1-10V) [eapbook]. However, most ionic EAPs offer only small force, display low electromechanical efficiency and have short lifetime compared to traditional electromechanical actuators. Several practical solutions have been proposed to improve the total actuator force; e.g., designing specific shapes [Wang] or bundling multiple actuators [Fernandez]. In order to increase the efficiency, however, it is vital to understand the details of the actuation process and the ion migration at atomistic level [eapbook].

Ionic EAP materials are composed of three basic components: a porous electrode material (often carbon), an ionic transfer media and a polymer binder which adds toughness and flexibility. Several types of micro-porous carbon composite materials have been used in supercapacitors, where charges accumulate in a double layer on a large surface area. It has been claimed [Hoefer] that Carbide Derived Carbon (CDC) capacitor capacitance is mainly determined by two components: electrostatic/double layer capacitance [Brett] and faradaic/pseudocapacitive components [Conway]. Pore diameters smaller than 1 nm result in even higher capacitance due to larger surface area and confinement effects [Huang]. CDCs are one of the best known nanoporous materials for ion storage, since the pore-size is uniform and can be fine-tuned in a wide range [Gogotsi]. For EAP applications, ionic liquids [Armand et al, Nature Materials, 8 (2009) 621] (ILs) are frequently used as ion transfer media. ILs, or molten salts, consist of charged particles without additional solvent. Due to their low vapor pressure, ILs avoid evaporation of the electrolyte when functioning in a dry environment. IL electrolytes can also improve the cycle lifetime of the material compared to water based electrolytes [biomedbook]. The EAP actuator comprise two electrode sheets of the above mentioned components laminated together, with an ion permeable membrane in between, impregnated with electrolyte.

Different kinds of ion storage, ion transport medium, binder and membrane materials offer countless possibilities to experiment with. For example, IL electrolytes in Nafion membranes have been tested in combination with metal [Bennett], carbon nanotubes [Akle], CDC [Viljar] or RuO2 [Akle, Viljar] electrodes. CDC in a polytetrafluoroethylene (PTFE) matrix has also been used as electrodes, in combination with an IL electrolyte and an ion permeable paper membrane [Janno]. Asaka et al. [Asaka-2005, Asaka-2008] have studied carbon bucky gel actuators, where the electrodes contain carbon nanotubes in different ILs, supported by polyvinylidene fluoride (PVDF)-based binders [Asaka-2005]. The largest strain was achieved by using 1-ethyl-3-methylimidazolium tetrafluoroborate (EMI-BF4) as the IL [Asaka-2008]. Carbon nanotube sheets have also been demonstrated to work as actuators in water based electrolytes [Baughman-1999].

The EAP bending motion is caused either by electrode or membrane expansion at one side of the device and/or contraction at the other side, upon actuation. The mechanisms causing the expansions and contractions are still to a large degree debated [Kiyohara]. Suggestions include bond length changes due to repulsive Coulomb forces  accompanying double layer charging [Baughman-1999], insertion of counterions [Baughman-1995], electro-osmosis [Asaka-1995], electrostatic repulsion of the charged molecules in the material [Baughman-1999], decreased interfacial tension at the pore surfaces due to change in double-layer charges [Oren], etc.

A correlation has been found between increased accumulation of ions on the electrode surface (i.e., the capacity) and improved peak strain [Akle], but that result was seen to be dependent on electrolyte type [Janno]. Considering the large influence from the choice of IL or the type of carbon on the EAP performance [Janno, Viljar], the primary factor for strain ratio and maximum strain seems to be the ionic transport rather than changes in electronic configuration. When comparing EAPs with EMI-trifluoromethanesulfonate (EMI-Tf)-based electrolyte with those using tetraethyl ammonium (TEA) BF4-based electrolyte, which has a larger effective ion size due to ion pairing, the EMI-Tf can generate larger strains and has larger capacitance [Janno]. Increasing the ion mobility would, therefore, significantly help increasing both the strain ratio and the maximum strain of EAPs [biomedbook].

Several approaches can be used for optimizing ionic conductivity. It is general knowledge from the field of battery polymer electrolytes that changing the monomeric sequence [ref.req.], adding plasticizers [Dias] or nano-particle fillers [Ahmad] all have proven successful strategies. MD simulations generate a detailed view of the ion movement processes, and has been frequently used to study electrolyte systems [Heiki, Daniel, Anti, Borodin, etc].

In this study, the properties and actuation mechanism of EAPs based on CDC carbon and EMI-BF4 IL are investigated with Molecular Dynamics (MD) simulation techniques. Changes in the microstructure are observed while varying the charge accumulated in the carbon part of the electrodes, in an attempt to explain the volume change leading to actuation and to search for possibilities of enlarging the peak strain and ion mobility.

# Methodology

The method of Molecular Dynamics (MD) is based on step-wise calculations of the forces acting on each atom within a fixed model. This force field is composed of the chemical interactions in the system: bond stretchings, bond angle vibrations, dihedral angle torsion rotations, van der Waals forces, and electrostatic interactions. The net force acting on an atom from all other particles in the system, together with its current position and velocity are used to calculate its position and velocity at the next time-step. This generates trajectories of all the particles in the model. By continuously sampling the atomic coordinates, diffusion coefficients and other macroscopic characteristics can be estimated, while transport mechanisms also can be analyzed on a more subtle molecular level. [Rapaport]

In this work, the simulation results were generally analyzed by Radial Distribution Functions (RDFs) and Coordination Numbers (CNs), while Space Distribution functions [Liu-2004] were used to find the coordination sphere radii and the most frequent interaction sites for ions and molecules.

## Simulation details

Each system was first equilibrated by a 2 ns long MD simulation in the NVT ensemble at 293 K temperature in the original 40 Å cubic cell to relieve internal stress originating in the generation. Thereafter,  a 10 ns long simulation followed in the NPT ensemble at 293 K temperature, using a Nose-Hoover barostat with 1 atm pressure and  a relaxation time of  0.3 ps.

The simulations used a Verlet leap-frog algorithm with 1 fs timestep. Temperature was kept at 293 K by a Nose-Hoover thermostat with 0.1 ps relaxation time. Ewald summation with 10-5 precision was used for all electrostatic interactions. The cubic symmetry of the simulation cell was retained in all simulations.

## Simulated systems

Nanoporous amorphous CDC carbon consists of graphene-like sheets, for which the amount of long-range ordering depends on the quenching rate [Palmer]. The fully amorphous forms without any long-range structural order have the largest surface area [Leis], which was also chosen for this study. The structure was approximated by Separate slightly curved graphene flakes of similar sizes, small enough to allow the charge distribution to be calculated by QC.

To gain insight into the dynamical behaviour of the actuator and the ion conduction mechanism, the charge of the CDC carbon was varied between +2, 0 and -2 unit charges per carbon flake, whereafter the anion-cation ratio was adjusted to maintain electroneutrality.

The carbon to IL (here: EMI-BF4; the molecular structure and atom labels used are presented in Fig. 1) ratio was also varied, in the proximity of experimentally estimated values[Janno, Arulepp]. Experimentally, the IL content would be determined from the saturation concentration of the electrode material, but in an MD simulation, the amount of each component must be controlled directly.

The polymer binder was not included in the simulation because it has no other known function besides binding the material together. Carbon based actuators can actuate without any binding polymer [Janno]. It also has very low concentration, so there is low probability of any polymer existing in a randomly chosen piece of the material with as large volume as the simulation cell used in this study.

The components used to create four systems according to Table 1 were:

- Carbon flakes

- 1-Ethyl-3-methyl-imidazolium (EMI+) cations

- Boron tetrafluoride (BF4-) anions

Table 1: Description of simulated systems

| System nr. | IL:Carbon mass ratio | Carbon | EMI+ cations | BF4- anions | Cell size | Density |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | mass-% | No. of flakes | Flake charge | mass-% | No. of cations | mass-% | No. of anions | (Å) | (g/cm3) |
| 1 | 1.89 | 34.6 | 24 | +2 | 32.6 | 165 | 32.8 | 213 | 41.12 | 1.34 |
| 2 | 1.89 | 34.6 | 24 | 0 | 36.7 | 186 | 28.7 | 186 | 41.47 | 1.31 |
| 3 | 1.89 | 34.6 | 24 | -2 | 40.9 | 207 | 24.5 | 159 | 41.75 | 1.28 |
| 4 | 1.13 | 47.0 | 24 | 0 | 29.8 | 111 | 23.3 | 111 | 42.38 | 1.33 |

Figure 1: Atom labels used for the ionic liquid EMI-BF4

## Construction of simulation cells

The nanoporous amorphous CDC carbon consists of graphene-like sheets without long-range ordering [Palmer]. Separate slightly curved graphene flakes were used to create a similar structure. The individual shapes of the flakes were initially created in planar form by putting together 6-member carbon rings with occasional 5-member rings (defects). The energy of the flakes was minimized by 1 ns long MD simulations in vacuum with 0.1 ps timestep at 293K temperature in NVE ensemble. The defects caused the flakes to bend. 8 different carbon flakes were created with the number of carbon rings in each flake between 24 and 27, up to 3 of which were 5-sided. In  the following simulations,  3 repeats of each flake type was included, summing up to 24 carbon flakes per system. An example of the shape one carbon flake after equilibration is depicted in Fig. 2. The detailed parameters of each flake are listed in Appendix X.

The amorphous structure of the simulated material was generated with Monte Carlo inspired methods, using in-house software [mcgen]. The carbon flakes were rotated in rigid body manner and sequentially inserted in random locations where the atoms would not coincide with each other until the required density was achieved. Two methods were used to place cations and anions in the pores of the carbon. First they were also rotated and sequentially inserted in random locations. Then a sequential testing of all empty spaces was done at regular intervals and the ions were inserted at each available space without rotation until sufficient density was achieved.

The models were created in cubic simulation boxes measuring 40×40×40 Å with periodic boundary conditions. The model with neutral carbons was created first. For charged carbon flakes, the configuration of the carbon flakes was left unchanged, but their partial atomic charges were modified according to the QC calculations. All carbon flakes of a system were given equal charges. To maintain both mass and neutrality, 27 anions were removed and 21 cations were inserted for each +2e increase of the charge of a carbon flake (+48e increase of net charge over all carbon flakes). The compositions of studied systems are listed in Table 1.

Figure 2: The shape of carbon flake shape no. 2. (List of shapes is presented in Appendix X table X.

## Force fields

The force field used was a combination of parameters derived from quantum chemical calculations and force fields found in literature. The partial charges  for carbon and hydrogen atoms in the graphene flakes were calculated for each charge (0, +2 or -2) and for each type of the carbon flake (with different number and location of defects) using PM6 [PM6] semi-empirical optimization method with open shells (UHF). An example of the charges is represented in Fig. 3. The complete list of partial charges in each type of carbon flakes can be found in appendix X.

Parameters for bonded interactions between carbon atoms within the carbon flakes were taken from Walther et al. [Walther]. Parameters from [AMBER] were used for hydrogen atoms at the edges of carbon flakes.

The description of the EMI-BF4 interactions was taken from Lopes et al. [Lopes]. van der Waals forces between atoms with force fields originating from separate sources were calculated using standard combination rules (1) for the Lennard-Jones potential (2) parameters for each atom pair (1 and 2 subscripts denote Lennard-Jones parameters of the atom types):

(1)

(2)

All force field parameters are presented in Appendix 1.

Figure 3: Partial charges of carbon flake type #7 with flake charge -2.Can the covalent bonds be added in this figure?

## Analysis methods

# Results

## System description

The volume of the system has stabilized to 71 nm3 after the first 1 ns of the simulation in NPT ensemble (Fig. X4), the density 1.31 g/cm3 (Table 1) is similar to the measured density (~1 g/cm3) of an actual actuator [private communication with Janno].

The carbon and IL are evenly distributed in the simulation cell with no large-scale phase separation (Fig. X5, X6). In the first coordination sphere of cations around carbon flakes the preferred orientation of cations is parallel with the carbon surface so that N1...C and N2...C distances are equal to 5.0 Å (Fig. X7).

## The effect of charged carbon flakes

When a carbon flake is charged positively, it not only repels the cations, but also rotates them. When the carbon flake charge is increased from 0 to +2, the typical angle between carbon plane and N1...N2 line is  rotated by 11 degrees, from 0 (parallel to surface) to 11 deg, indicated by the difference in shifts of N1...C and N2...C coordination sphere radii from 5.0 to 5.7 Å for N1...C (Fig. X8 https://ims.ut.ee/mediawiki/index.php/File:Carbil-RDF-C-N1.png) and from 5.0 to 5.3 Å for N2...C (Fig. X9 https://ims.ut.ee/mediawiki/index.php/File:Carbil-RDF-C-N2.png).

## The effect of IL:Carbon ratio

## Other effects

## Conclusion

Figure X4: Volume of the uncharged system during simulation in NPT ensemble. (Horizontal axis: time / ps, vertical axis: volume / Å3)

Figures X5, X6: Carbon and IL part of the system with uncharged carbon after MD simulation.

## References

- [Bar-Cohen-1999] Y. Bar-Cohen, S. P. Leary, M. Shahinpoor, J. S. Harrison, J. G. Smith, Proc. SPIE, 3669, 57 (1999); doi:10.1117/12.349708  http://dx.doi.org/10.1117/12.349708

- [Bar-Cohen-2001] Y. Bar-Cohen, Proc SPIE Int Soc Opt Eng, 4329, 1-6, (2001); http://dx.doi.org/10.1117/12.432639

- [Mart] M. Anton, A. Punning, A. Aabloo, M. Listak, M. Kruusmaa, Towards Autonomous Robotic Systems (TAROS 2004), University of Essex, 1-7, (2004); http://www.essex.ac.uk/csee/research/publications/technicalreports/2004/csm415/Anton_etal.pdf

- [Liu-2008] Y. Liu, L. Shi, L. Liu, Z. Zhang, J. Leng, Proc. SPIE, 6927, 69271A, (2008); http://dx.doi.org/10.1117/12.775946

- [Spigna] N. Di Spigna, P. Chakraborti, P. Yang, T. Ghosh, P. Franzon, Proc. SPIE, 7287, 72871K, (2009); http://dx.doi.org/10.1117/12.816009

- [eapbook] Y. Bar-Cohen (editor), Electroactive Polymer (EAP) Actuators as Artificial Muscles: Reality, Potential, and Challenges, Second Edition (SPIE Press Book), ISBN: 9780819452979

- [Wang] H. Wang, C. Li, ICMTMA'09. International Conference on Measuring Technology and Mechatronics Automation, 1, 73-76, (2009); http://dx.doi.org/10.1109/ICMTMA.2009.114

- [Fernandez] D. Fernández, L. Moreno, J. Baselga, Proc SPIE Int Soc Opt Eng, 5759, 361, (2005);  http://dx.doi.org/10.1117/12.599108

- [Akle] B. J. Akle, M. D. Bennett, D. J. Leo, K. B. Wiles, J. E. Mcgrath, J. Mater. Sci., 42, 7031-41, (2007); http://dx.doi.org/10.1007/s10853-006-0632-4x`

- [Hoefer] M. Hoefer, P. R. Bandaru, Appl. Phys. Lett. 95, 183108 (2009); http://dx.doi.org/10.1063/1.3258353

- [Brett] C. M. A. Brett, A. M. O. Brett, Electrochemistry: Principles, Methods, and Applications (Oxford University, Oxford, 1993).

- [Conway] B. E. Conway, J. Electrochem. Soc. 138, 1539 (1991).

- [Huang] J. Huang, B. G. Sumpter, V. Meunier, Chemistry - A European Journal, 14, 6614 (2008); http://dx.doi.org/10.1002/chem.200800639

- [Gogotsi] Y. Gogotsi, A. Nikitin, H. Ye, W. Zhou, J. E. Fischer, B. Yi, H. C. Foley, M. W. Barsoum, Nature Materials, 2, 591 (2003); http://dx.doi.org/10.1038/nmat957

- [biomedbook] F. Carpi (editor), E. Smela (editor), Biomedical Applications of Electroactive Polymer Actuators, Wiley 2009, ISBN: 978-0-470-77305-5

- [Bennett] M. D. Bennett, D. J. Leo, Sensors and Actuators A, 115, 79 (2004); http://dx.doi.org/10.1016/j.sna.2004.03.043

- [Viljar] V. Palmre, D. Brandell, U. Mäeorg, J. Torop, O. Volobujeva, A. Punning, U. Johanson, M. Kruusmaa, A. Aabloo, Smart Mater. Struct. 18, 095028 (2009); http://dx.doi.org/10.1088/0964-1726/18/9/095028

- [Janno] J. Torop, M. Arulepp, J. Leis, A. Punning, U. Johanson, V. Palmre, A. Aabloo, Materials, 3, 9 (2010); http://dx.doi.org/10.3390/ma3010009

- [Asaka-2005] T. Fukushima, K. Asaka, A. Kosaka, T. Aida, Angew. Chem. Int. Ed. 44, 2410-2413, (2005); http://dx.doi.org/10.1002/anie.200462318

- [Asaka-2008] K. Asaka, K. Mukai, I. Takeuchi, K. Kiyohara, T. Sugino, N. Terasawa, K. Hata, Proc. SPIE, 7037, 703710 (2008); http://dx.doi.org/10.1117/12.794503

- [Baughman-1999] R. H. Baughman, C. Cui, A. A. Zakhidov, Z. Iqbal, J. N. Barisci, G. M. Spinks, G. G. Wallace, A. Mazzoldi, D. De Rossi, A. G. Rinzler, O. Jaschinski, S. Roth, M. Kertesz, Science, 284, 1340 (1999); http://dx.doi.org/10.1126/science.284.5418.1340

- [Kiyohara] K. Kiyohara, T. Sugino, I. Takeuchi, K. Mukai, K. Asaka, J. Appl. Phys. 105, 063506 (2009)

- [Asaka-1995] K. Asaka, K. Oguro, Y. Nishimura, M. Mizuhata, H. Takenaka, Polym. J., 27, 436 (1995); http://dx.doi.org/10.1295/polymj.27.436

- [Oren] Y. Oren, I. Glatt, A. Livnat, O. Kafari, and A. Soffer, J. Electroanal. Chem. Interfacial Electrochem. 187, 59 (1985); http://dx.doi.org/10.1016/0368-1874(85)85575-1

- [Dias] F. B. Dias, L. Plomp, Journal of Power Sources, 88, 169 (2000); http://dx.doi.org/10.1016/S0378-7753(99)00529-7

- [Ahmad] S. Ahmad, S.A. Agnihotry, Current Applied Physics, 9, 108 (2009); http://dx.doi.org/10.1016/j.cap.2007.12.003

- [Heiki] H. Kasemägi, M. Klintenberg, A. Aabloo, J. O. Thomas, Solid State Ionics, Volume 147, Issues 3-4, April 2002, Pages 367-375, http://dx.doi.org/10.1016/S0167-2738(02)00013-9

- [Umecky] T. Umecky, Y. Saito, H. Matsumoto, J. Phys. Chem. B, 113, 8466 (2009); http://dx.doi.org/10.1021/jp9043946

- [Han] Z. J. Han, R. Morrow, B. K. Tay, D. McKenzie, Appl. Phys. Lett. 94, 043118 (2009); http://dx.doi.org/10.1063/1.3077605

- [Yushin] G. N. Yushin, E. N. Hoffman, A. Nikitin, H. Ye, M. W. Barsoum, Y. Gogotsi, Carbon, 43, 2075 (2005); http://dx.doi.org/10.1016/j.carbon.2005.03.014

- [mcgen] E. Soolo, J. Karo, H. Kasemägi, M. Kruusmaa, A. Aabloo, Proc. SPIE, 6168, 61682A (2006); http://dx.doi.org/10.1117/12.658664

- [dlpoly] W. Smith, T. Forester, The DL_POLY Project,TCS Division, Daresbury Laboratory, Daresbury, Warrington, WA44AD, England

- [Hentscke] R. Hentschke, B. L. Schürmann, J. P. Rabe, J. Chem. Phys. 96, 6213 (1992)

- [Okada] O. Okada, K. Oka, S. Kuwajima, K. Tanabe, Molecular Simulation, 21, 325-342, (1999); http://dx.doi.org/10.1080/08927029908022072

- [Lopes] J. N. C. Lopes, J. Deschamps, A. A. H. Pádua, J. Phys. Chem. B, 108, 2038–2047, (2004); http://dx.doi.org/10.1021/jp0362133

- [webelements] http://webelements.com

- [Palmer] J.C. Palmer, A. Llobet, S.-H. Yeon, J.E. Fischer, Y. Shi, Y. Gogotsi, K.E. Gubbins, Carbon, 48, 1116 (2010); http://dx.doi.org/10.1016/j.carbon.2009.11.033

- [Rapaport] D. C. Rapaport, The Art of Molecular Dynamics Simulation, Second Edition, Cambridge University Press, 2004.

- [Niu] S. Niu, Z. Cao, S. Li, T. Yan, J. Phys. Chem. B, 114, 877 (2010); http://dx.doi.org/10.1021/jp909486z

- [Daniel] D. Brandell, H. Kasemägi, A. Aabloo, Electrochimica Acta, 55, 1333 (2010); http://dx.doi.org/10.1016/j.electacta.2009.04.070

- [Liu-2004] Z. Liu, S. Huang, W. Wang, J. Phys. Chem. B, 108, 12978 (2004); http://dx.doi.org/10.1021/jp048369o

- [Newkome] G. R. Newkome (Editor), Advances in dendritic macromolecules, vol. 5, 2002; ISBN: 0-7623-0839-7

- [Floris] F. M. Floris, J. M. Martínez, J. Tomasi, The Journal of Chemical Physics, 116, 5460 (2002); http://dx.doi.org/10.1063/1.1453957

- [Arulepp] M. Arulepp, J. Leis, M. Lätt, F. Miller, K. Rumma, E. Lust, A.F. Burke, Journal of Power Sources, 162, 1460 (2006); http://dx.doi.org/10.1016/j.jpowsour.2006.08.014

- [Janno-personal] Janno Torop, personal communication

- [Leis] J. Leis, A. Perkson, M. Arulepp, M. Kaarik, G. Svensson, Carbon 39, 2043 (2001)

- [PM6]  J. J. P. Stewart, J. Mol. Mod., 13, 1173-1213 (2007); http://dx.doi.org/10.1007/s00894-007-0233-4

- [Walther] J. H. Walther, R. Jaffe, T. Halicioglu, P. Koumoutsakos, J. Phys. Chem. B, 105, 9980 (2001); http://dx.doi.org/10.1021/jp011344u

# Comments

How is the idea with this order of the authors?

We also need to state in the introduction what EAP system we are analyzing, not oly the methodology...

The introduction ends too abrupbtly. It need to be explained how these sentences will be investigated (or how they are of relevance) in the simulations.

We want to simulate CDC, but do not know what it looks like. Therefore we used an amorphous mixture of carbon flakes and propose it as a model to  describe CDC. (Amorphous mixture of carbon flakes, not Amorphous Carbon).

I don舩 understand. Is the graphene flakes a model of model of amorphous carbon? And the idea must be that the model is realistic �not to maximize its surface area?

Somewhre in supplementary materials should be thw whole list and detailed description of these flakes

Kas j臺 nii, et jv舁i ja optimaalne C-C kaugus laengust ei olenenud ?

Reply to Tarmo Tamm (16.12.2010, 12:13): "..."

Need to state that the forcefield bond parameters were not changed with the charge. However, for atoms more than 4 bonds away from each other, the coulombic forces are still calculated.

page 167

# Text boxes

Figure 4:

Figure 1:

Figure 2:

Figure 3:

Figure 5:

Figure 6: