Molecular Dynamics simulations of EMI-BF4 in nanoporous carbon for electroactive polymer actuators.

Endel Soolo, Daniel Brandell, Anti Liivat, Heiki Kasemägi, Tarmo Tamm, Alvo Aabloo

# Abstract

# Introduction

Electroactive polymers (EAP) are materials which change their shape in response to electric stimulation, and are therefore useful as lightweight actuators in for example space industry [Bar-Cohen-1999, Bar-Cohen-2001] and medicine applications [Bar-Cohen-2001], or biomimetic robotics [Mart, Liu-2008]. EAPs can generally be divided into two basic categories: ionic and electronic EAPs. Ionic EAPs act by ion/ionpair relocation during actuation, similar to supercapacitors. They are better suited for miniature devices, since they can be operated under low voltage (1-10V) [eapbook]. However, most ionic EAPs offer only small force, display low electromechanical efficiency and have short lifetime compared to traditional electromechanical actuators. Several practical solutions have been proposed to improve the total actuator force; e.g., designing specific shapes [Wang] or bundling multiple actuators [Fernandez]. In order to increase the efficiency, however, it is vital to understand the details of the actuation process and the ion migration at atomistic level [eapbook].

Ionic EAP materials are composed of three basic components: a porous electrode material (often carbon), an ionic transfer media and a polymer binder which adds toughness and flexibility. Several types of micro-porous carbon composite materials have been used in supercapacitors, where charges accumulate in a double layer on a large surface area. It has been claimed [Hoefer] that Carbide Derived Carbon (CDC) capacitor capacitance is mainly determined by two components: electrostatic/double layer capacitance [Brett] and faradaic/pseudocapacitive components [Conway]. Pore diameters smaller than 1 nm result in even higher capacitance due to larger surface area and confinement effects [Huang]. CDCs are one of the best known nanoporous materials for ion storage, since the pore-size is uniform and can be fine-tuned in a wide range [Gogotsi]. For EAP applications, ionic liquids [Armand et al, Nature Materials, 8 (2009) 621] (ILs) are frequently used as ion transfer media. ILs, or molten salts, consist of charged particles without additional solvent. Due to their low vapor pressure, ILs avoid evaporation of the electrolyte when functioning in a dry environment. IL electrolytes can also improve the cycle lifetime of the material compared to water based electrolytes [biomedbook]. The EAP actuator comprise two electrode sheets of the above mentioned components laminated together, with an ion permeable membrane in between, impregnated with electrolyte.

Different kinds of ion storage, ion transport medium, binder and membrane materials offer countless possibilities to experiment with. For example, IL electrolytes in Nafion membranes have been tested in combination with metal [Bennett], carbon nanotubes [Akle], CDC [Viljar] or RuO2 [Akle, Viljar] electrodes. CDC in a polytetrafluoroethylene (PTFE) matrix has also been used as electrodes, in combination with an IL electrolyte and an ion permeable paper membrane [Janno]. Asaka et al. [Asaka-2005, Asaka-2008] have studied carbon bucky gel actuators, where the electrodes contain carbon nanotubes in different ILs, supported by polyvinylidene fluoride (PVDF)-based binders [Asaka-2005]. The largest strain was achieved by using 1-ethyl-3-methylimidazolium tetrafluoroborate (EMI-BF4) as the IL [Asaka-2008]. Carbon nanotube sheets have also been demonstrated to work as actuators in water based electrolytes [Baughman-1999].

The EAP bending motion is caused either by electrode or membrane expansion at one side of the device and/or contraction at the other side, upon actuation. The mechanisms causing the expansions and contractions are still to a large degree debated [Kiyohara]. Suggestions include bond length changes due to repulsive Coulomb forces  accompanying double layer charging [Baughman-1999], insertion of counterions [Baughman-1995], electro-osmosis [Asaka-1995], electrostatic repulsion of the charged molecules in the material [Baughman-1999], decreased interfacial tension at the pore surfaces due to change in double-layer charges [Oren], etc.

A correlation has been found between increased accumulation of ions on the electrode surface (i.e., the capacity) and improved peak strain [Akle], but that result was seen to be dependent on electrolyte type [Janno]. Considering the large influence from the choice of IL or the type of carbon on the EAP performance [Janno, Viljar], the primary factor for strain ratio and maximum strain seems to be the ionic transport rather than changes in electronic configuration. When comparing EAPs with EMI-trifluoromethanesulfonate (EMI-Tf)-based electrolyte with those using tetraethyl ammonium (TEA) BF4-based electrolyte, which has a larger effective ion size due to ion pairing, the EMI-Tf can generate larger strains and has larger capacitance [Janno]. Increasing the ion mobility would, therefore, significantly help increasing both the strain ratio and the maximum strain of EAPs [biomedbook].

Several approaches can be used for increasing ionic conductivity. It is general knowledge from the field of battery polymer electrolytes that changing the monomeric sequence [ref.req.], adding plasticizers [Dias] or nano-particle fillers [Ahmad] all have proven successful strategies. In this context, MD simulations have helped generating a detailed view of the ion movement processes, and has been frequently used to study electrolyte systems [Heiki, Daniel, Anti, Borodin, etc].

In this study, the structure-dynamic properties of ionic motion in EAPs based on CDC carbon and EMI-BF4 ILs are investigated using MD simulation techniques. Changes in the microstructure are investigated when the charge accumulated in the carbon electrodes is varied, in an attempt to fundamentally understand the volume change causing actuation, and to search for strategies for enlarging peak strain and ion mobility.

# Methodology

The method of Molecular Dynamics (MD) is based on step-wise calculations of the forces acting on each atom within a fixed model. This force field is composed of the chemical interactions in the system: bond stretchings, bond angle vibrations, dihedral angle torsion rotations, van der Waals forces, and electrostatic interactions. The net force acting on an atom from all other particles in the system, together with its current position and velocity are used to calculate its position and velocity at the next time-step. This generates trajectories of all the particles in the model. By continuously sampling the atomic coordinates, diffusion coefficients and other macroscopic characteristics can be estimated, while transport mechanisms also can be analyzed on a more subtle molecular level. [Rapaport]

In this work, the simulation results were generally analyzed by Radial Distribution Functions (RDFs) and Coordination Numbers (CNs), while Space Distribution functions [Liu-2004] were used to find the coordination sphere radii and the most frequent interaction sites for ions and molecules.

## Simulated systems

Nanoporous amorphous CDC carbon consists of slightly curved graphene-like sheets, for which the amount of long-range ordering depends on the quenching rate [Palmer]. The structure was here approximated by separate slightly curved graphene flakes of similar sizes with 24 to 27 aromatic rings each. If the flakes were larger than that, then the number of flakes in the simulation box would be so small that the structure would not be amorphous. To gain insight into the structural changes associated with the ion conduction mechanism during actuation, the charge of the CDC carbon was varied between +2, 0 and -2 unit charges per carbon flake for all flakes in the MD box, whereafter the anion-cation ratio was adjusted to maintain electroneutrality.

The carbon to IL (here: EMI-BF4; the molecular structure and atom labels used are presented in Fig. 1) ratio was also varied, in the proximity of experimentally estimated values[Janno, Arulepp].

Due to its chemical inertness and low concentration, the polymer binder was excluded in the simulations.

The three different components – carbon flakes, EMI+ cations and BF4- anions – were inserted into four MD boxes according to Table 1.

Table 1: Description of simulated systems

| System nr. | IL:Carbon mass ratio | Carbon | EMI+ cations | BF4- anions | Cell size | Density |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | mass-% | No. of flakes | Flake charge | mass-% | No. of cations | mass-% | No. Of anions | (Å) | (g/cm3) |
| 1 | 1.89 | 34.6 | 24 | +2 | 32.6 | 165 | 32.8 | 213 | 41.12 | 1.34 |
| 2 | 1.89 | 34.6 | 24 | 0 | 36.7 | 186 | 28.7 | 186 | 41.47 | 1.31 |
| 3 | 1.89 | 34.6 | 24 | -2 | 40.9 | 207 | 24.5 | 159 | 41.75 | 1.28 |
| 4 | 1.13 | 47.0 | 24 | 0 | 29.8 | 111 | 23.3 | 111 | 42.38 | 1.33 |

Figure 1: Atom labels used for the ionic liquid EMI-BF4

## Construction of simulation cells

Separate slightly curved graphene flakes were used to create a structure resembling CDC carbon. The individual shapes of the flakes were initially created in planar form by putting together 6-member carbon rings with occasional 5-member rings (defects). The energy of the flakes was minimized by 1 ns long MD simulations in vacuum with 0.1 fs timestep in NVE ensemble using DLPOLY energy minimization routine with the same forcefield as was used in the following MD simulations of the uncharged flakes. The defects caused the flakes to bend. To allow some variation of the carbon flakes, 8 different types of flakes were created with 24-27 aromatic rings in each flake, including 0-3 5-sided rings. In  the following MD simulations, 3 flakes of each type were included, thus resulting in 24 carbon flakes per system. An example of the shape one carbon flake after equilibration is depicted in Fig. 2. The detailed parameters of each flake are listed in Appendix X.

The amorphous structure of the simulated material was generated with Monte Carlo inspired methods, using in-house software [mcgen]. The carbon flakes were rotated in rigid body manner and sequentially inserted in random locations where the atoms would not coincide with each other until the required density was achieved. Anions and cations were thereafter sequentially inserted into random locations in the carbon matrix until sufficient density was achieved.

The models were created in cubic simulation boxes measuring 40×40×40 Å with periodic boundary conditions. The model with neutral carbons was created first, while for the systems with charged carbon the configuration of the carbon flakes was left unchanged, but their partial atomic charges were modified according to QC calculations described below. All flakes in a system were given equal charges. To maintain both mass and electroneutrality, 27 anions were removed and 21 cations were inserted for each +2e increase of the charge of a carbon flake. The compositions of all studied systems are listed in Table 1.

Figure 2. Shape of a carbon flake consisting of 27 aromatic rings, one with 5 carbon atoms (flake no. 2 according to Appendix X, Table X).

## Force fields

The force field used was a combination of parameters derived from quantum chemical calculations and force fields found in literature. The partial charges  for carbon and hydrogen atoms in the graphene flakes were calculated for each charge (0, +2 or -2) and for each type of the carbon flake (with different number and location of defects) using PM6 [PM6] semi-empirical optimization method with open shells (UHF). An example of the charges is represented in Fig. 3. The complete list of partial charges in each type of carbon flakes can be found in Appendix X.

Parameters for bonded interactions between carbon atoms within the carbon flakes were taken from Walther et al. [Walther], while parameters from AMBER [AMBER] were used for hydrogen atoms at the edges of the carbon flakes.

The description of the EMI-BF4 interactions was taken from Lopes et al. [Lopes]. van der Waals forces between atoms with force fields originating from separate sources were calculated using standard combination rules (1) for the Lennard-Jones potential (2) parameters for each atom pair (1 and 2 subscripts denote Lennard-Jones parameters of the atom types):

(1)

(2)

All force field parameters are presented in Appendix 1.

Figure 3: Partial charges of a carbon flake (type no. 7, Appendix X) with flake charge -2.

## Simulation details

Each system was first equilibrated by a 2 ns long MD simulation in the NVT ensemble at 293 K temperature in the original 40 Å cubic cell to relieve internal stress originating in the generation. Thereafter,  a 10 ns long simulation followed in the NPT ensemble at 293 K temperature, using a Nose-Hoover barostat with 1 at pressure and a relaxation time of  0.3 ps.

The simulations used a Verlet leap-frog algorithm with 1 fs timestep. Temperature was kept at 293 K by a Nose-Hoover thermostat with 0.1 ps relaxation time. Ewald summation with 10-5 precision was used for all electrostatic interactions. The cubic symmetry of the simulation cell was retained in all simulations.

## Analysis methods

### Pore size and content distribution

The spaces between carbon flakes were modeled as an array of non-overlapping spheric pores. The pores were found by starting with a grid of equally spaced dots covering the whole simulation cell. Around each dot a sphere was created with the radius equal to the distance from the nearest CDC carbon or hydrogen atom minus the van der Waals radius of the atom. The spheres were then sorted by size and all spheres overlapping with a sphere larger than themselves was deleted. The number of cations and anions with their central point within the pore radius were counted and the distribution of sphere sizes were divided into subdivisions based on the number of cations within each pore.

# Results

## System description

The volume of the system has stabilized to 71 nm3 after the first 1 ns of the simulation in NPT ensemble (Fig. 4), the density 1.31 g/cm3 (Table 1) is similar to the measured density (~1 g/cm3) of an actual actuator [private communication with Janno].

The carbon and IL are evenly distributed in the simulation cell with no large-scale phase separation (Fig. 5, 6).

Figure 4: Volume of the uncharged system during simulation in NPT ensemble. The energy equilibration routine was used during the first 200 ps, followed by regular MD simulation.

Figures 5, 6: Carbon and IL part of the system with uncharged carbon after MD simulation.

### Pore sizes

Due to the different sizes of cations and anions, they occupy differently sized pores in the CDC. When the carbon flakes are electroneutral, then single cations most often occupy pores with 6 Å diameter and single anions occupy pores with 4 Å diameter (Fig. 7). The difference disappears for larger pores as clusters with equal numbers of cations and anions are able to appear. Clusters with two anions and two cations can be most often found in pores with 9 Å diameter (Fig. 7).

When positive charge is introduced to the carbon flakes, then the cations move into slightly smaller pores, with the mean size of a pore containing a single cation increasing from 6 Å to 7 Å (Fig. 8). When the carbon flakes are charged negatively, significant amount of cations move into smaller pores with only 4 Å diameter.

The most frequent pore size containing a single anion stays at 4 Å when positive charge is applied (Fig. 9), but their count in larger 6 Å is still diminished and their number in smaller 4 Å pores increased. When negative charge is applied, then 4 Å is no longer the probability maximum for pores containing a single anion. The single cations and single anions appear to be changing their places between the 4 Å and 6 Å pores.

Figure 7: Spherical pore size distribution, divided by the number of cations or anions in a pore.

Figure 8: Distribution of spherical pore sizes containing a single cation

Figure 9: Distribution of spherical pore sizes containing a single anion

### Cations and carbon flakes

The CDC carbon atoms are coordinated with cations, with the first coordination sphere at 4.3Å radius. The coordination number 1 is at 5.2Å radius (Fig. 10).

In the first coordination sphere of cations around carbon flakes the preferred orientation of cations is parallel with the carbon surface so that N1...C and N2...C distances are equal to 5.0 Å (Fig. 13). An example of such configuration is depicted in Fig. X20.

Most of the cations lie flat over the CDC carbon surface as indicated by the equal 4.2 to 4.3Å radiuses of the first coordination spheres of CDC carbon with all aromatic ring atoms: C1a (Fig. 11), C2a (Fig. 12), N1 (Fig, 13) and N2 (Fig. 14). An example of such configuration is presented in Fig. 17.

The parallel configuration applies to 80% of all cations on the CDC surface as can be determined from the ratio of coordination numbers for C...C2a (CN 0.48, Fig. 12) and C...N1 (CN 0.38, Fig. 13) at the same 4.5Å distance. In that case the CDC carbons can be coordinated either by C2a and C3a carbons (example in Fig. 18) or by C1a carbon (example in Fig. 19).

When the carbon flakes are charged positively with charge +2e on each flake, then the electrostatic repulsion causes 15% of the cations to turn around the C2a-C3a bond (e.g. around the longitudinal axis of the molecule or around the x-axis in Fig. 1) from orientation parallel with the carbon surface to orientation perpendicular with the carbon surface, as indicated by the shift of C...C1a coordination from first coordination sphere with 4.3Å radius to second coordination sphere with 6.3Å radius (Fig. 11) while the coordination spheres for C...C2a (Fig. 12) and C...C3a remain unchanged. The proportion of the cations remaining parallel with the carbon surface can be determined to be 96% in uncharged system and 79% in system with positively charged carbon flakes by comparing the  coordination numbers of C...C1a (Fig. 11) and C...C2a (12) at 5.0Å radius, e.g. after the first coordination sphere.

During this rotation (around the longitudinal axis or x-axis in Fig. 1) the outer ethyl group atom C2e remains coordinated with the carbon surface at 4.2 Å distance (Fig. 16) while the inner ethyl group atom C1e is moving away from carbon surface, from first coordination sphere with 4.2 Å radius to second coordination sphere with 5.2 Å radius (Fig. 15).

The molecule also rotates around the axis perpendicular with the aromatic ring plane (z-axis, Fig. 1). When the carbon flake charge is increased from 0 to +2, the molecul rotates  11 degrees as depicted in Fig. 19, indicated by the N1...C first coordination sphere radius increasing from 5.0 Å to 5.7 Å (Fig. 13) while the N2...C first coordination sphere radius only increases from 5.0 Å to 5.3 Å (Fig. 14).

90 degree rotation around the y-axis on Fig. 1 can also be noticed, resulting in the increase of the proportion of cations oriented with an end to the carbon flake (Fig. 20) instead of being parallel with the surface as in Fig. 17.

When the carbon flakes are charged negatively with charge -2e on each flake, then cations are preferencially coordinated to the CDC carbon surface with the C1a carbon atom. This configuration is 7% more common than coordination with C2a and C3a, as indicated by the ratio of C...C1a and C...C2a coordination numbers at 5 Å radius (Fig. 11, 12).

The ion does not rotate around the axis perpendicular with the aromatic ring plane (z-axis in Fig. 1)  in case of negative charging, as indicated by the equal shifts of first coordination sphere radii for C...N1 (Fig. 13) and C...N2 (Fig. 14).

Fig. 10: Radial distribution function for CDC carbon atoms and any non-hydrogen atom of the cation, reduced by 8, the number of such atoms in a cation.

Fig. 11: Radial distribution function for CDC carbon atoms and aromatic ring carbon atom C1a of the cation. CN of the charged systems is divided by the change in the total number of cations compared with the uncharged system.

Fig. 12: Radial distribution function for CDC carbon atoms and aromatic ring carbon atom C2a of the cation. CN of the charged systems is divided by the change in the total number of cations compared with the uncharged system.

Fig. 13: Radial distribution function for CDC carbon atoms and aromatic ring nitrogen atom N1 of the cation. CN of the charged systems is divided by the change in the total number of cations compared with the uncharged system.

Fig. 14: Radial distribution function for CDC carbon atoms and aromatic ring nitrogen atom N1 of the cation. CN of the charged systems is divided by the change in the total number of cations compared with the uncharged system.

Fig. 15: Radial distribution function for CDC carbon atoms and ethyl group inner carbon atom C1e of the cation. CN of the charged systems is divided by the change in the total number of cations compared with the uncharged system.

Fig. 16: Radial distribution function for CDC carbon atoms and ethyl group outer carbon atom C2e of the cation. CN of the charged systems is divided by the change in the total number of cations compared with the uncharged system.

Figure 17: Configuration of a cation flat over the carbon flake surface.

Figure 18: Configuration of a cation coordinated with a carbon flake through C1a and C1e atoms (aromatic ring is perpendicular to the carbon surface).

Figure 19: Configuration of a cation coordinated with a carbon flake through C1a and C1e atoms (aromatic ring is perpendicular to the carbon surface). The rotation of the cation when the carbon flake charge is changed from neutral to +2 is denoted with the arrow and shadow image.

Figure 20: cluster of ions around a carbon flake with +2 charge. The highlighted cation configuration is specific to positively charged carbon flakes and unlikely to be present in systems with neutral carbon flakes.

### Anions and carbon flakes

Anions coordinate the CDC carbon in three coordination spheres, with 4.6 Å, 6.4 Å and 8 Å radii and coordination numbers 0.6, 2.8 and 9, respectively (Fig. 21).

When the charge on the carbon flakes is changed, the anions coordination structure completely changes. Anions are moving between the first and third coordination sphere.

When the carbon flakes are charged positively, the coordination number for C...B first coordination sphere, measured at 5.2 Å radius, increases from 0.6 to 1.3 and in case of negative charge it drops to 0.3 (Fig. 21).

Fig. 21: Radial distribution function for CDC carbon and anion boron atoms. CN of the charged systems is divided by the change in the total number of anions compared with the uncharged system.

### Ion-ion interaction

When the size of the pore allows, a cation is always surrounded by anions, which can be located in several locations around the cation. In the first coordination sphere with 5Å radius around the centre of the aromatic ring, there are typically 4 atoms (CN in Fig. 22). Two coordination spheres can be distinguished around an average cation atom. First coordination sphere with 4.2Å mean radius contains 2 anions and second coordination sphere with 6Å radius has two more anions (Fig. 23).

Three of the anions are coordinated with the methyl group carbon (Fig. 25), so one has to be at the other far end of the cation. Two anions are in the first and two in the second coordination shell for the aromatic ring carbon C1a (Fig. 24).

An example of anions coordinating a cation is presented in Fig. 26.

The charging of carbon flakes does not significantly change the ion-ion interaction (Fig. 22, 23, 24, 25).

Fig. 22. RDF for cation aromatic ring center points and anion boron atoms. CN of the charged systems is divided by the change in the total number of anions relative to the uncharged system.

Fig. 23. RDF for any cation non-hydrogen atom and anion boron atoms. CN of the charged systems is divided by the change in the total number of anions relative to the uncharged system.

Fig. 24. RDF for cation aromatic ring carbon atom C1a and anion boron atoms. CN of the charged systems is divided by the change in the total number of anions relative to the uncharged system.

Fig. 25. RDF for cation methyl group carbon atom Cm and anion boron atoms. CN of the charged systems is divided by the change in the total number of anions relative to the uncharged system.

Figure 26: Typical configuration of anions coordinated with an cation.

### Mirror symmetry of the cation

The forcefield of the cations is completely symmetrical with the aromatic ring plane being a mirror plane for the molecule, so the cations can be expected to equally coordinate with both sides of the cations. The distribution of dihedral angles Ca1-N1-N2...B for anions coordinated with a cation is indeed symmetrical for boxes with neutral or positively charged carbon flakes. In the box with negatively charged carbon flakes, one probability maximum is shifted 10 degrees, from -40 deg to -50 deg. The probability minimum is also shifted 10 degrees, from 0 to -10 deg. (Fig. 27), but this does not significantly affect the number of anions on each side of the cation, which most often appears to be 2 on each side (Fig. 28, 29).

However, this does not mean that any particular cation should have two anions on one and two on the other side for the local environment can be less symmetrical. When anions are counted on the side of each cation, which has more anions than the other side, then the typical number can be found to be 3 (Fig. 30) while only one anion is on the other side (Fig. 31). Charge on the carbon flakes does not significantly affect the number of anions on the more populated side (Fig. 30), but on the other side a significant change is apparent. In negatively charged system the distribution is more symmetrical with 2 anions on the side less populated with anions, in negatively charged system it is less symmetrical with only one anion on the less-populated side. In negatively charged system the asymmetry can be explained by the cations laying with one side against carbon surface as depicted in Fig. 17 so anions can not fit inbetween.

Figure 27: Distribution of Ca1-N1-N2...B dihedral angle for anions coordinated with a cation (within 6.0 Å radius from the cation).

| Figure 28: Distribution of anion counts on one side of a cation (Ca1-N1-N2...B dihedral > 0) | Figure 29: Distribution of anion counts on other side of a cation (Ca1-N1-N2...B dihedral < 0) |
| --- | --- |
| Figure 30: Distribution of anion counts on the side of a cation with more anions than the other side | Figure 31: Distribution of anion counts on the side of a cation with less anions than the other side |

## Movement of the actuator

The simulation cell volume increased when negatively charged and decreased when positively charged. The volume change was equal in both direction, 2% per 2e of charge on each carbon flake (Table 1). The volume change can be explained by the movement of anions into the small pores (Fig. 9) when charged positively and out of the pores when charged negatively, because only in the C...B RDF (Fig. 21) does the direction of movement (closer when charged positively, further when charged negatively) coincide with the direction of detected volume change (expansion when charged negatively, contraction when charged positively, Table 1). Another cause for the volume change could be the changed composition of the unit cell. The number of cations inserted to replace the removed anions (or vice versa) was chosen so as to maintain the mass and total charge as the charge on carbon flakes was varied. However, the volume of the ions was not taken into account and cations and anions may have different volume to mass ratio as the ions were replaced by counterions

A volume change with this nature has previously been experimentally recorded [Ref. Req: some Japanese study, Janno knows where to find it].

If the same 2% volume change occurred in infinitesimally thin electrodes on two sides of a D=10 μm thick separator, then without considering the elastic response of the separator, the bending radius would be R=D/(2*0.02/3)=0.75mm and in case of 100 μm thick separator the bending radius would be 7.5mm. For De=100 μm thick electrodes D=10 μm thick separator, again without considering the elastic response, the bending radius would be R=(D+De)/(2*0.02/3)=8.25mm and in case of 100 μm thick separator the bending radius would be 15mm.

## Conclusion

## References

- [Bar-Cohen-1999] Y. Bar-Cohen, S. P. Leary, M. Shahinpoor, J. S. Harrison, J. G. Smith, Proc. SPIE, 3669, 57 (1999); doi:10.1117/12.349708  http://dx.doi.org/10.1117/12.349708

- [Bar-Cohen-2001] Y. Bar-Cohen, Proc SPIE Int Soc Opt Eng, 4329, 1-6, (2001); http://dx.doi.org/10.1117/12.432639

- [Mart] M. Anton, A. Punning, A. Aabloo, M. Listak, M. Kruusmaa, Towards Autonomous Robotic Systems (TAROS 2004), University of Essex, 1-7, (2004); http://www.essex.ac.uk/csee/research/publications/technicalreports/2004/csm415/Anton_etal.pdf

- [Liu-2008] Y. Liu, L. Shi, L. Liu, Z. Zhang, J. Leng, Proc. SPIE, 6927, 69271A, (2008); http://dx.doi.org/10.1117/12.775946

- [Spigna] N. Di Spigna, P. Chakraborti, P. Yang, T. Ghosh, P. Franzon, Proc. SPIE, 7287, 72871K, (2009); http://dx.doi.org/10.1117/12.816009

- [eapbook] Y. Bar-Cohen (editor), Electroactive Polymer (EAP) Actuators as Artificial Muscles: Reality, Potential, and Challenges, Second Edition (SPIE Press Book), ISBN: 9780819452979

- [Wang] H. Wang, C. Li, ICMTMA'09. International Conference on Measuring Technology and Mechatronics Automation, 1, 73-76, (2009); http://dx.doi.org/10.1109/ICMTMA.2009.114

- [Fernandez] D. Fernández, L. Moreno, J. Baselga, Proc SPIE Int Soc Opt Eng, 5759, 361, (2005);  http://dx.doi.org/10.1117/12.599108

- [Akle] B. J. Akle, M. D. Bennett, D. J. Leo, K. B. Wiles, J. E. Mcgrath, J. Mater. Sci., 42, 7031-41, (2007); http://dx.doi.org/10.1007/s10853-006-0632-4x`

- [Hoefer] M. Hoefer, P. R. Bandaru, Appl. Phys. Lett. 95, 183108 (2009); http://dx.doi.org/10.1063/1.3258353

- [Brett] C. M. A. Brett, A. M. O. Brett, Electrochemistry: Principles, Methods, and Applications (Oxford University, Oxford, 1993).

- [Conway] B. E. Conway, J. Electrochem. Soc. 138, 1539 (1991).

- [Huang] J. Huang, B. G. Sumpter, V. Meunier, Chemistry - A European Journal, 14, 6614 (2008); http://dx.doi.org/10.1002/chem.200800639

- [Gogotsi] Y. Gogotsi, A. Nikitin, H. Ye, W. Zhou, J. E. Fischer, B. Yi, H. C. Foley, M. W. Barsoum, Nature Materials, 2, 591 (2003); http://dx.doi.org/10.1038/nmat957

- [biomedbook] F. Carpi (editor), E. Smela (editor), Biomedical Applications of Electroactive Polymer Actuators, Wiley 2009, ISBN: 978-0-470-77305-5

- [Bennett] M. D. Bennett, D. J. Leo, Sensors and Actuators A, 115, 79 (2004); http://dx.doi.org/10.1016/j.sna.2004.03.043

- [Viljar] V. Palmre, D. Brandell, U. Mäeorg, J. Torop, O. Volobujeva, A. Punning, U. Johanson, M. Kruusmaa, A. Aabloo, Smart Mater. Struct. 18, 095028 (2009); http://dx.doi.org/10.1088/0964-1726/18/9/095028

- [Janno] J. Torop, M. Arulepp, J. Leis, A. Punning, U. Johanson, V. Palmre, A. Aabloo, Materials, 3, 9 (2010); http://dx.doi.org/10.3390/ma3010009

- [Asaka-2005] T. Fukushima, K. Asaka, A. Kosaka, T. Aida, Angew. Chem. Int. Ed. 44, 2410-2413, (2005); http://dx.doi.org/10.1002/anie.200462318

- [Asaka-2008] K. Asaka, K. Mukai, I. Takeuchi, K. Kiyohara, T. Sugino, N. Terasawa, K. Hata, Proc. SPIE, 7037, 703710 (2008); http://dx.doi.org/10.1117/12.794503

- [Baughman-1999] R. H. Baughman, C. Cui, A. A. Zakhidov, Z. Iqbal, J. N. Barisci, G. M. Spinks, G. G. Wallace, A. Mazzoldi, D. De Rossi, A. G. Rinzler, O. Jaschinski, S. Roth, M. Kertesz, Science, 284, 1340 (1999); http://dx.doi.org/10.1126/science.284.5418.1340

- [Kiyohara] K. Kiyohara, T. Sugino, I. Takeuchi, K. Mukai, K. Asaka, J. Appl. Phys. 105, 063506 (2009)

- [Asaka-1995] K. Asaka, K. Oguro, Y. Nishimura, M. Mizuhata, H. Takenaka, Polym. J., 27, 436 (1995); http://dx.doi.org/10.1295/polymj.27.436

- [Oren] Y. Oren, I. Glatt, A. Livnat, O. Kafari, and A. Soffer, J. Electroanal. Chem. Interfacial Electrochem. 187, 59 (1985); http://dx.doi.org/10.1016/0368-1874(85)85575-1

- [Dias] F. B. Dias, L. Plomp, Journal of Power Sources, 88, 169 (2000); http://dx.doi.org/10.1016/S0378-7753(99)00529-7

- [Ahmad] S. Ahmad, S.A. Agnihotry, Current Applied Physics, 9, 108 (2009); http://dx.doi.org/10.1016/j.cap.2007.12.003

- [Heiki] H. Kasemägi, M. Klintenberg, A. Aabloo, J. O. Thomas, Solid State Ionics, Volume 147, Issues 3-4, April 2002, Pages 367-375, http://dx.doi.org/10.1016/S0167-2738(02)00013-9

- [Umecky] T. Umecky, Y. Saito, H. Matsumoto, J. Phys. Chem. B, 113, 8466 (2009); http://dx.doi.org/10.1021/jp9043946

- [Han] Z. J. Han, R. Morrow, B. K. Tay, D. McKenzie, Appl. Phys. Lett. 94, 043118 (2009); http://dx.doi.org/10.1063/1.3077605

- [Yushin] G. N. Yushin, E. N. Hoffman, A. Nikitin, H. Ye, M. W. Barsoum, Y. Gogotsi, Carbon, 43, 2075 (2005); http://dx.doi.org/10.1016/j.carbon.2005.03.014

- [mcgen] E. Soolo, J. Karo, H. Kasemägi, M. Kruusmaa, A. Aabloo, Proc. SPIE, 6168, 61682A (2006); http://dx.doi.org/10.1117/12.658664

- [dlpoly] W. Smith, T. Forester, The DL_POLY Project,TCS Division, Daresbury Laboratory, Daresbury, Warrington, WA44AD, England

- [Hentscke] R. Hentschke, B. L. Schürmann, J. P. Rabe, J. Chem. Phys. 96, 6213 (1992)

- [Okada] O. Okada, K. Oka, S. Kuwajima, K. Tanabe, Molecular Simulation, 21, 325-342, (1999); http://dx.doi.org/10.1080/08927029908022072

- [Lopes] J. N. C. Lopes, J. Deschamps, A. A. H. Pádua, J. Phys. Chem. B, 108, 2038–2047, (2004); http://dx.doi.org/10.1021/jp0362133

- [webelements] http://webelements.com

- [Palmer] J.C. Palmer, A. Llobet, S.-H. Yeon, J.E. Fischer, Y. Shi, Y. Gogotsi, K.E. Gubbins, Carbon, 48, 1116 (2010); http://dx.doi.org/10.1016/j.carbon.2009.11.033

- [Rapaport] D. C. Rapaport, The Art of Molecular Dynamics Simulation, Second Edition, Cambridge University Press, 2004.

- [Niu] S. Niu, Z. Cao, S. Li, T. Yan, J. Phys. Chem. B, 114, 877 (2010); http://dx.doi.org/10.1021/jp909486z

- [Daniel] D. Brandell, H. Kasemägi, A. Aabloo, Electrochimica Acta, 55, 1333 (2010); http://dx.doi.org/10.1016/j.electacta.2009.04.070

- [Liu-2004] Z. Liu, S. Huang, W. Wang, J. Phys. Chem. B, 108, 12978 (2004); http://dx.doi.org/10.1021/jp048369o

- [Newkome] G. R. Newkome (Editor), Advances in dendritic macromolecules, vol. 5, 2002; ISBN: 0-7623-0839-7

- [Floris] F. M. Floris, J. M. Martínez, J. Tomasi, The Journal of Chemical Physics, 116, 5460 (2002); http://dx.doi.org/10.1063/1.1453957

- [Arulepp] M. Arulepp, J. Leis, M. Lätt, F. Miller, K. Rumma, E. Lust, A.F. Burke, Journal of Power Sources, 162, 1460 (2006); http://dx.doi.org/10.1016/j.jpowsour.2006.08.014

- [Janno-personal] Janno Torop, personal communication

- [Leis] J. Leis, A. Perkson, M. Arulepp, M. Kaarik, G. Svensson, Carbon 39, 2043 (2001)

- [PM6]  J. J. P. Stewart, J. Mol. Mod., 13, 1173-1213 (2007); http://dx.doi.org/10.1007/s00894-007-0233-4

- [Walther] J. H. Walther, R. Jaffe, T. Halicioglu, P. Koumoutsakos, J. Phys. Chem. B, 105, 9980 (2001); http://dx.doi.org/10.1021/jp011344u

# Comments

Should the word „dynamic“ be removed if dynamic properties (MSD) are not calculated?

These are only methods for analysing the strucutre �what about dynamics?

Vastus autorile  daniel (02.01.2011, 15:34): "..."

I will add dynamics here after I have used them in the Results part.

Is this not non-standard as compared to QC minimization?? And how is the energy minimized if energy is constant?

I do not know how the energy is maintained and minimized at the same time, but DL_POLY manual is also using the term „NVE ensemble“ for this method.

If there are slight differences in the flake shape, those should relax very quickly, because the vibration period for a bent  flake in MD simulation vacuum in NVT ensemble is only about 1 picosecond.

Somewhre in supplementary materials should be the whole list and detailed description of these flakes

From Daniel: What is the pore size distribution? How does it compare to experimental data on CDC? How does it change upon charging?

From Alvo: There are many different kinds of CDC with different pore size distribution.

It has been measured experimentally using gas absorption. Choose the one that is closest to the one I got and use it. Janno knows where to find them.

Recalibrate as the distribution of volume per each pore size to be comparable with experimental BET measurements.

From Urmas:

When the ion is inside the pore of similarily charged carbon, then there must be ion pairs in the pore, with the number of counterions at least equal with the number of the ions with same charge.

Should add ion pairs to the picture.

From Daniel: Are the carbons in the flakes positively or negativey charged, when the total charge is 0? How does this change upon charging (are they then all positive or negative)? Are the C-atoms in the flakes primarily coordinated to anions or cations?

From Daniel: There are far too many RDFs. How can the number of graphs be decreased, without decreasing the amount of information?

From Alvo: some could be moved to the supplementary material. But then they can not be used in the explanatory text.

Some cation-anion RDF graphs could be replaced by a SDF (3-dimensional distribution) plot.

Does the charging change the ratio of flat configuration and this configuration?

Add

From Daniel: Are there any SDF functions for this?

From Daniel: What is the coordination preference for the anions?

(Which part of the cation are the anions coordinated with?

Fig. Shows two atoms in 1st nd two atoms in 2nd coordination sphere. Write about where those are.)

Maybe a configuration with an anion near the end of  ethyl group would be more typical.

Jumped too fast to the charged state. First the static description and the dynamic properties need to be laid out precisely.

Can it be called the difference in mass density of cations vs. that of anions?

From Daniel: These effects need to be explained.

(Why does the material move?)

10um separator and 100um electrode (from Janno)

page 167

# Text boxes

Figure 11

Figure 28:

Figure 29:

Figure 12

Figure 13

Figure 30:

Figure 31:

Figure 1:

Figure 2:

Figure 3:

Figure 4:

Figure 14

Figure 5:

Figure 27:

Figure 6:

Figure 19:

Figure 7:

Figure 25

Figure 8:

Figure 26:

Figure 9:

Figure 20

Figure 10

Figure 15

Figure 16

Figure 24

Figure 17:

Figure 18:

Figure 21

Figure 22

Figure 23