## Slide 1
Modeling IPMC material with dynamic surface characteristics
David Pugal, Alvo Aabloo,
Kwang J. Kim, Youngsoo Jung
Active Materials and Processing Laboratory (AMPL)
Low Carbon Green Technology Laboratory (LCGTL)
Dept. of Mechanical Engineering
University of Nevada, Reno
Smart Materials, Adaptive Structures & Intelligent Systems
September 21 – 23, Oxnard, California
PICTURE

## Slide 2: Outline
IPMC material
Basic mathematical description of actuation
Surface electrode model
  Motivation
  Physics background
  Comsol Multiphysics simulations
  Results
Conclusions

## Slide 3: IPMC material
IPMC – Ionic Polymer-Metal Composite
  Electromechanical behavior
  Mechanoelectrical behavior
Nafion™ polymer
Hydrated cation

## Slide 4: Simple model
The simple physical model:
  Ion migration and diffusion, Nernst-Planck equation
    C – cation concentration
    D – Diffusion coefficient
    z – charge number
    – mobility
    F – Faraday constant
    – electric potential

## Slide 5: Simple model
The simple physical model:
  Ion migration and diffusion
  Electric field, Poisson’ equation
    Describes the electric field in the IPMC
    E – electric field
    – potential
    – charge density
    – electric permittivity
    F – Faraday constant

## Slide 6: Simple model
The simple physical model:
  Ion migration and diffusion
  Electric field, Poisson’ equation
  Stress-strain
    Stress is related to the charge density
  Not considered in this work

## Slide 7: Concentration - Bending
Concentration graph
  Bending related to concentration  electric properties

## Slide 8: Electrode modeling - Motivation
Some samples have shown significant dynamic surface resistance
  Related directly to voltage drop and therefore the actuation of IPMC
A. Punning, M. Kruusmaa and A. Aabloo, Sensors and Actuators, A: Physical 133 (1), 200 (2007).

## Slide 9: Electrode modeling - Motivation
The voltage drop along the electrode
  U0, U1, U3 measured on the one side of IPMC
  Some of the drop is due to electrolysis
  Part of it is due to surface resistance
A. Punning, Dissertation Thesis, Tartu University, 2007.
U0, U1,U3

## Slide 10: Electrode modeling - motivation
Patterned electrodes 3D bending Different areas with different surface characteristics
Electrode conductivity characterization

## Slide 11: Surface resistance model - background
Tie together the current flowing through the surface and the ionic current inside the polymer
Ramo-Shockley theorem
  Plasma phycis *
  Ion channels in proteins #
* P. Paris, M. Aints, M. Laan, and T. Plank, “Laser-induced current in air gap
at atmospheric pressure,” Journal of Physics D: Applied Physics 38(21),
pp. 3900–3906, 2005.
# W. Nonner, A. Peyser, D. Gillespie, and B. Eisenberg, “Relating Microscopic
Charge Movement to Macroscopic Currents: The Ramo-Shockley Theorem
Applied to Ion Channels,” Biophysical Journal 87(6), pp. 3716–3722, 2004.
Courtesy of M. Laan
Courtesy of M. Dingemans

## Slide 12: Surface resistance model – math.
Current in the external circuit:
By integrating over arbitrary trajectories, the charge:
The following relation for current density can be derived:

## Slide 13: Surface resistance model - idea
The electric current inside the IPMC is calculated by integrating the ion flux
The ion flux is “projected to the electrode” where it becomes a boundary condition for the electrode model
The voltage of the electrode model, in turn, becomes a boundary condition to the Poisson equation, which is responsible for the ion flux
voltage drop
electrode b.c
Ion flux
current

## Slide 14: Surface resistance model - Comsol
Implementation in Comsol
  2 different domains are modeled
    1: Polymer (Nernst-Planck and Poisson’ equation)
    2: Electrode (Ohm’ law)
  B.C. Boundary between the bulk Nafion and electrode:
    Integrated ion flux from domain 1 was projected as an input on domain 2:
1
2
Input voltage

## Slide 15: Surface resistance model - Comsol
Implementing in Comsol – meshing
Regular mapped mesh - faster
Free mesh – due to projection coupling

## Slide 16: Results
2D modeling – experimental setup
2D modeling – the model
+
P2
p3
-
-
+
Probe 2
Probe 3
+
-
Probe 2
Probe 3
Straight IPMC
Bent IPMC
Small area of higher
Surface resistance

## Slide 17: Results – 2D model, current
-
+
+
-

## Slide 18: Results – 2D model, Voltage

## Slide 19: Results – 2D model, Voltage

## Slide 20: Results
3D modeling – experimental setup
3D modeling – the model
  Scaled model is used!
Top view

## Slide 21: Results – 3D model

## Slide 22: Results – simplifications
Loose the feedback
  Better convergence
  Reduced calculation time
  Ionic current does cause the voltage drop on the electrodes
  The voltage drop does not change the ionic current
  Used for?

## Slide 23: Results – simplified model
Changed diffusion constant.
Electric current value is not correct

## Slide 24: Discussion
Some downsides of the model
  Time consuming calculation
  The convergence problems due to the feedback nature of the model
Possible solutions
  Different solver?
  Use time stepping instead of full time dependent solution

## Slide 25: Conclusions
The surface resistance model works fairly well
The 3D scaled model was developed
  With simple 3D IPMC, the surface could be omitted and the full scale model can be used
Using Ramo-Shockley theorem is beneficial, when the surface resistivity plays important role
  Surface treated IPMCs
  More complicated structures
Future
  Simplify the model, reduce solution time

## Slide 26: Thank you
Questions?