## Slide 1
MD Simulations of Fe Precipitates in Cu
x
z
Voids near the surface act as stress concentrators in a high external electric field. They are nucleation centers for dislocations that lead to stable protrusions on the surface. [2]
Simon Vigonski1, Vahur Zadin1, Alvo Aabloo1, Flyura Djurabekova2
1Institute of Technology, University of Tartu
2Univeristy of Helsinki
Correspond to: simon.vigonski@ut.ee
Tänusõnad – PUT57, CERN+ ….
Conclusions
Box dimensions: 186x193x199 Å
Cu <110> direction in z
Various r and h
Motivation
Setup
Frequent vacuum break-downs in CLIC accelerating structures are presumably caused by field-enhancing empitters appearing on the surface. The origin of these emitters is hypothesized to be caused by plastic deformations and dislocations. We investigate the effect of voids and precipitates on dislocation nucleation.
Methods
Near-surface voids
Fe precipitates in Cu
E = 22.8 GV/m, t = 180 ps
E = 22.8 GV/m, t = 10 ps
E = 29.1 GV/m
Continually increasing the electric field was found to create a void below the precipitate just before extensive surface vaporization.
Classical molecular dynamics with LAMMPS, using the Bonny et al. many-body EAM potential. [1]
[1] Bonny, G., Pasianot, R. C., Castin, N., Malerba, L., Philos. Mag. 89, 3531–3546 (2009).
[2] Pohjonen, A. S., Parviainen, S., Muranaka, T., Djurabekova, F., J. Appl. Phys. 114, 033519 (2013).
Unlike voids, Fe precipitates show little ability to nucleate dislocations. No surface geometry change is visible even under very high electric fields.
Inserting Fe as an fcc structure relaxes it into an irregular bcc sphere and creates a knot of Cu dislocations around it.
Irregular precipitates
Fe precipitates provide less dislocation nucleation than voids
Precipitates adjacent to the surface facilitate vaporization
Irregular precipitates offer more dislocation nucleation sites
A Fe precipitate protruding on the surface results in quick and extensive evaporation on the Fe-Cu-vacuum interface.
Fixed boundary
r
h
Force
Red – Fe
Blue – Cu dislocations