Electromechanical characteristics of actuators based on carbide-derived carbon

Janno Toropa, Friedrich Kaasika, Takushi Suginob, Alvo Aablooa, Kinji Asakab

a) IMS Lab, Institute of Technology, University of Tartu, Nooruse 1, 50411 Tartu, Estonia

b) National Institute of Advanced Industrial Science and Technology (AIST), 1-8-31 Midorigaoka, Ikeda, Osaka 563-8577, Japan

Abstract

An electromechanical transducer was prepared using non-ionic polymer, ionic liquid and carbide-derived carbon (CDC). Recently, simple layer-by-layer casting method for actuator production was discovered, using „bucky gel“ mixture as the precursor of actuator electrode layers. In this paper we investigate carbide-derived carbon as a new alternative to carbon nanotubes to replace nanotubes in the electrode layer of the transducer. At the initial stage of the study, the ratio of nanoporous high surface TiC-derived carbon powder, 1-ethyl-3-methylimidazolium tetrafluoroborate (EMIBF4) and polymer (PVdF(HFP)) was varied and each formed electrode was analyzed to find the optimal composition. The results revealed that the optimal component ratio for electrodes is: 35 wt% PVdF(HFP), 35 wt% EMIBF4 and 30 wt% CDC. The assembled three layer transducers were characterized by measuring blocking force, maximum strain, speed, power consumption and capacitance. The synthesized actuator showed very good force and capacitive characteristics and it is preferable for slow-response applications compared to transducers based on carbon nanotubes.

# Keywords: polymer actuator, carbide-derived carbon (CDC), ionic liquid

# INTRODUCTION

Electro-active polymers (EAPs) are materials that change their properties due to the electric potential difference. For example electromechanically active polymer materials convert electrical energy directly to mechanical. These kinds of materials can be used in robotics, microfluidics or bio-medical applications. These applications are possible because of the big strength to mass ratio of transducers and possibility to make actuators in different sizes and shapes. Baughman et. al. have reported the first bucky paper actuator that consists of two single-walled carbon nanotube (SWNT) sheets on both side of a double-sided Scotch tape and shows a bending motion in aqueous electrolytes []. They proposed a charge injection model due to quantum chemical and double-layer electrostatic effects. In their model, the actuation is caused by dimensional changes of SWNTs in the covalently bonded direction derived from the charge injection []. This dimensional change is free of Faradaic’ process that is inevitable for conductive polymer actuators and that restricts their lifetime and response speed.

Most of the EAP actuators operate in electrolyte solutions and deny that actuator assembly methods are quite complicated. Easier fabrication methods and ability to work in the air give EAP transducers large advantages in use as “artificial muscles”. However, there are already some outstanding examples of EAP actuator production for open-air applications. Fukushima et. al. have reported of a fully plastic actuator consisting of two ionic-liquid-based bucky gel electrodes and ionic liquid containing polymeric membrane between them []. This type of actuator can be prepared by simple layer-by-layer casting method. It is a dry-type polymer actuator with long-lived operation performance in air at low voltages. When voltage is applied, this actuator shows a bending motion towards the anode side, which is the same bending direction as observed for IPMCs and SWNT sheets. Electrochemical measurements showed that ion transfer occurred in bucky-gel actuators non-Faradaically by simple charge/discharge of ions in electrode layer. Charge injection of SWNTs and steric repulsion caused by ion transfer into electrode are suggested models for actuation mechanisms []. However, the actuation is somehow the result of the charge storage in the electrode based on pure double-layer charging. Ionic liquids (ILs), only source of ions for this type actuator are non-volatile molten salts that show high conductivities and wide electrochemical potential windows. Relatively high conductivity of ILs ensures quick response in actuation and large extent of movement of the actuator strip.

We propose a polymeric three layer actuator which electrodes are made of porous carbon material, base polymer and ionic liquid. The thin electrode film is made of nanoporous TiC-derived carbon powder and polyvinylidene fluoride-co-hexafluoropropylene (PVdF-HFP) as the binder polymer. Carbon produced by extraction of metals from metal carbides is called carbide-derived carbon (CDC). The described method of carbon synthesis offers unique control over carbon microstructure and allows to fine-tune the porosity of the product at nanoscale. Common applications proposed for CDCs are fuel cells, hydrogen storage and different extraction/purification methods of noble gases based on selective adsorption. However, main force of the development is focused on electrochemical storage devices, such as super- or ultracapacitors.

In principle, the design of ionic polymer actuators is comparable to supercapacitors. Supercapacitors are highly capacitive devices famous for their high power densities and energy conversion efficiency up to 98% during charging-discharging cycle. They consist of two high-surface areas, e.g. porous carbon material, electrodes and an ion permeable separator in between them. The porous polymer separator acts like a reservoir for electrolyte and avoids electronic conductance between the electrodes [,].This energy storage system based on a non-Faradaic process provides very fast charge and discharge making the electric double-layer capacitors (EDLCs) with the best candidates to meet the demand for high power and long durability. Recently, relationships between porous structures and electrochemical behavior have become increasingly important []. Although the use of various materials as EDLCs has been investigated, the application is limited in terms of specific energy. To enhance the specific energy and power of EDLCs, several researchers have put much effort into the development and modification of carbonaceous materials, such as controlling the pore size distribution, introducing electro-active metallic particles or electro- conducting polymers, and fabricating hybridtype cells[].

Our actuator consisting of polymer supported CDC electrodes and porous membrane between them was described before in []. Under low bias (1.5-3 V), the thin films made of carbon material changed their thickness accordingly to the charge inserted. In principle, the design of the ionic polymer actuator described in this article is comparable to supercapacitors or EDLCs. Thereby, relying on association by similarity, the electroactive mechanism of nanoporous carbon electrodes is related to electric double-layer formation during charging of the material, and the dimensional change of the actuator is the consequence of charge injection in carbon nanopores during the electric double-layer charging.

# EXperimental details

## Materials

CDC was purchased from Carbon Nanotech Ltd. 1-Ethyl-3-methylimidazolium tetrafluoroborate (EMIBF4) (Sigma Aldrich), and polyvinylidene fluoride-co-hexafluoropropylene (PVdF(HFP) (Sigma Aldrich) were used as received and without any further purification. Solvents 4-methyl-2-pentanone (MP), propylene carbonate (PC) were purchased from Sigma-Aldrich Co., and dimethylacetamide (DMAc) from Fluka.

Figure 1. Suggested model of CDC [] and molecular structures of ionic liquid EMIBF4 and polymer PVdF(HFP).

## Preparation of the actuator film

TiC-derived carbon powder, precursor of the actuator electrodes, was produced by Carbon Nanotech Ltd. TiC-derived carbon is synthesized from titanium carbide by chlorination at high temperatures (400 - 900 °C). The reaction product is amorphous carbon powder with particle sizes ranging 2 to 5 μm, and a large quantity of nanopores with pore sizes from 6 to 10 Å in carbon powder particles. The three-layer actuator fabrication process is described below. In the  first stage of investigation different electrode films were prepared to find the optimal composition and identify the suitability of CDC as actuator an electrode material. Respective data with different composition of electrode materials is delivered in Tab. 1. The electrode layer with steady structure and optimal properties was composed of 30 wt% CDC, 35 wt% EMIBF4, and 35 wt% PVdF(HFP).

Firstly PVdF(HFP) pellets were dissolved in DMAc. Concurrently EMIBF4 and CDC powder were mixed in 0,5 ml DMAc and treated in ultrasonic bath at maximum power for 30 minutes. After that, the polymer mixture was added to the CDC/IL suspension and stirred on a magnetic stirrer for 5 minutes and sonicated again for 20 minutes in ultrasonic bath. Finally it was poured out into Teflon mold. Separator was prepared from EMIBF4 and PVdF(HFP) solution wt 1/1, into a polymer solution was added IL and treated on ultrasonic bath for 25 minutes in maximum power and then poured out into a Teflon mold. MP and PC were used as solvents for electrolyte production.

The final step of actuator preparation is hot-pressing, where electrode films and the separator film are hot-pressed together. During solidification process CDC carbon particles deposit from the solution and therefore the upper side of the electrode film in the mold should be placed near the separator, because the conductivity of the electrode film is better on the side which was at the bottom of the mold during the drying process. The conductivity of the electrode material was characterized by standard four point method[].

## Measurement

The displacement measurements were performed using 7 mm × 25 mm size actuator strips. For electrochemical characterization, the actuator strip was connected to the gold electrodes and experimental set-up described in [] was used. Strain and speed of the actuators were characterized using the experimental set-up that is shown in Figure 2. The actuators were clamped in a vertical cantiliver position and the measurements were done in dry air. Actuator driving pulses (retangular) were applied through contacts made out of gold. The measurements were conducted with National Instruments LabView 8.2 control software. The driving voltage was generated by an NI  PCI- 6703  DAQ  board  and  amplified  by electric current from an NS LM675 power op-amp. Voltages with respect to the ground were measured with an NI PCI-6034 DAQ board. One input contact of the CDC actuator sample was also connected to the ground. The electric input current of the sample was measured as a voltage drop over the resistor R. The value of the resistor was 5 Ω.

Actuator bending motions were recorded with a FireWire camera (Dragonfly Express from Point Grey Research Inc), 3,75 frames per second. The camera was set transverse to the actuator that was illuminated from behind using frosted glass. In this camera position, the recorded image of the actuator consists of a single curved contrast line.

The actuator strip showed a bending motion when the voltage was applied. The measured displacement (D) is related to the curvature (1/R) as in eq. 1 []

where (L) is the length (mm) from fixed end of the gold electrodes to the point where actuator strip ends. Measured displacement (D) was transformed to strain difference of two carbon material electrode layers (ε) using the following equation on the assumption that the cross-sections are planes at any position along the actuator.

Where (L) is the length, (D) is the displacement and (W) is the thickness of the CDC based actuator strip (see Fig. 2).

Blocking force was measured at zero displacement using the Panlab MLT0201 load cell. Blocking force was measured 13 mm away from the contacts. The actuator had dimensions 16 x 6 x 0.3 mm, and weighed 48 mg

Figure 2. Experimental set-up for strain and speed characterization.

# Results and discussion

Displacement and blocking force measurements were performed for actuators IV, V and IX. The structure of the other prepared electrodes was not homogeneous enough to fabricate three-layer actuators. One of the typical time profiles of applied voltage, current and blocking force characteristics is represented in Fig. 4. The current profiles showed only charging or discharging. Similar current profiles are inherent to supercapacitors. After charging and before discharging (time period from 60 to 90 sec), the stored charge was collected by short-circuiting the actuator potential to ground, and the adsorbed energy was wasted through the low discharge resistor. Due to the low speed of desorption of ions of the ionic liquid from the porous carbon electrodes, the process of discharging is slow. During charging the current dies away slowly due to the internal resistance of the actuator. This could be the main factor why CDC based actuators give slower speed response compared to CNT based actuators, where conductivity of the electrode is significantly higher. The conductivity of the CDC based electrode side that was on top during the solidification process, was 5.95×10-4 S/cm and the other side’s conductivity was 8.68×10-4 S/cm. These conductivity values show us some unevenness of prepared electrodes and therefore it is very important how the actuator is placed together before hot-pressing. However the capacity of the CDC actuator is much higher compared to CNT based actuators.

High capacitance is expected to be the main reason why CDC based actuator has a very good blocking force to mass ratio. Typically the measured value of blocking force was 79 mN to both sides. This actuator weighed 48 mg. This makes the blocking force to mass ratio to 1.65 N/g. This result means that the blocking force that actuator can generate is 165 times greater that its own mass. To illustrate this result, there are frames from a video on the Fig. 3 where CDC actuator lifts 40 times its own weight. The mass of load is 2.4 g and mass of actuator is 0.06 g.In first no voltage applied to the actuator. In the second frame + 2.8 V was applied for one minute. And in the third frame  -2.8 V was applied for one minute.

Figure 3. Snapshots from a video recording where CDC actuator lifting an external load. The mass of load is 2.4 g and mass of actuator is 0.06 g.

Figure 4. Time profiles of voltage, generated current and blocking force when ±2.8 V square-wave voltage was applied

Table 1 Electrodes prepared to find optimal component ratio for the actuator.

| Sample notation Substance | I | II | III | IV | V | VI | VII | VIII | IX |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CDC carbon (wt%) | 10 | 20 | 30 | 40 | 50 | 60 | 60 | 70 | 30 |
| IL EMIBF4 (wt %) | 70 | 60 | 50 | 30 | 30 | 25 | 30 | 20 | 35 |
| PVdF(HFP) (wt%) | 20 | 20 | 20 | 30 | 20 | 15 | 10 | 10 | 35 |

The cyclic voltammetry of the electrode was measured to estimate the capacitance of the actuator strip. Fig. 5 shows the cyclic voltammograms collected at different sweep rate values. CV measurements were obtained by using two electrode configuration at PARSTAT 2273 advanced electrochemical system. The dimensions of actuator strip were: L=7.1 mm × W=2.8 mm × D=0.35 mm, and it weighed 9.9 mg. (L) being the length, (W) the width, and (D) the thickness of the actuator strip. Voltammograms show only electric double-layer capacitive properties, and Faradaic redox reactions were not observed. The capacitance of the actuator was calculated according to Eq.:

where (C) is the capacitance of the actuator strip in farads, (I) is the current current value in amperes, obtained from CV measurements and (dV/dt) is the sweep rate value in Vs-1. In this study the specific capacitance Cm in farads per gram (F/g) is expressed as follows:

where m is the weight (g) actuator strip.

Figure 5. Cyclic voltammograms of the actuator at different sweep rate values.

# Conclusions

In this paper an actuator composed of CDC, ionic liquid EMIBF4 and non-ionic polymer PVdF(HFP) using layer-by-layer casting method. At first the ratio of primary materials used in electrodes was changed. Optimal component ratio for the electrodes is: 35 wt% PVdF(HFP), 35 wt% EMIBF4 and 30 wt% CDC.  Prepared actuators were characterized by measuring blocking force, maximum strain, power consumption, speed and capacity. Actuators with best electrodes showed very good force values.

ACKNOWLEDGEMENTS

This research was supported by Estonian Information Technology Foundation, Estonian Ministry of Education and Science, also by Archimedes foundation. We like to thank Pille Rinne for reviewing our manuscript.

References

# Comments

Skeleti tehas pole nyyd õige?

?

See on dimethylacetamide (DMAc)

# Endnotes

[] Baughman, R.H., “Conducting polymer artificial muscles,” Synth. Met. 78, 2211-2212 (1996)

[] Roth, S., Baughman, R.H., “Actuators of individual carbon nanotubes,” Curr. Appl. Phys. 2, 311-314 (2002)

[] Fukushima, T., Asaka, K., Kosaka, A., Aida, T., “Fully plastic actuator through layer-by-layer casting with ionic-liquid-based bucky gel,” Angew. Chem. Int. Ed. 44, 2410-2413 (2005)

[] Kyohara, K., Sugino, T., Takeuchi, I., Mukai, K., Asaka, K., “Expansion and contraction of polymer electrodes under applied voltage,” J. Appl. Phys. 105, 063506-1-063506-8 (2009)

[] Conway, B.E. Electrochemical Supercapacitors. Scientific Fundamentals and Technological Applications. Kluwer Academic, Plenum Publishers, New York, 1999

[] Arulepp, M., Leis, J., Lätt, M., Miller, F., Rumma, K., Lust, E., Burke, A.F., „The advanced carbide-derived carbon based supercapacitor,“J. Power Sorces 162, 1460-1466 (2006)

[] Gogotsi, Y., Nikitin, A., Ye, H., Zhou, W., Fischer, J. E., Yi, B., Foley, H. C., Barsoum, M. W. “Nanoporous carbide-derived carbon with tunable pore size,” Nature Materials 2, 591-594 (2003)

[] Simon, P., Gogotsi, Y., „Materials for electrochemical supercapcitors,“ Nature Materials 7, 845-854 (2008)

[] Torop, J., Arulepp, M., Leis, J., Punning, A., Johanson, U., Palmre, V., Aabloo, A., “Nanoporous carbide-derived carbon material-based linear actuators,” Materials 3(1), 9-25 (2010)

[] Gogotsi, Y (ed), Nanomaterials Handbook CRC Press, Boca Raton, FL (2006), 239-282.

[] Punning, A., Johanson, U., Anton, M., Aabloo, A., Kruusmaa, M., “A distributed model of ionomeric polymer metal composite,” J. Intell. Mater. Struct. 20(14), 1711-1724 (2009)

[] Punning, A., Kruusmaa, M., Aabloo, A., “A self-sensing ion conducting polymer metal composite (IPMC) actuator,” Sensors actuators A 136, 656-664 (2007)

[] Takeuchi, I.,  Asaka, K., Kiyohara, K., Sugino, T., Terasawa, N., Mukai, K., Fukushima, T., Aida T., “Electromechanical behavior of fully plastic actuators based on bucky gel containing various internal ionic liquids,” Electrochim. Acta 54,1762-1768 (2009)