Characterization of electromechanically active polymers using EIS

Indrek Must, Karl Kruusamäe, Urmas Johanson, Tarmo Tamm, Andres Punning, Alvo Aabloo

Electromechanically active polymers (EAP) are composite materials that exhibit changes in their mechanical properties when introduced to an electric field. In this paper EAPs that consist of polymer membrane covered with a kind of conductive material are considered. Relatively low electric potential between the layers of conductive material causes transverse dislocation of ions in the polymer membrane, forcing an actuator made of this material to bend. Some of these materials have sensor properties, i.e. external mechanical deformation causes movement of ions which can, for example, be registered as short-circuit current.

The paper at hand considers two different types of bending EAPs: ionic polymer-metal composite (IPMC) and polymer-carbon composite (PCC). IPMC consists of thin ionic polymer membrane (typically Nafion®) which is covered by inert metal electrodes from both sides. The ionic membrane contains suitable counter-ions (Na+ or Li+) and solvent (traditionally water). A comprehensive review of IPMC’s operating principles can be found in [Shahinpoor 2001] and sensorial properties of IPMCs are overviewed in [Pugal 2010]. In recent years, there has been more development in polymer-carbon composite materials. PCC sheet is built using two layers of electrodes containing nanoporous carbon separated by thin ion-permeable polymer film; ionic liquid is used as electrolyte [Torop 2010].

Introduced EAPs possesses unique properties – they are soft, simple in construction, quiet in operation and easily made smaller in size. They offer great interest for various fields, including development of actuators for medical, space, military and MEMS applications. Due to their sensor properties, research of self-sensing actuators and energy harvesting devices is still a great interest in field of electromechanically active polymers.

Electrochemical Impedance Spectroscopy (EIS) offers vast oportunities for investigation of fundamental processes inside IPMC and PCC actuators and sensors. EIS  data can be used to determine energy storage (capacitive behaviour) and dissipation (resistance) properties simultaneously on the same scale and to describe electrical properties of these composite materials by developing complex equivalent circuit models [Bar-Cohen 2002 / Kruusamäe 2009 / Nakamura 2009 / ?]. An IPMC strip can be modelled as a distributed lossy RC line [Punning 2009].

To date, EIS has been implemented for different aspects of these materials. It has been shown that IPMC electrode resistance changes during actuation [Punning 2007, Chen, Tan 2008]. EIS is suggested for determination of the position of the IPMC actuator [Kruusamäe 2009]. It has been shown that impedance of IPMCs strongly relates to hydration level [Leary 1999]. Although, the fundamental processes of actuation in PCCs and IPMCs are still in debate and subject for further investigation.

In current work, impedance characteristics of IPMC and PCC materials are presented. Equivalent schematics of both types of actuators are specified by measuring impedances between and along the surface electrodes. Cross-electrode impedance reflects energetic efficiency of these actuators. In order to better implement the material’s sensory properties, behavior of surface electrode impedance during bending motion is also investigated. In case of IPMC, special attention is paid on effects caused by material degradation after standing unused for a long time or after a large number of working cycles. Identifying the electrical behavior and changes, occurring in the material during aging processes, can help to characterize the materials and to specify their working mechanism.

- Shahinpoor, M., Kim, K. J., “Ionic polymer–metal composites: I. Fundamentals”, Smart Materials and Structures 10(4), 819-833 (2001).

- Pugal, David; Jung, Kwangmok; Aabloo, Alvo; Kim, Kwang (2010) Ionic polymer-metal composite mechanoelectrical transduction: review and perspectives, Polymer International, 59(3), 279-289.

- Torop, Janno; Kaasik, Friedrich; Sugino, Takushi; Aabloo, Alvo; Asaka, Kinji (2010). Electromechanical characteristics of actuators based on carbide-derived carbon. In: Proceedings of the SPIE: Electroactive Polymer Actuators and Devices (EAPAD); San Diego, CA, USA; 7-11 March, 2010.  SPIE, 2010, 76422A-1 - 76422A-7.

- Torop, J., Arulepp, M., Leis, J., Punning, A., Johanson, U., Palmre, V., Aabloo, A., “Nanoporous carbide-derived carbon material-based linear actuators,” Materials 3(1), 9-25 (2010)

- Kruusamäe, K.; Punning, A.; Kruusmaa, M.; Aabloo, A. (2009). Dynamical variation of the impedances of IPMC. Proceedings of SPIE (72870V).SPIE

- Leary S and Bar-Cohen Y 1999 Electrical impedance of ionic polymeric metal composites Proc. SPIE’s 6th Annual Int. Symp. on Smart Structures and Materials vol 3669 (Bellingham,WA: SPIE Optical Engineering Press) pp 81–6

- (Z. Chen, X. Tan, A control-oriented and physics-based model for ionic polymer-metal composite actuators, IEEE/ASME Transactions on Mechatronics 13 (5) (2008) 519 – 529.)

- Punning, A.; Kruusmaa, M.; Aabloo, A. (2007). Surface resistance experiments with IPMC sensors and actuators. Sensors and Actuators A: Physical, 133(1), 200 - 209.

- Characterization of the electromechanical properties of ionomeric polymer-metal composite (IPMC) Yoseph Bar-Cohen, Xiaoqi Bao, Stewart Sherrit, and Shyh-Shiuh Lih, Proc. SPIE 4695, 286 (2002), DOI:10.1117/12.475173

- T. Nakamura, T. Ihara, T. Horiuchi, T. Mukai, and K. Asaka: "Measurement and Modeling of Electro-Chemical Properties of Ion Polymer Metal Composite by Complex Impedance Analysis", SICE Journal of Control, Measurement, and System Integration, Vol.2, No.6, pp.373-378, 2009.11．

- Punning, A.; Johanson, U.; Anton, M.; Aabloo, A.; Kruusmaa, M. (2009). A Distributed Model of Ionomeric Polymer Metal Composite. Journal of Intelligent Material Systems and Structures, 20(14), 1711 - 1724.