Characterization of electromechanically active polymers using EIS

Indrek Must, Karl Kruusamäe, Urmas Johanson, Tarmo Tamm, Andres Punning, Alvo Aabloo

Electromechanically active polymers (EAP) are composite materials that exhibit changes in their mechanical properties when introduced to an electric field. In this paper EAPs that consist of polymer membrane covered with a kind of conductive material are considered. Relatively low electric potential between the layers of conductive material causes transverse dislocation of ions in the composite, forcing an actuator made of this type of material to bend. Some of these materials also have sensor properties, i.e. external mechanical deformation causes movement of ions which can, for example, be registered as short-circuit current.

The paper at hand considers two different types of bending EAPs: ionic polymer-metal composite (IPMC) and polymer-carbon composite (PCC). IPMC consists of thin ionic polymer membrane (typically Nafion®) which is covered by inert metal electrodes from both sides. The ionic membrane contains suitable counter-ions (Na+ or Li+) and solvent (traditionally water). A comprehensive review of IPMC’s operating principles can be found in [1] and sensorial properties of IPMCs are overviewed in [2]. In recent years, the development of PCC materials has gained increasing attention. PCC sheet is built using two layers of electrodes containing nanoporous carbon separated by thin ion-permeable polymer film; ionic liquid is used as electrolyte [3, 4].

Introduced EAPs possess unique properties in comparison with conventional electro-mechanical actuators – they are soft, quiet in operation, simple in construction and easily made smaller in size. Therefore, they are considered attractive for development of actuators in the areas of e.g. medical, space, military or MEMS applications. Moreover, due to their sensor properties, research of self-sensing actuators and energy harvesting devices also offers a great interest in the field of EAPs.

Electrochemical Impedance Spectroscopy (EIS) provides vast oportunities for investigation of fundamental processes inside IPMC and PCC actuators and sensors. EIS  data can be used to determine energy storage (capacitive behaviour) and dissipation (resistance) properties simultaneously on the same scale and to describe electrical properties of these composite materials by developing complex equivalent circuit models. One of the basis of current paper is the approach that an IPMC strip can be modelled as a distributed lossy RC line [5].

To date, EIS has been applied in several papers in characterization of the composition and behavior of IPMCs [6, 7, 8, 9, 10], however, the amount of papers regarding this subject currently remains relatively low. Moreover, the fundamental processes of actuation in PCCs and IPMCs are still on a debate and give subject for further investigation. Therefore the intention of current paper is to present a systematic approach for the impedance study of these materials.

In this work, impedance characteristics of IPMC and PCC materials are presented. Equivalent schematics of both types of actuators are specified by measuring impedances between and along the surface electrodes. Cross-electrode impedance helps determination of energetic efficiency of these actuators. For better utilization of materials’ sensory properties, behavior of surface electrode impedance during bending motion is also investigated. In case of IPMC, special attention is paid on effects caused by material degradation when standing unused for a long time or after a large number of working cycles. Identifying the electrical behavior and changes, occurring in the material during aging processes, can help to further characterize these materials and to specify their working mechanism.

References

- Shahinpoor, M., Kim, K. J., “Ionic polymer–metal composites: I. Fundamentals”, Smart Materials and Structures 10(4), 819-833 (2001).

- Pugal, D., Jung, K., Aabloo, A., Kim, K., “Ionic polymer-metal composite mechanoelectrical transduction: review and perspectives”, Polymer International  59(3), 279-289 (2010).

- Torop, J., Kaasik, F., Sugino, T., Aabloo, A., Asaka, K., “Electromechanical characteristics of actuators based on carbide-derived carbon”, Proceedings of the SPIE  7642, 76422A (2010).

- Torop, J., Arulepp, M., Leis, J., Punning, A., Johanson, U., Palmre, V., Aabloo, A., “Nanoporous carbide-derived carbon material-based linear actuators,” Materials 3(1), 9-25 (2010).

- Punning, A., Johanson, U., Anton, M., Aabloo, A., Kruusmaa, M., “A Distributed Model of Ionomeric Polymer Metal Composite”, Journal of Intelligent Material Systems and Structures 20(14), 1711 - 1724 (2009).

- Kruusamäe, K.; Punning, A.; Kruusmaa, M.; Aabloo, A., “Dynamical variation of the impedances of IPMC”, Proceedings of SPIE 7287, 72870V (2009).

- Leary, S., Bar-Cohen, Y., “Electrical impedance of ionic polymeric metal composites”, Proceedings of SPIE 3669, 81-86 (1999).

- Chen, Z., Tan, X., “A control-oriented and physics-based model for ionic polymer-metal composite actuators”, IEEE/ASME Transactions on Mechatronics 13(5), 519 – 529 (2008).

- Takagi, K., Nakabo, Y., Luo, Z. W., Asaka, K., “On a distributed parameter model for electrical impedance of ionic polymer,” Proceedings of SPIE 6524, 652416 (2007).

- Nakamura, T., Ihara, T., Horiuchi, T., Mukai, T., Asaka, K., "Measurement and Modeling of Electro-Chemical Properties of Ion Polymer Metal Composite by Complex Impedance Analysis", SICE Journal of Control, Measurement, and System Integration 2(6), 373-378 (2009).