Molecular Dynamics simulations of Carbon-EMI-BF4-PTFE composites for electroactive polymer actuators.

Autors: Endel Soolo, Anti Liivat, Heiki Kasemägi, Daniel Brandell, Alvo Aabloo

# Abstract

# Introduction

Electroactive polymers (EAP) are materials, which change their shape while apply voltage to them They have good potential for developing lightweight actuators in small and microscale for space industry[intro4], biomimetic robotics[intro1] [intro6] and other microapplications[intro5] like microfluidics control etc

There are several types of EAP-s. Ionic EAPs are the materials which act due to ion/ionpair relocation. The advantage of these actuators is low voltage to drive them.

The disadvantage of these materials is commonly small absolute force and low electromechanical efficiency. There are proposed several practical solutions to enhance for force, like specific shape of EAP actuator [intro2] are multiple actuator bundle [intro3]. However it is vital for efficiency increase to understand physical properties of material at atomistic level. It enables to understand process of actuation and ion migration details[intro7].

To increase the actuation speed and efficiency it is necessary to increase ion migration speed[intro8]. In case of simple ion conducting polymers there has been attempts to add nanoparticles[intro9] into polymer. There is also possibility to use ionic liquid [intro8] instead of water.

Current work focuses on molecular dynamics study of ionic polymer ioniq-liquid composite materials. The material is carbide derived carbo based composite which includes some ppolytetrefluoroen[PTFE) and ionic liquid [EMI-BF4)[references to ourselves…]

A discussion is necessary here on the carbon-PTFE-IL systems. What function do they serve for artificial muscles? Have these materials been investigated experimentally? What are their advantages, and how do they behave? And what components do they consist of? What is the specific role of PTFE and carbon?

Furthermore: what specific aspect would we like to investigate in this study?

# Methodology

The method of Molecular Dynamics is based on periodically calculating the forces acting on each atom of a model, based on a forcefield composed of bond stretch, valence angle flex and dihedral torsion reactions and Van der Waals and electrostatic interactions. The net force acting on each atom, together with its current position and speed are used to find the position and speed at the next timestep. From the continuous history of atom coordinates in time can diffusion coefficients and other macroscopic characteristics be calculated while the movements can also be analysed on the more subtle molecular level.

Lisada viited

## Simulated systems

| System name | PTFE | Carbon | EMI+BF4 | Electric field values |
| --- | --- | --- | --- | --- |
|  | mass % | chains | mass % | Platelets | mass % | ion pairs |  |
|  | 2.7% | 1 | 35.6% | 57 | 61.7% | 132 | 0; 50V/mm |
|  | 5.4% | 2 | 32.6% | 52 | 62.0% | 132 | 0; 50V/mm; 0 (recovery after removal of the electric field) |
|  | 8.1% | 3 | 32.6% | 52 | 59.3% | 126 | 0; 50V/mm |
|  | 16.2% | 6 | 30.7% | 49 | 53.1% | 113 | 0; 50V/mm |

Table 1: Simulated systems

Why simulate four different systems?

The following molecules were present in the simulation cell:

- Carbon in the form of graphene fragments with 22 atoms each. (C22)

- Ethyl-methyl-imidazol ions (EMI)

- Boron tetrafluorate anions (BF4)

- Polytetrafluoroethylene fragments: CF3-(CF2)20-CF3 (PTFE)

The introduction mentions CDC, but here it is grapheme??

The concentrations of the components were based on a electrode compound used in supercapacitors [ref.req.]

## Simulation box

The size of simulation box for all cases was 40x40x40 A. The cubic symmetry was retained over all simulations.The Inital models were generated by three steps. First, a  300 ns MD simulation of carbon placelet was simulated in vacuo and a selection of its possible shapes was taken from the simulation history. The simulatiuon temperature was 293K ….etc….

As a next step, a 40 Angström cubic box was filled with porous carbon by adding one randomly selected shape of the carbon piece at a time at random orientation and rotation in the simulation box. The configuration acceptence criteria was based on total energy difference while adding a sincle carbon placelet. In-house Monte Carlo software mcgen was used [][This procedure is difficult to understand – can it be described more easily?]

Next the ionic liquid was inserted by same methodology. To avoid charge buildup in the box, the anions and cations were inserted intermittently (one cation, then one anion) with the energy check after each ion.

At last, the PTFE molecules were generated randomly, one monomer at a time, only checking for geometric constraints and not for energy.[mcgen]

[Is the resulting material a complete mix of all components?]

## Force fields

Several components of the Forde field was found elsewhere. Force field for carbon was published by Henske et al [Hentscke]. Force field for PTFE was described in [Okada]. Cation-anion interaction forcefield is described in [Lopes].

The Van der Waals forces of the separate force fields were decribed as Lennard Jones type and in case there was no previously published force field available the following combination rule was applied: [what rules?]

[formula comes out wrong…].,

where….

The force field is described in Tables 2 to 5. [If these are published, it is necessary to republish?]

| Substance | Atom/Ion label | Charge /e | Mass /au |  |  | number per molecule |
| --- | --- | --- | --- | --- | --- | --- |
| Carbon | C | 0 | 12.0107[webelements] |  |  | 22 |
| PTFE | C9 | 0.63[okada] | 12.0107[webelements] |  |  | 2 |
|  | C8 | 0.48[okada] | 12.0107[webelements] |  |  | 20 |
|  | F9 | -0.21[okada] | 18.9984[webelements] |  |  | 6 |
|  | F8 | -0.24[okada] | 18.9984[webelements] |  |  | 40 |
| EMI | NA (nitrogen) | 0.15[Lopes] | 14.0067[webelements] |  |  | 2 |
|  | CR (carbon) | -0.11[Lopes] | 12.0107[webelements] |  |  | 1 |
|  | CW | -0.13[Lopes] | 12.0107[webelements] |  |  | 2 |
|  | C1 | -0.17[Lopes] | 12.0107[webelements] |  |  | 2 |
|  | CE | -0.05[Lopes] | 12.0107[webelements] |  |  | 1 |
|  | HA | 0.21[Lopes] | 1.00794[webelements] |  |  | 3 |
|  | H1 | 0.13[Lopes] | 1.00794[webelements] |  |  | 5 |
|  | HC | 0.06[Lopes] | 1.00794[webelements] |  |  | 3 |
| BF4 | B | +1.1504[Lopes] | 10. 811[webelements] |  |  | 1 |
|  | F | -0.5376[Lopes] | 18.9984[webelements] |  |  | 4 |

Table 2: Forcefield parameters of single atoms

| Formula | Atom label 1 | Atom label 2 | k or k12 | K6 | r0 | number per molecule |
| --- | --- | --- | --- | --- | --- | --- |
| 1 |  |  |  |  |  |  |
| 2 |  |  |  |  |  |  |

Table 3: Forcefield bond parameters

Harmonic bond potential:

(1)

12-6 type two-atom potential:

(2)

In the formulas, U is the potential energy of the bond, r is the interatomic distance and r0, k12 and k6 are bond parameters.

| Formula | Atom label 1 | Atom label 2 | Atom label 3 | K |  | number per molecule |
| --- | --- | --- | --- | --- | --- | --- |
| 3 |  |  |  |  |  |  |

Table 4: Forcefield valence angle potential parameters

Harmonic angle potential:

(3)

| Formula | Atom label 1 | Atom label 2 | Atom label 3 | Atom label 4 | A | B | C |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 4 |  |  |  |  |  |  |  |
| 5 |  |  |  |  |  |  |  |
| 6 |  |  |  |  |  |  |  |

Table 5: Forcefield dihedral parameters

„cos“ dihedral potential:

(4)

„cosb“ dihedral potential:

(5)

„cos3“ dihedral potential:

(6)

## Simulations

Each system was first run through a 2 ns long MD simulation using the NVT ensemble in the original 40Å cubic cell to relieve internal stresses left from the generation. Then external electic field of 50V/mm was added and the simulations continued for next 2 ns [electrical field simulations have not been motivated!]. Thereafter the simulations, both with and without external electric field, were continued for the next 10 ns using a NPT ensemble and Nose-Hoover barostat with pressure of 1 atm and relaxation time of 0.3 ps. For verification purposes, the initial NVT simulations were also continued until 10 ns long from the beginning. In the NVT simulation of the material with 5.4% polymer content, an unusual layered structure appeared in the electric field. The NVT simulation of this system was carried on for another 10 ns with E=0 to analyse how its structure would respond to the removal of the electric field.

The simulations used Verlet Leapfrog algorithm with 1 fs timestep. Temperature was kept at 293K by a Nose-Hoover thermostat with 0.1 ps relaxation time. Ewald summation with 10-5 precision was used for the electrostatics.

## Analysis methods

### RDF

### MSD

### Time evolution histogram

The aromatic ring centre locations were calculated for the cations and marked as points X.

The first coordination sphere radius for anions around a cation was found from the RDF of X..B.

The distribution of coordination times was composed by counting the number of

consecutive simulation snapshots (taken after every 1 picosecond) that each anion spent in the

coordination sphere of a unchanged cation. The results were shown with log-log axes and

the coefficients for the equation p(t)=b*t^a were calculated. [I don’t understand this!?]

### Inertia ellipsoid shape

From each snapshot the cation centers' (points X) and the anion central atoms'

(B) coordinates were extracted.  For each group of one cation and all of the

anions coordinated with it, inertia tensors were calculated, assuming the mass

of the cation to be concentrated in point X and the mass of each anion to its

central B atom. The distributions of the inertia tensors greatest, next

greatest and least principal axes were calculated.

The shape of the inertia ellipsoid shows whether the anions prefer to stay in

one plane or are distributed uniformly over a sphere.

# System description

# Analysis

The mobility of both the anions and cations was greatest with the polymer content of 5.4% (fig.). The ion mobility was  greater with the electric field applied (fig.). The mobility of the polymer was also greatest at 5.4% polymer content (fig.), increasing with the added electric field (fig.).

The first coordination sphere radius for cation-anion pairs (X...F) was  6.1Å. The less defined second coordination sphere had 7.5Å radius. Increase of the polymer content and applying the electric field was associated with more of  anion-cation coordination (fig.), (fig.) and lessened ion coordination with graphite (fig.).

The increased mobility could have been facilitated by coordination with the more mobile polymer chain and detachment from the stationary graphite particles.

# Results

# References

- [mcgen]

- [Hentscke]

- [Okada] http://dx.doi.org/10.1080/08927029908022072

- [Lopes] http://dx.doi.org/10.1021/jp0362133

- [webelements] http://webelements.com

- [intro1] M. Anton, A. Punning, A. Aabloo, M. Listak, M. Kruusmaa, Proceedings of TAROS 2004 “Towards Autonomous Robotic Systems”

- [intro2] H. Wang, C. Li, ICMTMA, http://dx.doi.org/10.1109/ICMTMA.2009.114

- [intro3] D. Fernández, L. Moreno, J. Baselga, Proc SPIE Int Soc Opt Eng, http://dx.doi.org/10.1117/12.599108

- [intro4] Y. Bar-Cohen, S. P. Leary, M. Shahinpoor, J. S. Harrison, J. G. Smith, Proc. SPIE, Vol. 3669, 57 (1999); doi:10.1117/12.349708  http://dx.doi.org/10.1117/12.349708

- [intro5] N. Di Spigna, P. Chakraborti, P. Yang, T. Ghosh, P. Franzon, Proc. SPIE, Vol. 7287, 72871K (2009); http://dx.doi.org/10.1117/12.816009

- [intro6] Y. Liu, L. Shi, L. Liu, Z. Zhang, J. Leng, Proc. SPIE, Vol. 6927, 69271A (2008); http://dx.doi.org/10.1117/12.775946

- [intro7] Y. Bar-Cohen (editor), Electroactive Polymer (EAP) Actuators as Artificial Muscles: Reality, Potential, and Challenges, Second Edition (SPIE Press Book), ISBN: 9780819452979

- [intro8] F. Carpi, E. Smela, Biomedical Applications of Electroactive Polymer Actuators, Wiley 2009, ISBN: 978-0-470-77305-5

- [intro9] H. Kasemägi, M. Klintenberg, A. Aabloo, J. O. Thomas, Solid State Ionics, Volume 147, Issues 3-4, April 2002, Pages 367-375, http://dx.doi.org/10.1016/S0167-2738(02)00013-9