Molecular Dynamics simulations of Carbon-EMI-BF4-PTFE composites for electroactive polymer actuators.

Authors: Endel Soolo, Anti Liivat, Heiki Kasemägi, Daniel Brandell, Alvo Aabloo

# Abstract

# Introduction

Electroactive polymers (EAP) are materials, which change their shape when voltage is applied to them. They have good potential for developing lightweight actuators in small and microscale for space industry[intro4, intro4a], medicine[intro4a], biomimetic robotics[intro1] [intro6] and other microapplications[intro5] like microfluidics control etc.

There are several types of EAP-s. Ionic EAPs are the materials which act due to ion/ionpair relocation. The advantage of these actuators is low control voltage required.

The disadvantage of these materials is commonly small absolute force and low electromechanical efficiency. There are proposed several practical solutions to enhance for force, like specific shape of EAP actuator [intro2] are bundling of multiple actuators [intro3]. However it is vital for efficiency increase to understand physical properties of material at atomistic level. It enables to understand the details of the process of actuation and ion migration[intro7].

To increase the actuation speed and efficiency it is necessary to increase ion migration speed[intro8]. In case of simple ion conducting polymers there have been attempts to add nanoparticles[intro9] into polymer. There is also possibility to use ionic liquid [intro8] instead of water. Carbon nanotube sheets have been demonstated to work as actuators, harnessing a quantum chemical effect not susceptible to the destructive processes happening in EAP-s based on Faraday processes [Baughman].

Ionic liquid has been used as the electrolyte with good long-term stability in dry environment in Nafion based EAP [Bennett] and also with carbon nanotubes in an ionic liquid gel supported by polymer [Asaka].

Current work focuses on molecular dynamics study of ionic polymer ionic-liquid composite materials. The material is carbide derived carbon based composite which includes some polytetrefluoroen [PTFE] and ionic liquid [EMI-BF4] [references to ourselves…]. The material would be used for the electrode layers of an actuator with IL gel electrolyte like the Bucky gel in [Asaka]. Both CDC and nanotubes have large gravimetric surface areas. [ref. req.]

A discussion is necessary here on the carbon-PTFE-IL systems. What function do they serve for artificial muscles? Have these materials been investigated experimentally? What are their advantages, and how do they behave? And what components do they consist of? What is the specific role of PTFE and carbon?

The mixture is artificial muscle material. To make the muscle, two sheets of this material would be put together with a membrane in between.

So, are they electrodes, electrolytes, or both? What happens during actuation? And, some of the questions are still unaswered...

[About the usage of ionic liquid, I will add reference to some work referred in [biomedbook]

Carbon (nanotubes) with ionic liquid has been tested experimentally by Kinji Asaka.

EAPs with ionic liquid have also been tested experimentally by Barbar J. Akle.

The results of these studies needs to be summarised in the introduction. But, has no one studied this system experimentally?

Furthermore: what specific aspect would we like to investigate in this study?

We are most interested in the effect of the carbon content to the ion mobility.

Why?

# Methodology

The method of Molecular Dynamics is based on periodically calculating the forces acting on each atom of a model, based on a forcefield composed of bond stretch, valence angle flex and dihedral torsion reactions and Van der Waals and electrostatic interactions. The net force acting on each atom, together with its current position and speed are used to find the position and speed at the next timestep. From the continuous history of atom coordinates in time can diffusion coefficients and other macroscopic characteristics be calculated while the movements can also be analysed on the more subtle molecular level.

Add references

## Simulated systems

Why simulate four different systems?

Why is there a variation in the proportions between carbon and the IL?

In the experimental methods, the lowest possible polymer concentration able to keep the EAP mechanically stable, is .... % [ref. req.]. Carbon is the most conducting part of the EAP [req. req.] and the polymer has only the supporting role [ref. req.]. The current research was focused on the question whether it would be beneficial to increase the carbon content above the experimentally tested limits, i.e. what effect would it have on the ion mobility and the ionic conductivity of the material.

The polymer content was varied by starting with the lowest polymer content and intermittently replacing either some carbon platelets or some IL ions with a PTFE chain, keeping the density as close to constant as allowed by the requirement of integral numbers of particles in the simulation cell. The mass ratio of carbon to IL varied from 0.52 to 0.58 due to the model creation process.

| System nr. | PTFE | Carbon | EMI+BF4 | Electric field values |
| --- | --- | --- | --- | --- |
|  | mass % | chains | mass % | platelets | mass % | ion pairs |  |
| 1 | 2.7% | 1 | 35.6% | 57 | 61.7% | 132 | 0; 50V/mm |
| 2 | 5.4% | 2 | 32.6% | 52 | 62.0% | 132 | 0; 50V/mm; 0 (recovery after removal of the electric field) |
| 3 | 8.1% | 3 | 32.6% | 52 | 59.3% | 126 | 0; 50V/mm |
| 4 | 16.2% | 6 | 30.7% | 49 | 53.1% | 113 | 0; 50V/mm |

Table 1: Simulated systems

The following molecules were present in the simulation cell:

- Carbon in the form of graphene fragments with 22 atoms each. (C22)

- Ethyl-methyl-imidazol ions (EMI)

- Boron tetrafluorate anions (BF4)

- Polytetrafluoroethylene fragments: CF3-(CF2)20-CF3 (PTFE)

The introduction mentions CDC, but here it is grapheme??

CDC carbon is used because it is one of the finest carbon powders available, almost composed of separate graphene sheets.

Is graphene really a good approximation for CDCs? Has somebody else used this?

The concentrations of the components were based on a electrode compound used in supercapacitors [ref.req.]

## Simulation box

The size of simulation box for all cases was 40x40x40 A. The box was cubic with the symmetry being retained in all simulations. The amorphous carbon part of the inital models were generated by first inserting carbon platelets in random orientations. The ionic liquid molecules were thereafter inserted into the spaces between the carbon platelets, and, finally the PTFE polymer was grown into the last empty spaces, also by the Monte Carlo method.

[what does “full of” mean?] [porous carbon is mentioned only here! Is this amorphous carbon, or graphene?] [how were these pores found/defined?] [by Monte-Carlo?]

The individual carbon platelet shapes were created by a 300 ns MD simulation of a carbon placelet in vacuo at temperature of ... K. 10 configurations were taken from that simulation, one after every 30 ns. Repeatedly, one of the 10 configurations was randomly selected,  rotated by a random angle and positioned at a random place in  the box. If the insertion of that platelet in such position increased the total energy of the box by ΔE, then with probability commensurate with the Boltzmann factor exp(-ΔE/kT) that insertion was accepted, otherwise another configuration, orientation and position were tried. In-house Monte Carlo software mcgen [mcgen] was used for all operations of the initial model generation, except the MD simulation of the carbon platelet that was done with DL_POLY [dlpoly].

The ionic liquid was inserted by the same methodology as the carbon. To avoid charge buildup in the box, the anions and cations were inserted intermittently (one cation, then one anion) with the energy being checked after each ion.

The PTFE molecules were generated one monomer at a time, only checking for geometric constraints and not for interaction energy with the previous molecules.[mcgen]

[Is the resulting material a complete mix of all components?] [Yes, it is the complete material for the outer layers of an artificial muscle.]

## Force fields

Several components of the Forde field was found elsewhere. Force field for carbon was published by Henske et al [Hentscke]. Force field for PTFE was described in [Okada]. Cation-anion interaction forcefield is described in [Lopes].

The Van der Waals forces of the separate force fields were decribed as Lennard Jones type and in case there was no previously published force field available the following combination rule was applied:  [what rules?]  ., where ε1, ε2, ε are the potential well depths and σ1, σ2, σ are the Lennard-Jones radii for the first and second atom, and for the combined potential, respectivelty.

The force field is described in Tables 2 to 5.[If these are published, it is necessary to republish?]

The force fields for separate PTFE and separate EMI-BF4 have been published before. I have just put them together as a forcefield for the complete EAP material.

| Substance | Atom/Ion label | Charge /e | Mass /au |  |  | number per molecule |
| --- | --- | --- | --- | --- | --- | --- |
| Carbon | C | 0 | 12.0107[webelements] |  |  | 22 |
| PTFE | C9 | 0.63[okada] | 12.0107[webelements] |  |  | 2 |
|  | C8 | 0.48[okada] | 12.0107[webelements] |  |  | 20 |
|  | F9 | -0.21[okada] | 18.9984[webelements] |  |  | 6 |
|  | F8 | -0.24[okada] | 18.9984[webelements] |  |  | 40 |
| EMI | NA (nitrogen) | 0.15[Lopes] | 14.0067[webelements] |  |  | 2 |
|  | CR (carbon) | -0.11[Lopes] | 12.0107[webelements] |  |  | 1 |
|  | CW | -0.13[Lopes] | 12.0107[webelements] |  |  | 2 |
|  | C1 | -0.17[Lopes] | 12.0107[webelements] |  |  | 2 |
|  | CE | -0.05[Lopes] | 12.0107[webelements] |  |  | 1 |
|  | HA | 0.21[Lopes] | 1.00794[webelements] |  |  | 3 |
|  | H1 | 0.13[Lopes] | 1.00794[webelements] |  |  | 5 |
|  | HC | 0.06[Lopes] | 1.00794[webelements] |  |  | 3 |
| BF4 | B | +1.1504[Lopes] | 10. 811[webelements] |  |  | 1 |
|  | F | -0.5376[Lopes] | 18.9984[webelements] |  |  | 4 |

Table 2: Forcefield parameters of single atoms

| Formula | Atom label 1 | Atom label 2 | k or k12 | k6 | r0 | number per molecule |
| --- | --- | --- | --- | --- | --- | --- |
| 1 |  |  |  |  |  |  |
| 2 |  |  |  |  |  |  |

Table 3: Forcefield bond parameters

Harmonic bond potential:

(1)

12-6 type two-atom potential:

(2)

In the formulas, U is the potential energy of the bond, r is the interatomic distance and r0, k12 and k6 are bond parameters.

| Formula | Atom label 1 | Atom label 2 | Atom label 3 | k |  | number per molecule |
| --- | --- | --- | --- | --- | --- | --- |
| 3 |  |  |  |  |  |  |

Table 4: Forcefield valence angle potential parameters

Harmonic angle potential:

(3)

| Formula | Atom label 1 | Atom label 2 | Atom label 3 | Atom label 4 | A | B | C |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 4 |  |  |  |  |  |  |  |
| 5 |  |  |  |  |  |  |  |
| 6 |  |  |  |  |  |  |  |

Table 5: Forcefield dihedral parameters

„cos“ dihedral potential:

(4)

„cosb“ dihedral potential:

(5)

„cos3“ dihedral potential:

(6)

## Simulations

Each system was first run through a 2 ns long MD simulation using the NVT ensemble in the original 40Å cubic cell to relieve internal stresses left from the generation. To emulate the working conditions of an EAP, an external electic field of 50V/mm was then added and the simulations continued for next 2 ns. [electrical field simulations have not been motivated! ] [We need to discuss that.] Thereafter the simulations, both with and without external electric field, were continued for the next 10 ns using a NPT ensemble and Nose-Hoover barostat with pressure of 1 atm and relaxation time of 0.3 ps. For verification purposes, the initial NVT simulations were also continued until 10 ns long from the beginning. In the NVT simulation of the material with 5.4% polymer content, an unusual layered structure appeared in the electric field. The NVT simulation of this system was carried on for another 10 ns with E=0 to analyse how its structure would respond to the removal of the electric field.

The simulations used Verlet Leapfrog algorithm with 1 fs timestep. Temperature was kept at 293K by a Nose-Hoover thermostat with 0.1 ps relaxation time. Ewald summation with 10-5 precision was used for the electrostatics.

## Analysis methods

### RDF

### MSD

### Time evolution histogram

The aromatic ring centre locations were calculated for the cations and marked as points X.

The first coordination sphere radius for anions around a cation was found from the RDF of X..B.

The distribution of coordination times was composed by counting the number of

consecutive simulation snapshots (taken after every 1 picosecond) that each anion spent in the

coordination sphere of a unchanged cation. The results were shown with log-log axes and

the coefficients for the equation p(t)=b*t^a were calculated. [I don’t understand this!?] [I will rewrite.]

### Inertia ellipsoid shape

From each snapshot the cation centers' (points X) and the anion central atoms'

(B) coordinates were extracted.  For each group of one cation and all of the

anions coordinated with it, inertia tensors were calculated, assuming the mass

of the cation to be concentrated in point X and the mass of each anion to its

central B atom. The distributions of the inertia tensors greatest, next

greatest and least principal axes were calculated.

The shape of the inertia ellipsoid shows whether the anions prefer to stay in

one plane or are distributed uniformly over a sphere.

# System description

# Analysis

The mobility of both the anions and cations was greatest with the polymer content of 5.4% (fig.). The ion mobility was  greater with the electric field applied (fig.). The mobility of the polymer was also greatest at 5.4% polymer content (fig.), increasing with the added electric field (fig.).

The first coordination sphere radius for cation-anion pairs (X...F) was  6.1Å. The less defined second coordination sphere had 7.5Å radius. Increase of the polymer content and applying the electric field was associated with more of  anion-cation coordination (fig.), (fig.) and lessened ion coordination with graphite (fig.).

The increased mobility could have been facilitated by coordination with the more mobile polymer chain and detachment from the stationary graphite particles.

# Results

# References

- [mcgen] E. Soolo, J. Karo, H. Kasemägi, M. Kruusmaa, A. Aabloo, Proc. SPIE, 6168, 61682A (2006); http://dx.doi.org/10.1117/12.658664

- [Hentscke]

- [Okada] O. Okada, K. Oka, S. Kuwajima, K. Tanabe, Molecular Simulation, 21, 325-342, (1999); http://dx.doi.org/10.1080/08927029908022072

- [Lopes] J. N. C. Lopes, J. Deschamps, A. A. H. Pádua, J. Phys. Chem. B, 108, 2038–2047, (2004); http://dx.doi.org/10.1021/jp0362133

- [webelements] http://webelements.com

- [intro1] M. Anton, A. Punning, A. Aabloo, M. Listak, M. Kruusmaa, Towards Autonomous Robotic Systems (TAROS 2004), University of Essex, 1-7, (2004); http://www.essex.ac.uk/csee/research/publications/technicalreports/2004/csm415/Anton_etal.pdf

- [intro2] H. Wang, C. Li, ICMTMA'09. International Conference on Measuring Technology and Mechatronics Automation, 1, 73-76, (2009); http://dx.doi.org/10.1109/ICMTMA.2009.114

- [intro3] D. Fernández, L. Moreno, J. Baselga, Proc SPIE Int Soc Opt Eng, 5759, 361, (2005);  http://dx.doi.org/10.1117/12.599108

- [intro4] Y. Bar-Cohen, S. P. Leary, M. Shahinpoor, J. S. Harrison, J. G. Smith, Proc. SPIE, Vol. 3669, 57 (1999); doi:10.1117/12.349708  http://dx.doi.org/10.1117/12.349708

- [intro4a] Y. Bar-Cohen, Proc SPIE Int Soc Opt Eng, 4329, 1-6, (2001); http://dx.doi.org/10.1117/12.432639

- [intro5] N. Di Spigna, P. Chakraborti, P. Yang, T. Ghosh, P. Franzon, Proc. SPIE, 7287, 72871K, (2009); http://dx.doi.org/10.1117/12.816009

- [intro6] Y. Liu, L. Shi, L. Liu, Z. Zhang, J. Leng, Proc. SPIE, 6927, 69271A, (2008); http://dx.doi.org/10.1117/12.775946

- [intro7] Y. Bar-Cohen (editor), Electroactive Polymer (EAP) Actuators as Artificial Muscles: Reality, Potential, and Challenges, Second Edition (SPIE Press Book), ISBN: 9780819452979

- [intro8] F. Carpi, E. Smela, Biomedical Applications of Electroactive Polymer Actuators, Wiley 2009, ISBN: 978-0-470-77305-5

- [intro9] H. Kasemägi, M. Klintenberg, A. Aabloo, J. O. Thomas, Solid State Ionics, Volume 147, Issues 3-4, April 2002, Pages 367-375, http://dx.doi.org/10.1016/S0167-2738(02)00013-9

- [Baughman] R. H. Baughman, C. Cui, A. A. Zakhidov, Z. Iqbal, J. N. Barisci, G. M. Spinks, G. G. Wallace, A. Mazzoldi, D. De Rossi, A. G. Rinzler, O. Jaschinski, S. Roth, M. Kertesz, Science 284, 1340 (1999); http://dx.doi.org/10.1126/science.284.5418.1340

- [Bennett] M. D. Bennett, D. J. Leo, Sensors and Actuators A, 115, 79 (2004); http://dx.doi.org/10.1016/j.sna.2004.03.043

- [eapbook] Y. Bar-Cohen (editor), Electroactive Polymer (EAP) Actuators as Artificial Muscles: Reality, Potential, and Challenges, Second Edition (SPIE Press Book), ISBN: 9780819452979

- [biomedbook] F. Carpi (editor), E. Smela (editor), Biomedical Applications of Electroactive Polymer Actuators, Wiley 2009, ISBN: 978-0-470-77305-5

- [Asaka] T. Fukushima, K. Asaka, A. Kosaka, T. Aida, Angew. Chem. Int. Ed. 44, 2410-2413, (2005); http://dx.doi.org/10.1002/anie.200462318