Molecular Dynamics simulations of Carbon-EMI-BF4-PTFE composites for electroactive polymer actuators.

Authors: Endel Soolo, Anti Liivat, Heiki Kasemägi, Daniel Brandell, Alvo Aabloo

# Abstract

# Introduction

Electroactive polymers (EAP) are materials, which change their shape in response to electric stimulation, useful for lightweight actuators in small and microscale for space industry[Bar-Cohen-1999, Bar-Cohen-2001], medicine[Bar-Cohen-2001], biomimetic robotics[Mart, Liu-2008] and other microapplications[Spigna] like microfluidics control, etc.

The many types of EAPs can be divided into two basic categories: ionic and electronic.

Electronic EAPs harnessing electrostatic forces in the material, requiring large control voltages in the kV range to operate. Ionic EAPs act due to ion/ionpair relocation. They offer low control voltage (1-10V)[eapbook], which is better suited for use in miniature devices.

The current ionic EAPs offer commonly only small force, low electromechanical efficiency and have short lifetime compared with traditional electromechanical actuators. For improving the total force of an actuator, several practical solutions have been proposed, like specific shape of EAP actuator [Wang] or bundling of multiple actuators [Fernandez]. For increasing efficiency, however, it is vital to understand the physical properties of the material and the details of the process of actuation and ion migration at atomistic level[eapbook].

The ionic EAP materials are composed of three basic components. First, the porous elctrode material, where carbon is often used, but RuO2 [Akle] can also be used. Several types of microporous carbon composite materials have been used in supercapacitors where charge accumulates in double layer on their large surface area. It has been claimed [Hoefer] that CDC capacitor capacitance is mainly determined by  electrostatic/double layer capacitance [Brett] and faradaic/pseudocapacitive components[Conway]. In case of pore diameters under 1 nm, another mode of charge storage emerges where ions desolvate to fit into the pores, resulting in much larger capacitance[Huang]. CDC is one of the best known nanoporous materials for ion storage because the size of its pores is consistent and can be finely tuned in wide range by controlling the chlorination temperature of the metal carbide[Gogotsi].

For the second component, ion transfer media, ionic liquids (IL) are currently the material of choice. IL consist only of charged particles with no solvent. Due to their very low vapour pressure, they avoid a common problem with water: evaporation of the electrolyte out of an EAP material when being used in dry environment. IL electrolytes can also improve the cycle lifetime of the material, compared with water based electrolytes [biomedbook].

The third component is a polymer binder, which is usually added for toughness and flexibility.

To complete the actuator, two electrode sheets made of the above mentioned components would be laminated together, with a porous or ion permeable membrane inbetween, often also imregnated with electrolyte. The membrane can also be the active part as in case of ionic polymer metal composite (IPMC) actuators.

Different kinds of ion storage, ion transport, binder and membrane  materials offer countless possibilities to experiment with. For example, IL electrolyte in Nafion membrane has been tested with metal[Bennett], carbon nanotubes[Akle], CDC [Viljar] or RuO2 [Akle, Viljar] electrodes. CDC in PTFE matrix has also been used for the electrodes with IL electrolyte and ion permeable paper membrane[Janno]. Asaka et al [Asaka-2005, ....] have extensively studied carbon bucky gel material actuators where the electrodes contains carbon nanotubes in 1-butyl-3-methylimidazolium tetrafluoroborate (BMI-BF4) ionic liquid, supported by poly(vinylidene fluoride-co-hexafluoropropylene) binder [Asaka-2005]. Carbon nanotube sheets have also been demonstated to work as actuators in water based electrolyte [Baughman-1999].

In EAP actuators one electrode expands and/or other contracts or in the case of IPMC, one side of the membrane contracts  and/or the other expands, causing a bending motion. The mechanism that causes such expansion and contraction is still unknown and debated [Kiyohara]. The proposed mechanisms for expansion include change of the bond lengths due to electrochemical double layer charging [Baughman-1999], insertion of counterions [Baughman-1995], [Kiyohara claims that it is also in Asaka-1995], water introduced by electro-osmosis [Asaka-1995], electrostatic repulsion of the charged molecules of the material [Baughman-1999], decreased interfacial tension on the pore surfaces due to change in double layer charges [Oren] etc.

Correlation has been found between increased accumulation of ions on the electrode surface (capacity) and improved peak strain without specifying the mechanism of actuation[Akle], but that result can not extrapolated to different electrolytes [Janno].

Considering the huge influence the choice of ionic liquid and the type of carbon have on the EAP performance [Janno, Viljar], the primary limiting factor for the strain ratio and maximum strain seems to be the speed of ionic transport, not the quantum mechanical changes in electronic configurations. Increasing the ion mobility could help significantly increase both the strain ratio and maximum strain of EAP-s [biomedbook].

In search of the best ionic conductor, several approaches can be used. In case of a similar problem of increasing the ion mobility in polymer electrolytes for rechargeable batteries, for example changing the polymer topopogy from regular to irregular[ref.req.], adding plastifiers[Dias] or nanoparticulate fillers [Ahmad] have been reported as successful.

In this study, the composition of the electrode material is the object of scrutiny as the ratios of the three electrolyte components are varied and the properties of the electrode materials with different composition are assessed by  Molecular Dynamics (MD) simulations. The usefulness of MD simulation is in the detailed view to the ion movement processes. It has been used to explain the effect of the nanoparticles on polymer electrolytes as causing reduced crystallinity and thereby increasing the amorphous regions where the ionic conductivity is better than in the cristalline regions [Heiki]. Computer simulations also allow to go outside the normal range of compositions, like decreasing the binder content below the minimum required to keep the material solid, and to determine if the volume freed that way inside the material could be put to better use by filling it with some active component (in this case mor carbon or IL), allowing to determine whether or not there would it would be necessary to search for a binder effective in smaller concentrations. Four different electrode compositions are studied, with different IL/Carbon ratios and different amounts of binder polymer in the mixture.

For most electrolytes the ion mobility is directly bound with the diffusion coefficient through the Einstein's relation. However, the ion mobility in IL does not follow the usual pattern. Instead the change of orientation of the ions in electric field can increase the ion mobility by several orders of magnitude compared with the values estimated from diffusion coefficient without electric field [Umecky], despite the fact that any external fields applied to IL are rapidly neutralized by the formation of double layers on the electrode surfaces, its formation time (50 ms for NaCl solution in water [Han]) is still many orders of magnitude longer than the timescale of MD simulation. To better understand the changes the organizaition of the ions has to undergo when the EAP is energized, simulations of each electrode composition were done with and without an external electric field and the resultant ion configurations compared with each other.

# Methodology

The method of Molecular Dynamics is based on periodically calculating the forces acting on each atom of a model, based on a forcefield composed of bond stretch, valence angle flex and dihedral torsion reactions and Van der Waals and electrostatic interactions. The net force acting on each atom, together with its current position and speed are used to find the position and speed at the next timestep. From the continuous history of atom coordinates in time can diffusion coefficients and other macroscopic characteristics be calculated while the movements can also be analysed on the more subtle molecular level. [Rapaport]

The simulatation results were analysed by the following means:

Radial Distribution Function (RDF)[Daniel], Coordination Number (CN)[Daniel], Radial-Angular Distribution[Niu] and Space Distribution functions[Liu] were used  to find the coordination sphere radii and the most probable interaction sites for ions and molecules.

Mean Square Displacement (MSD)[Daniel] was used to calculate the diffusion coefficients and compare the ion mobility and ionic conductivity values with the experimental results available, allowing to select the most effective ion conductor amongst the simulated systems.

The shape (flatness or roundness) of the ion clusters was analysed by replacing each cluster of anions coordinated with the same cation with its inertia ellipsoid and comparing the most probable values for the lengths of the three principal axes of a ellipsoid with each other.

The stability of the ion-ion coordination was reflected by Mean Residence Time (MRT) [Floris] of ions in the coordination spheres of their counterions. MRT is also useful for determining the diffusion mechanisms[Newkome].

## Simulated systems

In experimental setting the PTFE to CDC ratio can be directly controlled before mixing, while the IL content is determined by the saturation of the electrode material when soaked in the electrolyte. CDC to PTFE mass ratio of 0.10 has been used for EAP actuators [Janno] and 0.09 for supercapacitors[Arulepp]. In case of computer simulation, the amount of each component can be controlled directly. To explain the movement of the actuator and determine the ion conduction mechanism, which probably involves some interaction between the carbon and IL electrolyte, the relative amounts of those components were varied. The IL to carbon ratio of the electrodes was varied in proximity of their ratio in similar EAP and supercapacitor materials, the properties of which have previously been experimentally evaluated. The amount of polymer binder was also varied to determine if it has any effect on the ionic mobility.

The components were inserted into the simulation cell in the following form with the ratios of each component given in table 1:

- Carbon in the form of curved graphene flakes with 22 atoms each. (C22)

- Ethyl-methyl-imidazol (EMI+) cations

- Boron tetrafluorate (BF4-) anions

- Polytetrafluoroethylene (PTFE) polymer fragments: CF3-(CF2)20-CF3

The simulation cell was prepared by Monte Carlo methods, considering that there is only short-range ordering in CDC [Palmer] and the other components of the electrode are totally amorphous.

The carbon part of the initial model was created first. CDC can be represented by graphene-like sheets and it has effectively no long-range ordering [Palmer]. To create such a structure, separate pieces of graphene sheets were inserted into the simulation cell in random orientations.

mc

| System nr. | IL/Carbon mass ratio | Carbon | EMI+BF4 | PTFE | Electric field values |
| --- | --- | --- | --- | --- | --- |
|  |  | mass % | flakes | mass % | ion pairs | mass % | chains |  |
| 2 | 1.90 | 32.6% | 52 | 62.0% | 132 | 5.4% | 2 | 0; 50V/mm; 0 (recovery after removal of the electric field) |
| 3 | 1.82 | 32.6% | 52 | 59.3% | 126 | 8.1% | 3 | 0; 50V/mm |
| 4 | 1.73 | 30.7% | 49 | 53.1% | 113 | 16.2% | 6 | 0; 50V/mm |
| 1 | 1.73 | 35.6% | 57 | 61.7% | 132 | 2.7% | 1 | 0; 50V/mm |

Table 1: Simulated systems

## Simulation cell

Before MD simulation can be started, the locations of each atom in the simulation cell during the first moment of the simulation have to be determined. That was done using a in-house Monte Carlo software mcgen[mcgen], which starts with an empty simulation cell and utilises the Monte Carlo method to insert the simulation objects in units as big as an ion, a cabon flake or a monomer of a polyer chain at a time. It  selects a random location and orientation for the unit, evaluates its compatibility with other units already present around that location and decides whether to accept that location and go on to next unit, or to remove the last few units and try another position. After insertion, first the separation between all pairs of atoms are compared with a minimal allowed value. If some atoms are too close, then the configuration is discarded immediately. If adequate spacing between atoms exists, then  the total energy increase ΔE from the insertion is calculated using the MD forcefield. The configuration is always accepted if ΔE<0, but if ΔE>0, then the acceptance or dismissal is decided randomly, with the probability of acceptance being commensurate with the Boltzmann factor  p ~ exp(-ΔE/kT).[mcgen].

The models were created in a cubic cell measuring 40x40x40 Å with periodic boundary conditions. The cell was first filled with nanoporous carbon, then the electrolyte ions were inserted into the pores and spaces between the carbon flakes, and, finally the PTFE polymer was grown into the last empty spaces.

That order was chosen because the carbon flakes were the largest and PTFE monomers were the smallest units used in the generation process, and the probability of finding a large enough space to fit a large unit is continuously decreased as the density of the material in the simulation cell approaches the density of the complete electrode material with impregnated with electrolyte.

The nanoporous carbon consists of graphene-like sheets with effectively no long-range ordering [Palmer]. To create such a structure, separate slightly bent graphene flakes were used. The individual carbon flake shapes were created by a 300 ns long MD simulation of a single carbon flake in vacuo at temperature of 293K, using DL_POLY [dlpoly] software. 10 configurations were taken from that simulation, each with a differently bent shape. In each step of the carbon generation process, one of the 10 configurations was randomly selected,  rotated by a random angle and positioned at a random place in  the cell.

The ionic liquid was inserted one ion at a time, by the same methodology as the carbon. To avoid charge buildup in the box, which would excessively increase the insertion energy of any subsequent ions, the anions and cations were inserted intermittently.

The PTFE molecules were generated last, one monomer at a time, this time only checking for geometric constraints and ignoring the interaction energy.

The model for the electrode material with the least amount of polymer binder was created first. The other systems were created from the first one by removing some of the carbon flakes or IL ions from the cell and growing another chain of polymer into the freed up space.

## Force fields

Several components of the Forde field was found elsewhere. Force field for carbon was published by Henske et al [Hentscke]. Force field for PTFE was described in [Okada]. Cation-anion interaction forcefield is described in [Lopes].

The Van der Waals forces of the separate force fields were decribed as Lennard Jones type and in case there was no previously published force field available the following combination rule was applied: , where ε1, ε2, ε are the potential well depths and σ1, σ2, σ are the Lennard-Jones radii for the first and second atom and for the combined potential, respectivelty.

The force field is described in Tables 2 to 5.

| Substance | Atom/Ion label | Charge /e | Mass /au |  |  | number per molecule |
| --- | --- | --- | --- | --- | --- | --- |
| Carbon | C | 0 | 12.0107[webelements] |  |  | 22 |
| PTFE | C9 | 0.63[okada] | 12.0107[webelements] |  |  | 2 |
|  | C8 | 0.48[okada] | 12.0107[webelements] |  |  | 20 |
|  | F9 | -0.21[okada] | 18.9984[webelements] |  |  | 6 |
|  | F8 | -0.24[okada] | 18.9984[webelements] |  |  | 40 |
| EMI | NA (nitrogen) | 0.15[Lopes] | 14.0067[webelements] |  |  | 2 |
|  | CR (carbon) | -0.11[Lopes] | 12.0107[webelements] |  |  | 1 |
|  | CW | -0.13[Lopes] | 12.0107[webelements] |  |  | 2 |
|  | C1 | -0.17[Lopes] | 12.0107[webelements] |  |  | 2 |
|  | CE | -0.05[Lopes] | 12.0107[webelements] |  |  | 1 |
|  | HA | 0.21[Lopes] | 1.00794[webelements] |  |  | 3 |
|  | H1 | 0.13[Lopes] | 1.00794[webelements] |  |  | 5 |
|  | HC | 0.06[Lopes] | 1.00794[webelements] |  |  | 3 |
| BF4 | B | +1.1504[Lopes] | 10. 811[webelements] |  |  | 1 |
|  | F | -0.5376[Lopes] | 18.9984[webelements] |  |  | 4 |

Table 2: Forcefield parameters of single atoms

| Formula | Atom label 1 | Atom label 2 | k or k12 | k6 | r0 | number per molecule |
| --- | --- | --- | --- | --- | --- | --- |
| 1 |  |  |  |  |  |  |
| 2 |  |  |  |  |  |  |

Table 3: Forcefield bond parameters

Harmonic bond potential:

(1)

12-6 type two-atom potential:

(2)

In the formulas, U is the potential energy of the bond, r is the interatomic distance and r0, k12 and k6 are bond parameters.

| Formula | Atom label 1 | Atom label 2 | Atom label 3 | k |  | number per molecule |
| --- | --- | --- | --- | --- | --- | --- |
| 3 |  |  |  |  |  |  |

Table 4: Forcefield valence angle potential parameters

Harmonic angle potential:

(3)

| Formula | Atom label 1 | Atom label 2 | Atom label 3 | Atom label 4 | A | B | C |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 4 |  |  |  |  |  |  |  |
| 5 |  |  |  |  |  |  |  |
| 6 |  |  |  |  |  |  |  |

Table 5: Forcefield dihedral parameters

„cos“ dihedral potential:

(4)

„cosb“ dihedral potential:

(5)

„cos3“ dihedral potential:

(6)

## Simulations

Each system was first run through a 2 ns long MD simulation using the NVT ensemble in the original 40Å cubic cell to relieve internal stresses left from the generation. To emulate the working conditions at the first moment when voltage is applied to an EAP, an external electic field of 50V/mm was then added and the simulations continued for next 2 ns. [electrical field simulations have not been motivated! ] [We need to discuss that.] Thereafter the simulations, both with and without external electric field, were continued for the next 10 ns using a NPT ensemble and Nose-Hoover barostat with pressure of 1 atm and relaxation time of 0.3 ps. For verification purposes, the initial NVT simulations were also continued until 10 ns long from the beginning. In the NVT simulation of the material with 5.4% polymer content, an unusual layered structure appeared in the electric field. The NVT simulation of this system was carried on for another 10 ns with E=0 to analyse how its structure would respond to the removal of the electric field.

The simulations used Verlet Leapfrog algorithm with 1 fs timestep. Temperature was kept at 293K by a Nose-Hoover thermostat with 0.1 ps relaxation time. Ewald summation with 10-5 precision was used for the electrostatics.

The cubic symmetry of the simulation cell was retained in all simulations.

## Analysis methods

### RDF

### MSD

### Time evolution histogram

The aromatic ring centre locations were calculated for the cations and marked as points X.

The first coordination sphere radius for anions around a cation was found from the RDF of X..B.

The distribution of coordination times was composed by counting the number of

consecutive simulation snapshots (taken after every 1 picosecond) that each anion spent in the

coordination sphere of a unchanged cation. The results were shown with log-log axes and

the coefficients for the equation p(t)=b*t^a were calculated. [I don’t understand this!?] [I will rewrite.]

### Inertia ellipsoid shape

From each snapshot the cation centers' (points X) and the anion central atoms'

(B) coordinates were extracted.  For each group of one cation and all of the

anions coordinated with it, inertia tensors were calculated, assuming the mass

of the cation to be concentrated in point X and the mass of each anion to its

central B atom. The distributions of the inertia tensors greatest, next

greatest and least principal axes were calculated.

The shape of the inertia ellipsoid shows whether the anions prefer to stay in

one plane or are distributed uniformly over a sphere.

# System description

# Analysis

The mobility of both the anions and cations was greatest with the polymer content of 5.4% (fig.). The ion mobility was  greater with the electric field applied (fig.). The mobility of the polymer was also greatest at 5.4% polymer content (fig.), increasing with the added electric field (fig.).

The first coordination sphere radius for cation-anion pairs (X...F) was  6.1Å. The less defined second coordination sphere had 7.5Å radius. Increase of the polymer content and applying the electric field was associated with more of  anion-cation coordination (fig.), (fig.) and lessened ion coordination with graphite (fig.).

The increased mobility could have been facilitated by coordination with the more mobile polymer chain and detachment from the stationary graphite particles.

The radial-angular distribution of cations around anions (Fig. 1, 2) of cations around anions does not show any systematic shift with the increase of polymer content or with the addition of  electric field. Differences between the systems  are small and random.

When comparing the radial-angular distributions of different cation atoms in reference of the anion, it is apparent that every other cation atom has two peaks of maximal probability in the 4-6Å distance region (Fig.2), only the methyl group carbon has a single peak (Fig.1), so the anion-cation coordination sphere radius is primarily determined by the methyl group.

Fig. 1. Two-dimensional radial-angular distribution of the C1 (cation methyl group) ... B (anion) distance and the C1...B-F angle for 8% polymer content and no external electric field. The nearest F atom to the C1 atom was used for the angle.

Fig. 2. Angular-radial distribution of the cation CR carbon in reference of the anion in case of 8% polymer content and no external electric field. The angle between the B-F bond of the anion and the B...CR line is represented on the horizontal axis and the B...CR distance on the vertical axis. The frequency of appearance in the simulation is represented by colors.

The amount of the polymer binder was not found to significantly effect the ionic conductance.

# Results

# References

- [Bar-Cohen-1999] Y. Bar-Cohen, S. P. Leary, M. Shahinpoor, J. S. Harrison, J. G. Smith, Proc. SPIE, 3669, 57 (1999); doi:10.1117/12.349708  http://dx.doi.org/10.1117/12.349708

- [Bar-Cohen-2001] Y. Bar-Cohen, Proc SPIE Int Soc Opt Eng, 4329, 1-6, (2001); http://dx.doi.org/10.1117/12.432639

- [Mart] M. Anton, A. Punning, A. Aabloo, M. Listak, M. Kruusmaa, Towards Autonomous Robotic Systems (TAROS 2004), University of Essex, 1-7, (2004); http://www.essex.ac.uk/csee/research/publications/technicalreports/2004/csm415/Anton_etal.pdf

- [Liu-2008] Y. Liu, L. Shi, L. Liu, Z. Zhang, J. Leng, Proc. SPIE, 6927, 69271A, (2008); http://dx.doi.org/10.1117/12.775946

- [Spigna] N. Di Spigna, P. Chakraborti, P. Yang, T. Ghosh, P. Franzon, Proc. SPIE, 7287, 72871K, (2009); http://dx.doi.org/10.1117/12.816009

- [eapbook] Y. Bar-Cohen (editor), Electroactive Polymer (EAP) Actuators as Artificial Muscles: Reality, Potential, and Challenges, Second Edition (SPIE Press Book), ISBN: 9780819452979

- [Wang] H. Wang, C. Li, ICMTMA'09. International Conference on Measuring Technology and Mechatronics Automation, 1, 73-76, (2009); http://dx.doi.org/10.1109/ICMTMA.2009.114

- [Fernandez] D. Fernández, L. Moreno, J. Baselga, Proc SPIE Int Soc Opt Eng, 5759, 361, (2005);  http://dx.doi.org/10.1117/12.599108

- [Akle] B. J. Akle, M. D. Bennett, D. J. Leo, K. B. Wiles, J. E. Mcgrath, J. Mater. Sci., 42, 7031-41, (2007); http://dx.doi.org/10.1007/s10853-006-0632-4x`

- [Hoefer] M. Hoefer, P. R. Bandaru, Appl. Phys. Lett. 95, 183108 (2009); http://dx.doi.org/10.1063/1.3258353

- [Brett] C. M. A. Brett, A. M. O. Brett, Electrochemistry: Principles, Methods, and Applications (Oxford University, Oxford, 1993).

- [Conway] B. E. Conway, J. Electrochem. Soc. 138, 1539 (1991).

- [Huang] J. Huang, B. G. Sumpter, V. Meunier, Chemistry - A European Journal, 14, 6614 (2008); http://dx.doi.org/10.1002/chem.200800639

- [Gogotsi] Y. Gogotsi, A. Nikitin, H. Ye, W. Zhou, J. E. Fischer, B. Yi, H. C. Foley, M. W. Barsoum, Nature Materials, 2, 591 (2003); http://dx.doi.org/10.1038/nmat957

- [biomedbook] F. Carpi (editor), E. Smela (editor), Biomedical Applications of Electroactive Polymer Actuators, Wiley 2009, ISBN: 978-0-470-77305-5

- [Bennett] M. D. Bennett, D. J. Leo, Sensors and Actuators A, 115, 79 (2004); http://dx.doi.org/10.1016/j.sna.2004.03.043

- [Viljar] V. Palmre, D. Brandell, U. Mäeorg, J. Torop, O. Volobujeva, A. Punning, U. Johanson, M. Kruusmaa, A. Aabloo, Smart Mater. Struct. 18, 095028 (2009); http://dx.doi.org/10.1088/0964-1726/18/9/095028

- [Janno] J. Torop, M. Arulepp, J. Leis, A. Punning, U. Johanson, V. Palmre, A. Aabloo, Materials, 3, 9 (2010); http://dx.doi.org/10.3390/ma3010009

- [Asaka-2005] T. Fukushima, K. Asaka, A. Kosaka, T. Aida, Angew. Chem. Int. Ed. 44, 2410-2413, (2005); http://dx.doi.org/10.1002/anie.200462318

- [Baughman-1999] R. H. Baughman, C. Cui, A. A. Zakhidov, Z. Iqbal, J. N. Barisci, G. M. Spinks, G. G. Wallace, A. Mazzoldi, D. De Rossi, A. G. Rinzler, O. Jaschinski, S. Roth, M. Kertesz, Science, 284, 1340 (1999); http://dx.doi.org/10.1126/science.284.5418.1340

- [Kiyohara] K. Kiyohara, T. Sugino, I. Takeuchi, K. Mukai, K. Asaka, J. Appl. Phys. 105, 063506 (2009)

- [Asaka-1995] K. Asaka, K. Oguro, Y. Nishimura, M. Mizuhata, H. Takenaka, Polym. J., 27, 436 (1995); http://dx.doi.org/10.1295/polymj.27.436

- [Oren] Y. Oren, I. Glatt, A. Livnat, O. Kafari, and A. Soffer, J. Electroanal. Chem. Interfacial Electrochem. 187, 59 (1985); http://dx.doi.org/10.1016/0368-1874(85)85575-1

- [Dias] F. B. Dias, L. Plomp, Journal of Power Sources, 88, 169 (2000); http://dx.doi.org/10.1016/S0378-7753(99)00529-7

- [Ahmad] S. Ahmad, S.A. Agnihotry, Current Applied Physics, 9, 108 (2009); http://dx.doi.org/10.1016/j.cap.2007.12.003

- [Heiki] H. Kasemägi, M. Klintenberg, A. Aabloo, J. O. Thomas, Solid State Ionics, Volume 147, Issues 3-4, April 2002, Pages 367-375, http://dx.doi.org/10.1016/S0167-2738(02)00013-9

- [Umecky] T. Umecky, Y. Saito, H. Matsumoto, J. Phys. Chem. B, 113, 8466 (2009); http://dx.doi.org/10.1021/jp9043946

- [Han] Z. J. Han, R. Morrow, B. K. Tay, D. McKenzie, Appl. Phys. Lett. 94, 043118 (2009); http://dx.doi.org/10.1063/1.3077605

- [Yushin] G. N. Yushin, E. N. Hoffman, A. Nikitin, H. Ye, M. W. Barsoum, Y. Gogotsi, Carbon, 43, 2075 (2005); http://dx.doi.org/10.1016/j.carbon.2005.03.014

- [mcgen] E. Soolo, J. Karo, H. Kasemägi, M. Kruusmaa, A. Aabloo, Proc. SPIE, 6168, 61682A (2006); http://dx.doi.org/10.1117/12.658664

- [dlpoly] W. Smith, T. Forester, The DL_POLY Project, TCS Division, Daresbury Laboratory, Daresbury, Warrington, WA44AD, England

- [Hentscke] R. Hentschke, B. L. Schürmann, J. P. Rabe, J. Chem. Phys. 96, 6213 (1992)

- [Okada] O. Okada, K. Oka, S. Kuwajima, K. Tanabe, Molecular Simulation, 21, 325-342, (1999); http://dx.doi.org/10.1080/08927029908022072

- [Lopes] J. N. C. Lopes, J. Deschamps, A. A. H. Pádua, J. Phys. Chem. B, 108, 2038–2047, (2004); http://dx.doi.org/10.1021/jp0362133

- [webelements] http://webelements.com

- [Palmer] J.C. Palmer, A. Llobet, S.-H. Yeon, J.E. Fischer, Y. Shi, Y. Gogotsi, K.E. Gubbins, Carbon, 48, 1116 (2010); http://dx.doi.org/10.1016/j.carbon.2009.11.033

- [Rapaport] D. C. Rapaport, The Art of Molecular Dynamics Simulation, Second Edition, Cambridge University Press, 2004.

- [Niu] S. Niu, Z. Cao, S. Li, T. Yan, J. Phys. Chem. B, 114, 877 (2010); http://dx.doi.org/10.1021/jp909486z

- [Daniel] D. Brandell, H. Kasemägi, A. Aabloo, Electrochimica Acta, 55, 1333 (2010); http://dx.doi.org/10.1016/j.electacta.2009.04.070

- [Liu-2004] Z. Liu, S. Huang, W. Wang, J. Phys. Chem. B, 108, 12978 (2004); http://dx.doi.org/10.1021/jp048369o

- [Newkome] G. R. Newkome (Editor), Advances in dendritic macromolecules, vol. 5, 2002; ISBN: 0-7623-0839-7

- [Floris] F. M. Floris, J. M. Martínez, J. Tomasi, The Journal of Chemical Physics, 116, 5460 (2002); http://dx.doi.org/10.1063/1.1453957

- [Arulepp] M. Arulepp, J. Leis, M. Lätt, F. Miller, K. Rumma, E. Lust, A.F. Burke, Journal of Power Sources, 162, 1460 (2006); http://dx.doi.org/10.1016/j.jpowsour.2006.08.014

- [Janno-personal] Janno Torop, personal communication

# Comments

So, are they electrodes, electrolytes, or both? What happens during actuation?

Has no one studied this system experimentally?

Heiki's PhD cites [R. Xue, C. A. Angell, Solid State Ionics, 25, 223 (1987)] and [J. Przyłuski, W. Wieczorek, Solid State Ionics, 53-56, 1071 (1992)].

Furthermore: what specific aspect would we like to investigate in this study?

We are most interested in the effect of the carbon content to the ion mobility.

We are looking for the mechanism how the ionic mobility is connected with carbon. There is not much data about different carbon content.

Why?

[Keerutada: otsime parimat ioonjuhti, mis tagaks ioonide parima liikuvuse. Liigutus on ilmselt põhjustatud ioonide liikuvusest.]

Check with Janno: relative to what component were the percentages calculated in his article?

Why simulate four different systems?

Why is there a variation in the proportions between carbon and the IL?

Varieeritakse süsiniku ja ioonvedeliku suhet, et selgitada välja ioonide liikumismehhanismi.

Varieeritakse umbes selles piirkonnas, kus eksperiment toimub [Janno].

The introduction mentions CDC, but here [in Simulation Details] it is grapheme??

CDC carbon is used because it is one of the finest carbon powders available, almost composed of separate graphene sheets.

Is graphene really a good approximation for CDCs? Has somebody else used this?

In nanoporous carbide derived carbon the average thickness of a graphitic crystals is 3 graphene monolayers. [Yushin]

[NB! Add some sentences from the Gogotsi's papers, where he explains why this graphene is the same structure as CDC.]

[what rules?]

If these are published, it is necessary to republish?

The force fields for separate PTFE and separate EMI-BF4 have been published before. I have just put them together as a forcefield for the complete EAP material.

page 167

References not used:

[Kornyshev] A. A. Kornyshev, J. Phys. Chem. B, 111, 5545 (2007); http://dx.doi.org/10.1021/jp067857o

[Baughman-1996] R. H. Baughman, Synthetic Metals, 78, 339 (1996); http://dx.doi.org/10.1016/0379-6779(96)80158-5

[Maginn] E. J. Maginn, J. Phys.: Condens. Matter, 21,  373101 (17pp) (2009); http://dx.doi.org/10.1088/0953-8984/21/37/373101