Appendix 1: The forcefield parameters.

The force field is described in Tables 2 to 8.

| Substance | Atom/Ion label | Charge /e | Mass /au | ε | σ | number per molecule |
| --- | --- | --- | --- | --- | --- | --- |
| Carbon | C | 0 | 12.0107[webelements] | 0.0628 | 3.82 | 22 |
| PTFE | C9 | 0.63[okada] | 12.0107[webelements] | 0.02007 | 2.9836 | 2 |
|  | F9 | -0.21[okada] | 18.9984[webelements] | 0.14779 | 2.5925 | 6 |
|  | C8 | 0.48[okada] | 12.0107[webelements] | 0.15858 | 2.6703 | 20 |
|  | F8 | -0.24[okada] | 18.9984[webelements] | 0.095 | 2.6727 | 40 |
| EMI | N1, N2 | 0.15[Lopes] | 14.0067[webelements] | 0.169886 | 3.25 | 2 |
|  | Ca1 | -0.11[Lopes] | 12.0107[webelements] | 0.069953 | 3.55 | 1 |
|  | Ca2, Ca3 | -0.13[Lopes] | 12.0107[webelements] | 0.069953 | 3.55 | 2 |
|  | Cm, Ce1 | -0.17[Lopes] | 12.0107[webelements] | 0.065955 | 3.5 | 2 |
|  | Ce2 | -0.05[Lopes] | 12.0107[webelements] | 0.065955 | 3.5 | 1 |
|  | Ha1, Ha2, Ha3 | 0.21[Lopes] | 1.00794[webelements] | 0.029980 | 2.42 | 3 |
|  | Hm1, Hm2, Hm3, He1, He2, | 0.13[Lopes] | 1.00794[webelements] | 0.02998 | 2.5 | 5 |
|  | He3, He4, He5 | 0.06[Lopes] | 1.00794[webelements] | 0.02998 | 2.5 | 3 |
| BF4 | B | +1.1504[Lopes] | 10. 811[webelements] | 0.094941 | 3.5814 | 1 |
|  | F | -0.5376[Lopes] | 18.9984[webelements] | 0.060953 | 3.1181 | 4 |

Table 2: Forcefield parameters of single atoms

| Formula | Atom label 1 | Atom label 2 | k / kcal/mol, A / (Å12·kcal/mol) | r0 / Å, B / (Å6·kcal/mol) | number per molecule |
| --- | --- | --- | --- | --- | --- |
| 1 | C | C | 310 | 1.53 | 27 |
| 1 | C9 | C8 | 357 | 1.53 | 2 |
| 1 | C8 | C8 | 344 | 1.53 | 19 |
| 1 | C9 | F9 | 508 | 1.349 | 6 |
| 1 | C8 | F8 | 391 | 1.365 | 40 |
| 2 | F8 | F9 | 1300000 | 0 | 12 (between non-bonded atoms) |
| 2 | F8 | F8 | 1300000 | 0 | 76 (between non-bonded atoms) |
| 1 | Ca1 | NA | 476.736410 | 1.315 | 2 |
| 1 | Ca2, Ca3 | NA | 426.817617 | 1.378 | 2 |
| 1 | Ca2 | Ca3 | 519.728671 | 1.341 | 1 |
| 1 | N1, N2 | Cm, Ce1 | 336.772714 | 1.466 | 2 |
| 1 | Ce1 | Ce2 | 267.746250 | 1.529 | 1 |
| 1 | B | F | 289.815611 | 1.39 | 4 |

Table 3: Forcefield bond parameters (formulas 1, 2)

Harmonic bond potential:

(1)

12-6 type two-atom potential:

(2)

In the formulas, U is the potential energy of the bond, r is the interatomic distance and r0, k12 and k6 are bond parameters.

| Atom label 1 | Atom label 2 | r0 / Å | number per molecule |
| --- | --- | --- | --- |
| Ca1, Ca2, Ca3 | Ha1, Ha2, Ha3 | 1.08 | 3 |
| Cm, Ce1, Ce2 | Hm1...Hm3,He1...He5 | 1.53 | 8 |

Table 4: Constraints

| Atom label 1 | Atom label 2 | Atom label 3 | k / kcal/mol | φ0 / deg | number per molecule |
| --- | --- | --- | --- | --- | --- |
| C | C | C | 40 | 109.5 | 42 |
| F9 | C9 | F9 | 104.4 | 108.79 | 6 |
| F9 | C9 | C8 | 80.2 | 110.14 | 6 |
| C9 | C8 | F8 | 84.7 | 107.2 | 4 |
| C9 | C8 | C8 | 97.9 | 116.51 | 2 |
| C8 | C8 | C8 | 97.9 | 116.51 | 18 |
| F8 | C8 | F8 | 106.3 | 108.84 | 20 |
| F8 | C8 | C8 | 79.5 | 108.45 | 76 |
| Ca3, Ca2 | N1, N2 | Ca1 | 69.886309 | 108.0 | 2 |
| Ca3, Ca2 | N1, N2 | Ce1, Cm | 69.886309 | 125.6 | 2 |
| Ca1 | N1, N2 | Ce1, Cm | 69.886309 | 126.4 | 2 |
| N1, N2 | Ca1 | Ha1 | 34.943155 | 125.1 | 2 |
| N1 | Ca1 | N2 | 69.886309 | 109.8 | 1 |
| N1, N2 | Ca3, Ca2 | Ca2, Ca3 | 69.886309 | 107.1 | 2 |
| N1, N2 | Ca3, Ca2 | Ha3, Ha2 | 34.943155 | 122.0 | 2 |
| Ca2, Ca3 | Ca3, Ca2 | Ha3, Ha2 | 34.943155 | 130.9 | 2 |
| N1 | Ce1 | He1, He2 | 74.806535 | 110.7 | 2 |
| N2 | Cm | Hm1, Hm2, Hm3 | 74.806535 | 110.7 | 3 |
| Ce1 | Ce2 | He3, He4, He5 | 74.806535 | 110.7 | 3 |
| Ce2 | Ce1 | He1, He2 | 74.806535 | 110.7 | 2 |
| N1 | Ce1 | Ce2 | 99.933123 | 112.70 | 1 |
| He1 | Ce1 | He2 | 65.945352 | 107.8 | 1 |
| He3, He4, He5 | Ce2 | He4, He5, He3, | 65.945352 | 107.8 | 3 |
| Hm1, Hm2, Hm3 | Cm | Hm2, Hm3, Hm1 | 65.945352 | 107.8 | 3 |
| F | B | F | 49.966562 | 109.5 | 6 |

Table 5: Forcefield valence angle potential parameters (formula 3)

Harmonic angle potential:

(3)

| Atom label 1 | Atom label 2 | Atom label 3 | Atom label 4 | A /(kcal/mol) | δ /deg | m | Number per molecule |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | C | C | C | 1.3 | 0 | 3 | 64 |

Table 6: Forcefield dihedral parameters for carbon (formula 4)

„cos“ dihedral potential:	U(φ)=A[1+cos(mφ -δ)]	(4)

| Atom label 1 | Atom label 2 | Atom label 3 | Atom label 4 | A0 /(kcal/mol) | B1 /(kcal/mol) | B2 /(kcal/mol) | B3 /(kcal/mol) | B4 /(kcal/mol) | B5 /(kcal/mol) | B6 /(kcal/mol) | Number per molecule |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| F9 | C9 | C8 | C8 | 0 | 0 | 0 | 0.5908 | 0 | 0 | 0 | 6 |
| C9 | C8 | C8 | C8 | 0 | 17.7 | 3.253 | 1.748 | 0.523 | -0.02 | -0.462 | 2 |
| C8 | C8 | C8 | C8 | 0 | 17.7 | 3.253 | 1.748 | 0.523 | -0.02 | -0.462 | 17 |

Table 7: Forcefield dihedral parameters for PTFE (formula 5)

„cosb“ dihedral potential:	U(φ)=A0/2 + Σi [Bi cos(iφ)]	(5)

| Atom label 1 | Atom label 2 | Atom label 3 | Atom label 4 | A1 /(kcal/mol) | A2 /(kcal/mol) | A3 /(kcal/mol) | Number per molecule |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ca3, Ce1 | N1 | Ca1 | N2, Ha1 | 0 | 4.647941 | 0 | 4 |
| Ca2, Cm | N2 | Ca1 | N1, Ha1 | 0 | 4.647941 | 0 | 4 |
| N2,Ha2 | Ca2 | Ca3 | N1, Ha3 | 0 | 10.743288 | 0 | 4 |
| Ca1, Ce1 | N1 | Ca3 | Ca2, Ha3 | 0 | 2.997516 | 0 | 4 |
| Ca1, Cm | N2 | Ca2 | Ca3, Ha2 | 0 | 2.997516 | 0 | 4 |
| Ca3 | N1 | Ce1 | He1, He2 | 0 | 0.131365 | 0 | 2 |
| Ca2 | N2 | Cm | Hm1, Hm2, Hm3 | 0 | 0.131365 | 0 | 3 |
| Ca1 | N1 | Ce1 | He1, He2 | 0 | 0 | 0 | 2 |
| Ca1 | N2 | Cm | Hm1, Hm2, Hm3 | 0 | 0 | 0 | 3 |
| Ca3 | N1 | Ce1 | Ce2 | -1.375752 | 1.058087 | 0.209468 | 1 |
| Ca1 | N1 | Ce1 | Ce2 | -0.771472 | 0 | 0 | 1 |
| N1 | Ce1 | Ce2 | He3, He4, He5 | 0 | 0 | 0 | 3 |
| He1, He2 | Ce1 | Ce2 | He3, He4, He5 | 0 | 0 | 0.317904 | 6 |
| Ce1 | N1 | Ha1, Ca3 | Ca3, Ha1 | 0 | 1.999140 | 0 | 2 |
| Cm | N2 | Ca1, Ca2 | Ca2, Ca1 | 0 | 1.999140 | 0 | 2 |
| Ha1 | Ca1 | N1, N2 | N2, N1 | 0 | 2.197382 | 0 | 2 |
| Ha2 | Ca2 | N2, Ca3 | Ca3, N2 | 0 | 2.197382 | 0 | 2 |
| Ha3 | Ca3 | N1, Ca2 | Ca2, N1 | 0 | 2.197382 | 0 | 2 |

Table 8: Forcefield dihedral parameters for EMI (formula 6)

„cos3“ dihedral potential:	U(φ)=(1/2)A1(1+cos(φ)) + (1/2)A2(1-cos(2φ)) + (1/2)A3(1+cos(3φ))	(6)