Electrode Reactions in Cu-Pt Coated Ionic Polymer Actuators

Urmas Johanson*, Uno Mäeorg**, Väino Sammelselg ***, Daniel Brandell*, Andres Punning*, Maarja Kruusmaa* and Alvo Aabloo*

*Institute of Technology, Tartu University, Nooruse 1, 50411 Tartu, Estonia

**Institute of Organic Chemistry, Tartu University, Jakobi 2, 51014 Tartu, Estonia

***Institute of Physical  Chemistry, Tartu University, Jakobi 2, 51014 Tartu, Estonia.

Abstract

Composite actuators consisting of sheets of the solid polymer electrolyte (similar to Nafion®) with Cu2+ counter-ions inserted and coated with platinum and copper metal layers (so-called Ionomeric Polymer-Metal Composites; IPMCs) have been synthesised and their electromechanical performance upon actuation has been monitored. Resistivity measurements on the electrodes show that the electrical conductivity of the membranes metal surface increases on the cathode side during the actuation process, contradictory to the situation when Cu is absent from the metal coating. This phenomenon is explained by the subsequent reduction of Cu2+ ions on the cathode upon actuation; Cu layer growth in this side prevents it from cracking and decreases its electrode resistance. The phenomenon opens up for longer life-times for Cu-based IPMCs. However, additional problems with Cu layer oxidation and Cu dendrite growth on the electrodes should be considered.

Keywords: Ionomeric Polymer-Metal Composite; Nafion; Copper-Platinum Electrode; Resistivity; Copper growth

*For correspondence: urmas.johanson@ut.ee

# Introduction

Electroactive polymers (EAPs) are polymer materials that change their shape or size in response to electrical stimuli. The feature makes this class of materials to a good candidate for using in the field of biomimetic devices, since it mimics the behaviour of biological muscles. EAPs inhibit similar properties to biological materials in terms of force, strain and speed. They are attractive for creating artificial muscles used in biologically inspired robots [1], biomedical devices and security applications [2].

Ion-conducting polymers have been used widely as EAP materials. They have the advantage of operating at low electric voltages. Among the most commonly used ionic EAP systems are the ionomeric polymer-metal composites (IPMCs), consisting of a 200 to 400 μm thick ionomer membrane (most commonly Nafion® [3]) plated with metal (typically with Pt or Au) and with metal ions coordinating to the ionic groups in the polymer. The material exhibits a bending motion when a potential of 1-5 V is applied over the metal surfaces [4], schematically shown in Figure 1. The applied electrical field causes the mobile cations in the swollen polymer film to move towards the cathode, which leads to an expansion at this side of the membrane and therefore causes the membrane to bend towards the anode in an actuating motion [5].

One of the problems facing these materials, and their future use as actuator, is that the bending motion gives rise to cracks in the surface metal layers that constitutes the electrodes. The cracks lead to leakage of solvent from the ionomer, and thus to lower ion conductivity and a lower degree of bending. The phenomenon also gives rise to a higher electronic resistance in the surface electrode layers, and thus to slower response time and a smaller actuating motion. Therefore, an increase of active lifecycles could be achieved by improving the mechanical and electrical properties of the surface electrode layers [6].

In our study presented here, we report on our efforts to overcome the problem with the metal cracking by using Cu as a composite material together with Pt as electrode, and Cu2+ as counter ion to the Nafion® sulphonate groups. Similar type of IPMC materials are reported first by Uchida and Taya [7-9]. They showed that when a voltage is applied over the membrane, the following electrochemical reactions occur in the material:

Anode reaction: Cu(s) + 5H2O → Cu2+ x 5H2O + 2e-

Cathode reaction: Cu2+ x 5H2O + 2e- → Cu(s) + 5H2O

They also observed that when a series of electrical impulses with the same voltage polarity were applied for a long time, copper on the surface of the anode vanished. At the same time a new copper layer was formed on the cathode side. In the meantime, Cu2+ ions in the polymer transported water molecules from the anode to the cathode side. The process is reversible, so that when the polarity of applied impulses to the electrodes change, the water and Cu-ions transport goes in the opposite direction through the membrane.

Since the expansion of the cracks in the Pt-layer occur on the same side of the membrane as the Cu layer growth (i.e. the cathode side), this growth may compensate for some of the cracking, leading to increased electrical conductivity and higher mechanical and chemical stability in the cathode surface layer. We have monitored this by measuring the resistivity in the two surface layers using the non-symmetrical actuation process.

# 2 Experimental

## 2.1 IPMC synthesis

Ready-made Pt-coated Na-ions containing MuscleSheet™ IPMCs were purchased from BioMimetics Inc. These IPMCs are 0.2-0.4 mm thick and contain ionic polymer which is similar to Nafion® 1110 but not fully fluorinated. Three 3 cm long strips were cut out, and their actuator response was tested prior to further synthesis. A SEM image of cross section of such IPMC sample is shown in Figure 1. All reactive used were analytical grade and were used without further purification. Subsequently strips were boiled for 20 minutes in 1 M HCl (aq) to substitute all Na+ -ions with H+ -ions. Thereafter, the sheets were put in 2 M CuSO4 (aq) for 12 hours; afterwards the presence of Cu2+-Nafion® was verified by optical microscopy: the cross-section of the membranes had a clear blue colour. The blue colour also indicates that each Cu2+ ion is complexed by 5 molecules of water. Finally, the IPMC sheets were coated with Cu layer by electrochemical plating from CuSO4 solution.  Copper layer on the electrode was prepared by electrochemical plating. The quantity of copper deposited during electrochemical plating was controlled by charge passed thru the system during the copper layer preparation. Calculated from passed current an average thickness of copper layer is 2 microns. After electrochemical plating, the formed copper layer is not very equal. It is well known that during electrochemical plating the electrical field is stronger at the rim and so is there the metal layer formation faster. A X-ray line-scan [   kuidas tehtud]of the IPMC cross section (Figure 2) shows how copper and copper ions and platinum are distributed over the IPMC cross section (thickness).

2.2 Surface resistivity measurements

The experimental setup used for the resistivity measurements and its benefits in the context of IPMCs have been described in detail elsewhere [10]. A schematic picture of the experimental setup is shown in Figure 3 and 4. We clamped the IPMC strips in vertical cantilever positions in a container filled with de-ionized water. Four pairs contacts (gold) were attached to each sample (see Figure 5). These contacts were made as lightweight as possible, but strong enough to ensure good contact. The measurements were conducted using National Instruments LabView7 control software. The driving voltage was generated by a NI PCI-6703 DAQ board and amplified with a NS LM675 power op-amp. Voltages on all contacts with respect to the ground were measured with National Instruments PCI-6034 DAQ board.

The measurements of the surface resistance were conducted using a four-probe system. This method has been shown to eliminate inexactnesses caused by the inconsistent current density and resistance from the contacts [11,12]. The actual values of the reference voltage U0 and the resistor R in Figure 4 were selected according to the range of the DAQ performing the measurements, but were all far below the voltage limit for electrolysis. The actual electric current during the measurement of membrane surface metal layer (electrode) resistance was in the range of 1-6 mA.

In order to ensure galvanic insulation of the contacts on the opposite sides of the sample during the measurements, a 8-channel 3-position switch was used. In position A in Figure 4, the driving voltage from the switch is fed to contacts 1-2 on the sample. In position B, the surface resistance on one side of the sample is measured between contacts 3-5, using the contacts 1-3-5-7. In position C, the surface resistance on the other side of the sample is measured between the contacts 4-6.

The measurements were conducted in the following order:

1. The switch was in position A, and the samples were fed with asymmetrical driving pulses: 2 seconds with one polarity, followed 1 second with the opposite polarity. The samples were treated for 100 cycles before the surface resistance was measured.

2. By swiftly switch to positions B and C, the surface resistances of both sides of the samples were measured.

The experiment was repeated by applying reversely asymmetrical driving pulses. Driving pulses for one cycle are shown in Figure 6.

# 3 Results and discussion

3.1 Pt-coated actuators

The data presented in Figure 7 shows how the surface resistivity changes for the first two of strips upon mechanical bending, prior to coating with Cu. The strips are somewhat bended in their relaxed states, which make the resistivity differ at the two sides at 0 degree bending. This is an artefact of that the Pt metal layer is uneven at the two different sides of the membrane.

It is clear here that the strips behave as expected: when bended to left, the metal surface layer on the right side of the electrode cracks, which results in a severe increase in resistivity. At the same time, the resistivity on the left side of the material decreases, due to that the metal particles are being pressed together. This process is reversible, so that when the material is bent in the other direction, to the right, the resistivity drops on the right side, while it increases on the left. Similar results have already been shown for the same kind of IPMCs [10].

3.2 Cu-Pt coated IPMCs

Table 1 summons the resistivity measurements of the three samples after they have been coated with an additional copper layer. Just as for the untreated membranes, there is a large difference in electrode resistivity between the left and right side of the membranes, and between the individual membranes, probably due to cracks and other imperfections in the coating metal layers. All samples were then first bended to the right direction for 100 cycles, where the motion during one cycle was actuated by a 2V pulse of 2 seconds, followed by a back relaxation from a -2V pulse during 1 second. It could be observed that the bending angle decreases continuously over the cycles, with the initial bending being at around 45º.

Due the ionic conductivity of the membrane, it is impossible to measure the electrode resistivity directly at the same time as when the voltage is applied to the sheet and therefore the corresponding measurements were done quickly after switching off the voltage. However, after switching off the outside voltage a very fast relaxation process of the sheet occurs. It relaxes back from, it is bent state due to water leakage through the electrode cracks and water diffusion towards the anode. This relaxation goes faster for the Cu/Cu2+-based IPMCs than for the conventional forms, based on Li+- or Na+-Nafion®. The reason for this is that the water molecules transported to the electrode surface are uncomplexed to any cation after the reduction of Cu2+ to Cu, and therefore are freely mobile. All measurements of the electrode resistivity were thus done in non-bent state. After these measurements, the polarity of the driving pulses was switched, and the samples were bent another 100 cycles to the left direction. Finally, they were bent yet another 100 cycles to the right direction.

It is clear from the data presented in Table 1 that the Cu-coated membranes display an opposite phenomenon compared with those only coated by Pt. The resistivity increases at the side to which the material is bended (the anode side) and it decreases at the other (cathode) side.  Therefore we assume (in accordance with the discussion in the Introduction) that a new layer of Cu is formed between Pt-particles in the electrode layer and also in the Nafion® matrix close to the Pt-electrode on the cathode side. At the same time, Cu is depleted from the anode side during the creation of Cu2+ ions. Both these electrode reactions occur while the Cu2+ ions migrate toward the cathode in the polymer matrix, and thus the process assists to pump water in that direction, causing the actuating motion. This continuous production of Cu2+ also represents an elimination of another limitation to the use of IPMCs, since back-diffusion of cations towards the anode will be much less of a problem. Yet another positive factor to take into account is that the number of possible mobile cations increases with several orders of magnitude compared to IPMCs without electrochemical electrode reaction. In IPMCs the number of mobile ions is usually limited by cations initially paired to the polymer –SO3- groups, while here new Cu2+ ions are created at the anode during the actuation process. Therefore the water quantity which can be transported in this system should be significantly higher. This, however, increases the importance of solvent leakage protection at the electrodes.

Although the variations in resistivity is large, and fluctuates severely upon switching the polarity for 100 cycles, it is also clear from the data presented in Table 1 that the final resistivity values of the electrodes are lower than the initial values prior to cycling. The only exception to this rule is the right side electrode of sample 3, which however displayed highly fluctuating values in resistivity, possibly due to an imperfect Pt coating. In fact, the data in Table 1 suggests that the electrode resistivity is continuously improving upon cycling. These results indicate that the Cu layers in the samples are displaced over the cycling process, getting more evenly distributed over the surface and in better contact with the Pt particles. From X-ray line-scan of such worked system it can be seen that Cu layer which was after preparing located in outer surface of platinum electrodes [Figure 2] is transported during experiment mainly to the inner surface of platinum electrodes [Figure 8].

The results in Table 1 are promising in the context of developing IPMCs, since they show that the problems of cracking here have been overcome, which opens up for longer lifetimes. At the same time such a change of electrode resistivity makes impossible to use such actuator as a self-sensing actuator because electrode resistivity depends now also about previous measurements and not only on the bending angle of actuator as it is in case of such type of actuator  without electrode reactions [13]. The problem with this type of IPMCs rather seems to be the Cu depletion on the anode side, which possibly is the reason for the decreasing bending angle upon cycling. This problem should however be possible to solve by improving methods of preparation of copper on the electrodes, or any other electronically conductive additive to the membrane surfaces. The artificial muscle fibres also actuate at a low voltage, which avoids the problems of electrolysis – common for other IPMCs – and generates bending as far as 90º already at 2V.

3.3 Unwanted side-reactions

Although the resistivity data for the Cu-coated IPMCs look promising, we observed  unwanted side-reactions during our measurements. These side-reactions in turn cause new problems for the IPMCs. First, if the sheet actuation was driven at to high voltage for a such type of material – 4.5 V – the system clearly short-circuit after 300 cycles. This indicates growth of Cu dendrites, which is known to occur in many other systems for example lithium batteries [14], and was confirmed by optical microscopy and SEM. From scanning electron microscope line-scan from such a copper plated actuator cross-section [Figure 9] shows that there is a quite a big amount of unevenly distributed copper inside of such IPMC-actuator. It is even more important that such actuator contains a lot of holes in polymer matrix as it can be seen of SEM image [Figure 10]. The only mechanism that may explain this type polymer structure changes is related to micro explosions of detonating gas (2:1 mixture of hydrogen and oxygen). Such in many case rounded holes inside solid polymer matrix can be made by using heat of the detonating gas explosions for melting the polymer matrix. Another important thing is the location of this type holes inside of the polymer matrix - in some cases corresponding holes are located only very close to the electrodes. This means that there are no very long dendrites inside of the polymer matrix because gas formation can occur only on the electrodes. Another SEM picture shows that in some other point of such actuator (much more close to the contacts) such type of holes are located also quite far from electrodes inside of the polymer matrix. X-ray map-pictures for copper shows also that amount of copper inside the polymer matrix is in this case much bigger and these higher concentrations can be found much deeper inside of the polymer matrix.

On the copper dendrites (which are connected with electrodes) is produced gaseous hydrogen and oxygen during the water electrolysis. After switching polarity detonating gas is produced:

(cathode): 2 H+ + 2 e- → H2 (gas)

(anode): 2 OH- - 2 e - → 1/2 O2 (gas) + H2O

After that occurs detonating gas explosion. For this reaction it is needed at the room temperature a catalyst (platinum). Such actuator which has platinum electrodes and which is prepared by using impregnation-reduction method contains always a very small amount of platinum inside of the polymer matrix (can be seen also on the X-ray line-scan (Figure 2)).

Obviously, dendrite growth terminates the actuation motion of the IPMC.

Another observation is the appearance of non-conductive insoluble Cu+ compounds on the electrodes. Cu+ ions are created through the spontaneous redox reaction between Cu atoms in the metal electrode layer and Cu2+ ions in the membrane:

Cu(s) + Cu2+ → 2 Cu+

Cu+ compounds are quite stable in these conditions (often insoluble in water), which means that the salt formation depletes the Cu(s) layers, and thus raises the resistivity again on the electrode surfaces; the salts are also electronically isolating. The formation of Cu+ salts severely decreases the lifetime of the IPMCs, and it was therefore necessary to conduct our resistivity measurements directly after the Cu-coating. If the samples were left overnight, the Cu-layer had transformed almost completely into Cu+ -salts.

The Cu+ formation was determined by visual observation. Typically copper coloured electrodes turned grey (the colour of platinum electrodes); Cu+ compounds are generally colourless and transparent in the wet state. After drying such samples it was possible to observe a layer of white insoluble compound – probably Cu2SO4 – on the surface of the electrodes. In addition, initially blue coloured ionic polymer layers turned colourless after long time (several days) due to the reduction of blue coloured Cu2+  to colourless Cu+ compounds.

# 4 Conclusions

We have here presented the quantitative study of the variations in electrode resistivity for Cu-coated Nafion®-based IPMCs upon actuation cycling. We showed that the depletion of Cu (s) at the anode side, and the formation of a new Cu (s) layer at the cathode side, give raise to an opposite resistivity profile than for ordinary Pt-coated IPMCs. This, in turn, represents an excellent possibility to overcome the problem of resistivity increase due to the electrode cracking on the cathode side upon actuation. Copper layer movement during actuation cycling is confirmed by Cu-IPMC actuator cross section X-ray analalysis. However, formation of Cu dendrites and insoluble Cu+ compounds cause severe limitations for these IPMCs, and these problems must be treated further. It is also necessary to overcome the water leakage through the electrode cracks.

# Acknowledgements

The financial support of the Estonian Science Foundation under Project No. 6765 is acknowledged. Daniel Brandell wishes to thank the European Science Foundation programme STIPOMAT for financial support.

References

[1] Y. Bar-Cohen, Biomimetics – Biologically inspired Technologies, CRC, 2005.

[2] M. Shahinpoor, K.J. Kim, Ionic polymer–metal composites: IV. Industrial and medical applications, Smart Mater. Struct. J., 14 (2005) 197

[3] K.A. Mauritz and R.B. Moore, State of Understanding of Nafion, Chem. Rev., 104 (2004) 4535.

[4] Y. Bar-Cohen, Electroactive Polymer (EAP) Actuators as Artificial Muscles - Reality, Potential and Challenges, SPIE Press, 2001.

[5] S. Nemat-Nasser, Micro-mechanics of Ionic Polymer-metal Composites J. Appl. Phys., 92 (2002) 2899.

[6] M. Shahinpoor, K.J. Kim, The effect of surface-electrode resistance on the performance of ionic polymer-metal composite (IPMC) artificial muscles, Smart Mater. Struct. J., 9 No 4 (2000) 543.

[7] M. Uchida and M. Taya, Solid polymer electrolyte actuator using electrode reaction, Polymer, 42 (2001) 9281.

[8] M. Uchida, X. Chunye, M. Le Guilly and M. Taya, Design of Nafion Actuator with Enhanced Displacement, Proceedings of the SPIE - The International Society for Optical Engineering, vol. 4695 (2002) 57.

[9] M. Le Guilly, M. Uchida and M. Taya, Nafion-based smart membrane as an Actuator Array, Proceedings of the SPIE - The International Society for Optical Engineering, vol. 4695 (2002) 78.

[10] A. Punning, M. Kruusmaa and A. Aabloo, Surface resistance experiments with IPMC sensors and actuators,  Sensors and Actuators A, 133 (2007) 200.

[11] S. Nemat-Nasser, C.W. Thomas, “Ionomeric polymer–metal composites”, in: Y. Bar-Cohen (Ed.), Electroactive Polymer (EAP) Actuators as Artifical Muscles. Reality, Potential, and Challenges, SPIE Press, Washington, 2001.

[12] Four Point Probe Theory, Retrieved 26 October 2005, http://www.fourpoint-probes.com/fpp.html.

[13] A. Punning, M. Kruusmaa, A. Aabloo, A self-sensing ion conducting polymer metal composite (IPMC) actuator, Sensors and Actuators A, 136 (2007), 656

[14] F. Orsini, A. du Pasquier, B. Beaudouin, J.M. Tarascon, M. Trentin, N. Langenhuizen, E. de Beer, P. Notten, In situ SEM study of the interfaces in plastic lithium cells, J. Power Sources, 81-82 (1999) 918.

Table 1. Electrode resistivity at the left and right electrode for Cu-coated Musclesheet® IPMCs after bending with 2 V for 2 seconds and relaxing with -2 V for 1 second.

| Total No. of bending cycles | Bending direction | Left electrode resistivity (Ω/cm) | Right electrode resistivity (Ω/cm) |
| --- | --- | --- | --- |
| Sample 1 |
| 0 |  | 9.5 | 57 |
| 100 | right | 2.4 | > 400 |
| 200 | left | 5.7 | 0.95 |
| 300 | right | 0.62 | 1.7 |
| Sample 2 |
| 0 |  | 4.1 | 26 |
| 100 | right | 1.5 | > 400 |
| 200 | Left | 2.1 | 3.2 |
| 300 | right | 0.58 | 21 |
| Sample 3 |
| 0 |  | 2.0 | 13 |
| 100 | right | 1.2 | 200 |
| 200 | Left | 2.0 | 0.65 |
| 300 | right | 0.60 | 100 |