Reviewer 1:

Question 1.

Astonishing (and somehow upsetting) is the fact that the authors do not cite their previous reference published recently in S&A,A. In there they present a novel self-sensing IMPC actuator and this is also the case in this manuscript. Although there are differences in the construction and in results, I do not comprehend why the authors omitted this referencing.

Answer 1.

Self-sensing properties of IPMC actuators are based on unchanged resistivity values of electrodes for every bended state of IPMC-actuator. The situation is completely different in case of IPMC-actuators with electrochemical electrode reactions. Copper layer formation in one electrode and disappearance in another electrode changes also electrode resistivity values and so the bending state is not anymore so exactly detectable from resistivity data.

IPMC actuator with such electrode reactions as it is in case of copper ions containing ionic polymer with electrodes containing copper very sensitive to the measurement history. It is possible to lose copper layer in one electrode and to get at the same time about two times thicker copper layer on another electrode and it is quite easy to predict that in such system the electrode resitivity values are completely different and self-sensing properties does not work anymore.

We did add corresponding information to the paper.

Question 2.

How the thickness of the electrodes was controlled

Answer 2.

Platinum electrode was made by BioMimetics Inc. during MuscleSheetTM preparation. From the cross-section pictures measured by using scanning electron microscope we did get the information that the platinum layers on the both sides of the artificial muscle have typically platinum electrodes with different thickness. Electrode resisistivity measurements data also confirms that electrodes on both sides of such IPMC actuator are typically not equal. Typically platinum electrode thickness measured from SEM images has a value between 3 and 8 microns.

Copper layer thickness: Copper layer on the electrode was prepared by electrochemical plating. The quantity of copper deposited during electrochemical plating was controlled by charge passed thru the system during the copper layer preparation. Calculated from passed current  average thickness of copper layer is 2 microns. We did add this part also to the paper.

Question 3.

Explanations of the formation of Cu dendrites.

Answer 3.

Copper dendrite growth is possible to show by scanning electron microscope pictures from such a copper plated actuator which was specally cycled for 300 times with following steps in one cycle: a) 0,5 seconds +4,5V and b) 0,5 seconds -4,5V.

In this case the cross-section picture shows that there is a quite a big amount of unevenly distributed copper inside of such IPMC-actuator. And what is even more important - such actuator contains a lot of holes in polymer matrix. The only mechanism which explains this type polymer structure changes is related with micro explosions of detonating gas (2:1 mixture of gaseous hydrogen and oxygen). Such in many case rounded holes inside solid polymer matrix can be made by using heat of the detonating gas explosions for melting the polymer matrix. Another important thing is the location of this type holes inside of the polymer matrix - in some cases corresponding holes are located only very close to the electrodes. This means that there are no very long dendrites inside of the polymer matrix because gas formation can occur only on the electrodes. Another SEM picture shows that in some other point of such actuator (much more close to the contacts) such type of holes are located also quite far from electrodes inside of the polymer matrix. X-ray map-pictures for copper shows also that amount of copper inside the polymer matrix is in this case much bigger and these higher concentrations can be found much deeper inside of the polymer matrix.

On the copper dendrites (which are connected with electrodes) is produced gaseous hydrogen and oxygen during the water electrolysis. After switching polarity detonating gas is produced:

(cathode): 2 H(+) - 2 e(-) -> H(2) (gas)

(anode): 2 OH(-) + 2 e (-) -> 1/2 O(2) (gas)

After that occurs detonating gas explosion. For this reaction it is needed at the room temperature a catalyst (platinum). And such actuator which has platinum electrodes and which is prepared by using impregnation-reduction method contains always a very small amount of platinum inside of the polymer matrix (can be seen also on the X-ray line-scan (Figure **)).

We did add this information also to the paper.

We have still an opinion that this paper contains a quite big amount of information which is directly related with chemistry (especially with electrochemistry) and we still have opinion that probably for this paper is the best place in S&A,B (Chemical).

Reviewer 2

Question 1.     Uchida and Taya stated that Cu layer was made after Pt plating for their samples. Is this work employed the same method?:

1) Yes, we did prepare corresponding copper layer exactly in the same way. MuscleSheet (TM) is covered with platinum electrodes and we did cover this material with additional copper layer.

Question 2.     What is the weight ratio of Pt/Cu metal in electrode?

Answer 2. It is a bit complicated to say which the exact weight ratio is (because we did not prepare platinum electrodes on both sides of actuator) but this is probably in range of 10:1 to 5:1.

Copper layer thickness: Copper layer on the electrode was prepared by electrochemical plating. The quantity of copper deposited during electrochemical plating was controlled by charge passed thru the system during the copper layer preparation. Calculated from passed current an average thickness of copper layer is 2 microns. After electrochemical plating with copper layer it can be see that formed layer is not very equal. It is well known that during electrochemical plating is the electrical field stronger at the rim and so is there the metal layer formation faster.

We did add this information also to the paper.

Question 3.     The thickness of electrode has very important effect on actuation behavior of IPMC. If there is a significant asymmetry between two electrodes the performance of this actuator may be seriously impaired. Could authors show cross-sectional view of IPMC?

Answer 3. SEM-i pilt.

Question 4.     The bending deformation of this system also depends on the migration of Cu++ in Nafion. It is recommended to determine the contribution from the generation of Cu++ at the anode in bending..

Answer 4. According to our opinion the bending deformation of this system is depending mainly (if not only) on the migration (electro-osmosis) of hydrated Cu2+ ions driven by electrical field in the polymer matrix. Because there should be no other cations than Cu2+ in this polymer, than all the deformation is related with movement of this cation. In water solution Cu(2+) cation is in hydrated form (with 5 molecules of water, with very typical blue colour). If the potential is too low for water electrolysis, then all current going thru the ionic polymer is connected with: 1) oxidation of metallic copper on the anode tu the Cu(2+) cation, 2) migration of the Cu(2+) cation in hydrated form (with 5 molecules of water) to the catode; 3) reduction of  Cu(2+) cation to the neutral Cu atoms on the surface of catode. Such behaviour is very different from the IPMC actuators, where moveable charged ions (cations in case of Nafion) are accumulating close to the one electrode (close to the catode in case of Nafion). This process is similar to the charging process of (electrolytic) capacitor and it means that charge distribution is changed after connecting with outside voltage source. In case of IPMC-actuator with copper layers on electrodes and Cu(2+) cations inside of the ionic polymer there is a quite stable ion distribution over the all ionic polymer all the time also during the actuator bending.

Question 5.     Authors are asked to provide scientific data to support their argument in this work. " a) formation of Cu dendrite  b) formation and quantitative analysis  of Cu+ ions .

Answer 5. a) Copper dendrite growth is possible to show by scanning electron microscope pictures from such a copper plated actuator which was specally cycled for 300 times with following steps in one cycle: a) 0,5 seconds +4,5V and b) 0,5 seconds -4,5V.

In this case the cross-section picture shows that there is a quite a big amount of unevenly distributed copper inside of such IPMC-actuator. And what is even more important - such actuator contains a lot of holes in polymer matrix. The only mechanism which explains this type polymer structure changes is related with micro explosions of detonating gas (2:1 mixture of gaseous hydrogen and oxygen). Such in many case rounded holes inside solid polymer matrix can be made by using heat of the detonating gas explosions for melting the polymer matrix. Another important thing is the location of this type holes inside of the polymer matrix - in some cases corresponding holes are located only very close to the electrodes. This means that there are no very long dendrites inside of the polymer matrix because gas formation can occur only on the electrodes. Another SEM picture shows that in some other point of such actuator (much more close to the contacts) such type of holes are located also quite far from electrodes inside of the polymer matrix. X-ray map-pictures for copper shows also that amount of copper inside the polymer matrix is in this case much bigger and these higher concentrations can be found much deeper inside of the polymer matrix.

On the copper dendrites (which are connected with electrodes) is produced gaseous hydrogen and oxygen during the water electrolysis. After switching polarity detonating gas is produced:

(cathode): 2 H(+) - 2 e(-) -> H(2) (gas)

(anode): 2 OH(-) + 2 e (-) -> 1/2 O(2) (gas)

After that occurs detonating gas explosion. For this reaction it is needed at the room temperature a catalyst (platinum). And such actuator which has platinum electrodes and which is prepared by using impregnation-reduction method contains always a very small amount of platinum inside of the polymer matrix (can be seen also on the X-ray line-scan (Figure **)).

We did add this information also to the paper.

Answer 5. b) About Cu(+) compound formation after the covering IPMC electrodes with copper layer.

We did clean a MuscleSheet(TM) type IPMC actuator by boiling in 1 M hydrochloric acid. After that we did clean this muscle from residue of hydrochloric acid by boiling in deionised water. And then we put this IPMC sample to the 1 M CuSO(4) solution for overnight.

Then we covered this sample by electrochemical plating method in the same solution with copper layer. After that we put this back to the same solution. And in this case we did recognize after staying overnight that insoluble colourless compound was formed. By using X-ray  microprobe elemental analysis we get data, that this (insoluble, in wet sate transparent) compound contains only following elements: a) copper b) chlorine. It gives to us a reason to suppose that this compound is CuCl because there is no other insoluble compound containing only these two elements. After that we did put freshly with copper layer covered IPMC sample to the deionised water and no essential visual changes did happend. From this information it can be concluded that small amount of Cl- -ions mainly from not fully clean IPMC-sample after boiling in hydrochloric acid did cause such compound formation.

Question 6.     Figure and table captions need to contain more detailed description of data and samples. ex) in Table 1; description of sample 1, 2 and 3?

Answer 6. All the 3 samples are prepared in the same way. There is variability in numbers but main trends are the same for all samples.

Question 7.     Table 1 is hard to understand. Please explain why negative potential was applied for relaxing?

Answer 7. Actually negative potentials are applied not for relaxing. Using of word “relaxation” in this case was a mistake; we did change this word in manuscript.

Opposite potentials are used for more uniform copper layer formation.

Question 8.     Please explain what is the meaning of +100 in table 1? Is there any specific reason to give 1 second for relaxation?

Answer 8. “+100” means additional 100 cycles in the same direction.

During 1 second of applied opposite potential sample bends back to opposite direction compared to the last bending. Aw also write in manuscript, the problem with this type of IPMCs rather seems to be the Cu depletion on the anode side, which possibly is the reason for the decreasing bending angle upon cycling. By applying 1 second opposite pulse we tried to avoid this problem (at least partially). And also opposite potentials are used for more uniform copper layer formation.