Figure 1. SEM image of the cross-section of a MuscleSheet™ IPMC before copper deposition.

Figure 2. X-ray line-scan of the IPMC cross-section after copper layer deposition on the electrodes.

Figure 3. The experimental setup for measuring resistance on the surface layer of an IPMC.

Figure 4. A Cu-coated IPMC sample with contacts.

Figure 5. Driving pulses during one cycle in a resitivity measurement.

Figure 6. Electrode resistivity at the left and right electrode for MuscleSheet™ IPMCs upon mechanical bending. Bending to negative angles corresponds to bending towards the left.

Figure 7. X-ray line-scan of the Cu-IPMC cross section after cycling 300 cycles with  voltage pulses of 2 V magnitude.

Figure 8. X-ray line-scan of the Cu-IPMC cross section after cycling 300 cycles with voltage pulses of 4.5 V magnitude.

Figure 9. SEM image of destroyed  Cu-IPMC cross section after cycling at 4.5 V.