Low voltage linear actuators based on carbide derived carbon powder

Janno Torop(a), Mati Arulepp(a,b), Jaan Leis(b,c), Andres Punning(a), Urmas Johanson(a), Alvo Aabloo(a)

(a) ‘IMS Lab, Institute of Technology, University of Tartu, Nooruse 1, 50411 Tartu, Estonia

(b) Carbon Nanotech Ltd, Riia 185, 51014 Tartu, Estonia

(c) Institute of Chemistry, University of Tartu, Viljandi 42, 50411 Tartu, Estonia

Abstract

Novel linear electromechanical actuators based on nanoporous TiC-derived carbons was prepared and studied. Traditionally, thin membranes containing mobile ions inside are used for bending actuators. We describe a linear actuator which consists from carbon material thin films and ionic liquid. The thin film is made from nanoporous TiC-derived carbon powder and polytetrafluoroethylene (PTFE) as a binder agent. The working mechanism of the actuators is based on the interactions between the high-surface carbide derived carbon (CDC) and the ions of the electrolyte. These actuators are able to generate linear actuation of about 1% from their thickness under the voltage less than 3 V. The motion starts already at 0.8V and the magnitude of actuation is related to the electrical charge of the device. Two different types of electrolyte were used: 1) Ionic liquid (EMITf) and 2) Tetra-alcyl-ammonium salt in propylene carbonate (PC) solution. The actuators with ionic liquid have 70% higher movement. The parameters of the actuators were studied by cyclic voltammetry and electrochemical impedance spectroscopy.

# Keywords: Linear actuator, carbide-derived carbon (CDC), ionic liquid, electroactive polymer (EAP)

# INTRODUCTION

There is an increasing interest in using soft actuators in the field of biomimetic devices, since they mimic the behavior of biological muscles. The materials are attractive for creating artificial muscles used in biologically inspired robots, not least underwater robotic applications[,,. In other hand, microapplications like MEMS, microfluidics and engineered devices housing hydrogel valves, filters, and lenses,, as well as other soft material actuators that mimic natural movement in microfluidics There exists today an emerging scientific field, where several electroactive polymers[] are exploited for a great variety of applications. Mechanical actuators that simultaneously may provide high power densities and large force generation capacities are of great scientific and technological interest. There are several electroactive materials well-known. Electroactive polymer (EAP) transducers have large displacement under low bias (several volts). So far, EAP actuators have serious disadvantage in practical use due to low force. Several applications require small displacement with considerably high force, therefore piesoceramics are often used to generate micron scale actuation with large forcing output. Carbon/polymer thin sheets, main components of supercapacitors, provide micron scale displacement under low bias, contrary to piesoceramics which require high voltage. Supercapacitors are highly capacitive devices famous for their high power densities and energy efficiency up to 97% during charging-discharging cycle [Conway]. In principal, the design of supercapacitors is comparable to ionic polymer actuators. They consist of two high surface area electrodes and separator in between. Porous polymer separator is a reservoir of electrolyte and reduces conductance between electrodes.

We propose the material with linear actuation properties which consists from carbon material thin films and ionic liquid. The thin film is made from nanoporous TiC-derived carbon powder and polytetrafluoroethylene (PTFE) as a binder agent.

Carbon produced by extraction of metals from metal carbides is called carbide derived carbon(CDC) . The described method[Gogotsi] of carbon synthesis offers unique control over carbon microstructure and allows to fine-tune porosity at the nanoscale. Applications proposed for CDCs are fuel cells, hydrogen storage and different extraction/purification methods of noble gases based on the selective adsorption. However, main force of the development is focused to electrochemical storage devices, such are super- or ultracapacitors.

Fig. 1. A structure (a) and High Resolution Transmission Electron Microscope (HRTEM) picture (b) of amorphous microporous carbon.

Microporous amorphous carbons have non-uniform distribution of the curved graphene flakes as shown in Figure 1. []. Carbon atoms have hybridization of sp2, but graphene forms 3D network. Advanced CDC materials have high electric double layer (EDL) capacitance (130 F g-1 in nonaq. electrolyte). Hahn et al. performed dilatometric studies on the porous and graphitic carbon electrodes and observed significant reversible volumetric effects in the electrodes during the charging-discharging, results confirmed the electroactive properties of porous carbon. The electroactive mechanism of carbon is based on the charging of electric double layer. The electric energy is stored by formation of double-layer at carbon/electrolyte interface, process is electrostatic and Faradaic reactions do not occur. Large capacity of porous carbon electrodes is provided by high specific surface area (typically 500 to 2000 m2g-1).

The expansion of the carbonaceous electrodes is generally undesired and crucial factor for the cycle ability of energy storage devices.

# Experimental Details

## Preparation of material

Carbon

TiC-derived carbon powder, precursor of the actuator electrodes, was produced by Carbon Nanotech Ltd.  TiC derived carbon is synthesized from titanium carbide by chlorination at high temperature (400 - 900 °C) Reaction product is amorphous carbon powder with particle size 2-5 m and large quantity of very small nanopores with pore size 6-9 Å in those powder particles.

Carbon-polymer film

The porous carbon electrodes films were prepared from the mixture of 92% (wt.) TiC-derived carbon powder and 8% (wt) PTFE binder polymer (Aldrich, 60% suspension in water) and rolled into to the thin active material sheet with a final thickness of 100 ± 5 m CDC powder (1g) was mixed with 6 mL of ethanol and added PTFE suspension in water to form slurry, which thereafter was gently pressed until a wet cake was formed. After evaporation of ethanol and water the cake was impregnated with heptane. A flatten carbon/polymer cake shaped to a multilayer cylinder and rolled in the axial direction of the cylinder. The latter procedure was repeated until elastic properties appeared to the carbon/polymer sheet. Finally, the heptane was removed at ~110ºC. The carbon/polymer sheet was rolled stepwise down to the desired thickness, dried in vacuum at 170ºC and coated from one side with a thin (~2(m) aluminum layer, using Plasma Activated Physical Vapor Deposition. The electrode discs of desired size were cut from these sheets.  Importance of aluminum coating for reducing the contact resistance between carbon layer and current collector is studied and confirmed by Leis et al. [ja viide kus?].

## Assembling of the actuators

The linear actuators 1 – 4 (see Table 1) were assembled from the pairs of carbon electrode discs (Ø 1,7 cm), separated with an ion-permeable separator paper from Kodoshi Nippon ( Fig. 2). Each actuator consisted of five electrode pairs with a total geometric surface area of 11.35 cm2. The electrode assembly was placed in the sealed aluminum container. The additional mechanical pressure (p=48 N cm-2) was applied by the spring through a special connecting rod. This rod was further used for measuring the linear movement of actuator by laser beam.

Fig. 2. The principal scheme of a linear actuator.

The actuator cells were vacuumed at 120° C for 24 h before being impregnated with the electrolyte. The electrolytes used in this study were 1.0 M tetraethylammonium tetrafluoroborate in propylene carbonate (“Honeywell Digirena ®” TEABF4/PC, H2O < 0.003 %) and the ionic liquid 1-ethyl-3methyl-imidazolium trifluoromethane-sulfonate (EMITf, Fluka)

Table 1. The linear actuators tested in this study

| Actuator # | Notation of actuator | Notation of CDC material | Electrolyte |
| --- | --- | --- | --- |
| 1 | TEA600 | TiC-600 | 1.0 M TEABF4/PC |
| 2 | TEA800 | TiC-800 | 1.0 M TEABF4/PC |
| 3 | EMI600 | TiC-600 | EMITf |
| 4 | EMI800 | TiC-800 | EMITf |

## Electromechanical measurements

The test cell of the linear actuator is depicted in consisted of two fundamental parts – the electrochemical actuator and the optical detecting mechanism. The actuator is assembled in a sealed cell. The cell incorporates a spiral spring, compressing the actuator by the force of 100N. The optical system is mounted on the top of the cell. The mechanical coupling between the actuator and the optical system is implemented by a shifting vertical rod. The movement of the rod is transferred to the moving mirror using a steel eccentric and a lever. This mechanics magnifies the scale of movement of the actuator by 25 times. Further magnification of the scale is performed by a laser beam, reflecting from the mirror and targeted to a distant screen, as depicted in Fig. 3. The described optical system is able to magnify the scale of movement of the linear actuator by thousands of times, depending solely on the distance of the screen. In the course of the experiments the distance to the screen was a few meters and the expansion of the actuator by 1 (m was detectable as a displacement of the spot of the laser beam on the screen by 1 cm. The displacement of the spot on the screen was recorded by a highspeed firewire camera and the motion was thereafter digitalized using LabView software. Simultaneously, the electrical parameters - voltage and electric current – were recorded using National Instruments PCI-6034 DAQ card and LabView software. The electric current was measured as a voltage drop over the low resistance R.

The extent of actuation of the actuators in time-domain was detected using a custom-made optical system. The measurements were performed in two modes: (i) a constant current charge-discharge process (CC mode, triangular voltage spread in time). In CC mode we observed tendency of decreasing performance when actuators were charged relatively high current. To achieve maximum performance of actuators we combined constant current method with constant potential method (ii) (CCCP mode, rectangular voltage spread in time). Actuation is correlated and limited with the charge inserted in actuator.

Fig. 3. Illustration of the experiment setup.

# Results and Discussion

To study the actuators in detail, the CCCP mode was used. After charging the actuator to 1.5-3 V using constant current IC (???), a constant potential VC (???) was applied for up to 5 minutes. This method helps to examine the dynamics and the amplitude of actuation. During the period of the constant potential the current decreases substantially and the maximum amplitude appears in few minutes. In the course of different experiments the amperage of the constant current was varied in the range of 50 to 1000 mA.

Fig. 4. CCCP measurement of EMI800 (IC = 400 mA, VC = 2.5V)

The mechanical response of linear actuator EMI800(#4 in Table 1) under voltage 2.5 V (CCCP mode) is shown in Fig. 4a. The actuation amplitude reaches its maximum and remains stable in about 120 seconds, while the voltage reaches its stable level already in 60 seconds. This diagram is very typical, the similar behavior was observed in all tested actuators. . The actuation-charge diagram shown in Fig. 4b indicates a nonlinear correlation between the actuation and electric charge stored and released during charging and discharging cycle of the actuator.

Fig. 5. CCCP measurement of EMI800 (IC = 1000 mA, VC = 3 V);a) voltage and current; b) actuation and charge

Fig. 5. depicts the series of periodic charging-discharging cycles of the actuator. As the charging current is high (1 A), the period of constant current ceases already in few seconds. During this time interval almost no movement is detected, since the voltage is low and the adsorption of ions is a diffusion-limited process in the porous electrodes. The current dies away slowly due to the internal resistance of the actuator. During discharging cycle the charge is released,current peak reaches up to 1.2 A and actuator shrinks. In our experiment ??? While discharging by a short-circuit, the adsorbed energy is wasted through the low ohmic discharge resistor. Kasulikkus….kasutegur….

## The actuation is correlated and limited with the charge inserted in actuator. Hahn et al[crossreference]expected that the charge specific expansion increases with the degree of graphitization and the apparent density of the carbon materials. They observed that the relative expansion of the graphitic carbon materials for a specific charge is larger than the respective expansion of microporous carbon materials. However, graphitic carbon materials demonstrated non reversible actuation due to ion intercalation process which causing volumetric dimensional changes in these materials. Relatively low density and sparsity of 3D network of porous carbon electrodes are main properties providing good reversibility during cycling between 0-3 volts.

# CONCLUSIONS

Wee demonstrated the actuator for short range actuation applications capable to develop pressure 50 N cm-2. Lifetime of the actuator is up to 106 cycles and energy efficiency 90 % due to device is evolved from material commonly used in supercapacitors. Improvements in energy efficiency may accelerate the development of electromechanical actuators as well as provide industrial and consumer applications.

Räägid yle:

Laengu ja liigutuse defineritud seos

Korratvus

Eluiga

Valmistamine

Mikrovalmistamine…

References

# Comments

Siiia lõik erinevatest aktuaatoritest akki?

viide kus describeeritud...

Kas on oma tehtud pilt? kui ei ole siis viide, kust võetud...

Paremat sõna vaja?? Omadussõna mis kirjeldaks pasta taolist ollust

Siia oleks mikrojoonist vaja…

Ei kasuta eksitavaid asesõnu..mis pingeni laeti?

Kas tõesti kõik kolm asja, pinge vool ja liigutus olio vahemikus -1-+7 ?

Janno:On jah nii trehvanud, et kõik kolm suurust mahuvad ilusti graafikule

Eir samplite erinevus, solventide erinevus…

Artiklil vist vaja oma rferentide stiil panna: Style 	SPIE REFERENCES

# Endnotes

Y. Bar-Cohen (ed.), Biomimetics – Biologically inspired Technologies, CRC Press, Boca Raton, FL (2006).

. Guo, T. Fukuda and K. Asaka, IEEE/ASME Trans. Mechatron. 8 (2003) 136–141.

N. Kamamichi, M. Yamakita, T. Kozuki, K. Asaka and Z.-W. Luo, Adv. Robotics, 21 (2007) 65–85.

Punning, A.; Anton, M.; Kruusmaa, M.; Aabloo, A. (2004). A Biologically Inspired Ray-like Underwater Robot with Electroactive Polymer Pectoral Fins. IEEE Confrence "Mechatronics and Robotics 2004" (MechRob04); Aachen, Germany; 13.-15.09.2004. Aachen: Eysoldt, 2004, (2), 241 - 245.

S. Collins, A. Ruina, R. Tedrake, M. Wisse, Science 2005, 307, 1082.

Aram J. Chung, Donn Kim and David Erickson, Lab Chip, 2008, 8, 330 – 338.

J. Y. Park, H. J. Oh, D. J. Kim, J. Y. Baek, S. H. Lee, J. Micromech. Microeng. 2006, 16, 656.

D. Kim, D. J. Beebe, Lab Chip 2007, 7, 193.

L. Dong, A. K. Agarwal, D. J. Beebe, H. R. Jiang, Nature 2006, 442, 551.

Gu Han Kwon, Joong Yull Park, Jeong Yoon Kim, Megan L. Frisk, David J. Beebe, and Sang-Hoon Lee, Small 2008, 4, No. 12, 2148–2153

Gogotsi, Y., Nikitin, A., Ye, H., Zhou, W., Fischer, J. E., Yi, B., Foley, H. C., Barsoum, M. W. Nanoporous carbide-derived carbon with tunable pore size. Nature Materials 2003, 2, 591-594

Hahn, M., Barbieri, O., Gallay, R., Kötz, R. A dilatometric study of the voltage limitation of carbonaceous electrodes in aprotic EDLC type electrolytes by charge-induced strain. Carbon 2006, 44, 2523

Hahn, M., Barbieri, O., Campana, F.P., Kötz, R., Gallay, R. Carbon based double layer capacitors with aprotic electrolyte solutions: the possible role of intercalation/insertion process. Appl. Phys. 2006, 633-638

Conway, B.E. Electrochemical Supercapacitors. Scientific Fundamentals and Technological Applications. Kluwer Academic, Plenum Publishers, New York, 1999