Electro-mechanical model of something

Authors: Veix, Punn, Alvo

INTRODUCTION

Electro-active polymers or EAPs are materials that change their shape and size when electrically stimulated. As both actuators and sensors they are considered attractive for various applications in e.g. biomedicine and robotics. Roughly EAPs can be divided into dielectric and ionic actuators. In this work the focus is on ionic EAPs. The state of art of EAP devices is reached the level of the first commercial outputs of EAP actuators, e.g. the ViviTouch tactile feedback system taking the gaming experience of mobile devices to the next level and Optotune’s electrically tuneable lens.

Although there are some commercial products of the EAPs, there is still much research to carry out. Whereas the bending motion of described actuators is easily attainable, it is rather complicated to estimate that bending motion and control the system precisely. Already some decent models have been developed to describe the tip displacement or the blocking force for instance. In the models currently available, several assumptions are made which are more or less limiting the usability of the models.

One possible approach to model the behaviour of an EAP is through the curvature and bending moments. Anton et al added an elongation to an IPMC actuator and constructed a mechanical model. One important conclusion of their work was that the distribution of an EIBM (Electrically Induced Bending Moment) is not constant along the length of the actuator i.e. the deflection of the actuator is growing faster near contacts and slower by moving away from contacts. One factor of this effect is the high resistance of the electrodes.

More particularly the effect clearly shows up in case of carbon polymer composites (CPC). Although, the variable curvature along the actuator can be avoided by adding an extra layer of gold for high surface conductance, it ruins one of the main advantages of CPC – it contains no metals.

Punning et al introduced the correspondence between IPMC (ionic polymer metal composites) and a RC transmission lines. It appears that the voltage distribution along the IPMC actuator can be expressed similarly as RC lines. Although there was noticeable linear correlation between the charge and the curvature, it was validated in a short time frame, thus neglected the back-relaxation phenomena. Therefore it is important to add a term describing back-relaxation for accurate modelling in a long time perspective.

The objective of the work is to obtain the time-dependent correspondence between the transient input voltage and the shape of the actuator. Similarly to the model of Punning, we consider EIBM to be a linear function of charge along the actuator. Compared to most of the models developed so far, the distributed curvature analysis adds the possibility to estimate the shape of the actuator much more precisely.

Back-relaxation.?

IPMC exhibits back-relaxation i.e. a slow large relaxation towards cathode after quick bending towards anode.

The major difference in actuation due to the size of the cations has been also denoted by Bar Cohen. (Two time constants.)

This paper is concerned with description of bending behaviour of ionic EAPs by means of electrically induced bending moment as a function of time and coordinate along the actuator.

Model description

The key component of the model is time dependent and coordinate dependent charge qs,t. This charge initiates internal stresses and results bending motion of the material. The model consists of two parts: an electrically induced quick bending that produces electrically induced bending moment (EIBM) followed by slow relaxation component in the opposite direction. The relaxation is described through back-relaxation bending moment (BRBM) – a bending moment opposite to EIBM that is increasing in time. For the sake of simplicity let us assume that the charge is producing EIBM linearly:

|  | EIBMs,t=α∙qs,t |  |
| --- | --- | --- |

where α is the coefficient relating charge and moment.

The relaxation of the actuator can be also expressed in terms of charge with an additional exponential term (eq. 2). This equation is very similar to the Kelvin-Voigt model which has been used to model creep of polymers. The difference lies on the argument of exponent where linear time component λt is replaced by an integral of charge over time. Notice that from the time charge has reached its maximum value i.e. charge is constant in time, the presented integral is simply growing linearly in time as the argument of exponent in Kelvin-Voigt model. Similarly to Kelvin-Voigt model we have accommodated the parameter λ that denotes the rate of relaxation and is expressed by λ=E/η, where E and η are the modulus of elasticity and viscosity of the material correspondingly.

|  | BRBMs,t=α∙qs,t∙1-e-λ0tqs,τ dτ |  |
| --- | --- | --- |

Combining eq. 1 and 2, the total bending moment is given by:

|  | Ms,t=EIBMs,t-BRBMs,t=α∙qs,t∙e-λ0tqs,τ dτ |  |
| --- | --- | --- |

We have stated the relations between the charge and corresponding bending moments. Next, a well-known Euler-Bernoulli beam theory is applied to obtain curvature from bending moments.

|  | ρs=dφds=MsEI |  |
| --- | --- | --- |

where EI is the bending stiffness, E is the effective modulus of elasticity and I is the second moment of area. In our case the cross-section of the beam is a rectangle, thus I can be found from I=(bh3)/12, where b and h are width and height of the cross-section of the beam respectively.

Denoting a=α/EI and substituting eq. 3 into eq. 4 we can now write the equation for curvature:

|  | ρs,t=a∙qs,t∙e-λ0tqs,τ dτ+ρ0s |  |
| --- | --- | --- |

where ρ0is the initial curvature of the actuator.

The curvature can be also presented in Cartesian coordinates as:

curves=0scos⁡(φs)ds+x0  0ssinφsds+y0

where x0 and y0 are the initial position of the curve and

φs=0sρsds+φ0

where φ0is initial angle at s=0.

Experimental setup

The actuation process of a carbon polymer composite (CPC) material was observed visually. The shape of the actuator was recorded by CCD camera (Pointgray) at 10 frames per second. Grabbed video was filtered after which the vector representation of the actuator was obtained. The length of each vector was 2.6 mm. All tasks from controlling the voltage between the electrodes up to the post processing of the curvature changes were carried out with NI LabView software with Matlab engine for numerical model evaluations. The four input parameters of the distributed RC model were determined using the differential evolution (DE) optimisation algorithm minimising the differences between the measured and the modelled voltage between electrodes along the actuator. DE algorithm is genetic type algorithm that combines and rearranges parameter vectors. The algorithm is converging fast and is effective for solving problems with multiple local minimums as this particular task is. The value of a was determined from eq. 1 by assuming the back-relaxation component to be zero near the beginning of the actuation. The second parameter λ can derived from eq. 5:

λ=lnρs,t-ρ0sa∙qs,t-0tqs,τ dτ

It is obvious that at the beginning of actuation the relative error of ρ is large thus has a major impact to λ. Therefore λ was determined by averaging the values in between 120s<t<300s. The parameters for distributed voltage optimised parameters for charge calculation along with the determined parameters a and λ are depicted in the table 1.

| Parameter | Value |
| --- | --- |
| R | 1.6kΩcm |
| C | 0.011Fcm |
| W | 5.11kΩ∙cm |
| G | 0.0981kΩ∙cm |
| a | 2.0 |
| λ | 1/0.3 |

Table 1. Measured parameters for CPC actuator.

:

Results

The simulated points are clearly following the actual shape of the actuator. The shape of the actuator

T

| Fig. 1 Measured and modelled shapes of the actuator at 2.5V. | Fig. 2. Measured and modelled shapes of the actuator at 2.5V |
| --- | --- |

Conclusion and discussion

Acknowledgments

References

[1] Chenying Yang, Wei Wang and Zhihong Li, "Optimization of corona-triggered PDMS-PDMS bonding method," in Nano/Micro Engineered and Molecular Systems, 2009. NEMS 2009. 4th IEEE International Conference on, 2009, pp. 319-322.

Load function by gravity: qs=w*cosφ(s)

Shear force: Vs=V0+qs ds

Moment: Ms=M0+Vs ds

Euler-Bernoulli’s law:

ρs=MsEI

where EI is the bending stiffness, E is the effective young modulus and I is the second moment of area. If the cross-section of the beam is a rectangle, I is represented as:

I=bh312

b and h are width and height of the cross-section of the beam respectively.

Angle-curvature relationship:

φs=ρsds

Relationship between the angles along the actuator and the corresponding point in (x,y) plane:

curves=cos⁡(φs)ds+x0 sin⁡(φs)ds+y0