# Optimization of electrochemically active material utilization in 3D microbattery by finite element modeling

Vahur Zadin, Heiki Kasemägi, Daniel Brandell, Alvo Aabloo

# Abstract:

Method for modeling ionic transport in 3D microbattery (3D-MB) has been presented. In 3D-MB performance of battery depends critically from homogeneous charge transfer between electrodes. Unlike in conventional battery, where homogeneous charge transfer between electrodes is independent from material parameters, in 3D-MB material properties and geometry must be carefully engineered to ensure charge transfer between electrodes to be as homogeneous as possible. 1D mathematical model describing conventional Li-Ion battery has been extended to describe ionic transport in 3D microbattery and FEA has been used to optimize electrochemically active surface area utilization by studying effects of changing electrode and conductivity, diffusion coefficient and length. As a result of simulations, it is clear, that optimization of electrochemically active surface area usage can be primarily done by manipulating with electrode conductivity and diffusion coefficient (quantify, set some numbers, how much better). As the range of manipulating with material properties is limited, changing electrode length can be used to fine-tune surface-area usage. Simulation results also points out some principal differences between conventional Li-Ion battery and 3D microbattery architectures. Extensions for basic model are presented to overcome those differences.(what is the meaning of this)

# Introduction

Portable microbattery supply is critical factor in many developing technologies – miniaturization of microelectronics has far outpaced advances in small scale power supplies. Lack of suitable portable power supplies is stopping development progress in many technology branches, like microelectromechanical devices (MEMS) [ reference here ]and biomedical micro machines. An example from MEMS based device is autonomous device that is powered by battery and consists of one or more sensors, computation and communication circuit with dimensions about 1 mm. By using such kind of configuration, problems with existing lithium-ion batteries, which are from nature 2D, are revealing themselves – in so small volumes, it is not possible to achieve sufficient energy densities. This problem can be solved by implementing batteries which are three-dimensional (3D) in their architecture. In current work, architecture of a battery is considered to be its geometrical design material properties. A conventional 2D-battery architecture can be represented as a sandwich, consisting of current collector, positive electrode, electrolyte (separator), negative electrode and current collector in a layer-by-layer configuration (Fig. 1). 3D-micro-batteries (3D-MBs) consist of same components, but with a more complex spatial distribution. The increased area-gain achieved by designing the battery in the third dimension can theoretically expand the energy density within an order of magnitude or more. Examples of possible 3D-MB architectures are presented in Fig. 2: 3D-interdigitated (a), 3D-trench (b), 3D-concentric (c) and aperiodic (d) architectures. It should be pointed out, however, that so far no one has yet completed synthezing a commercial full micro-battery system based on these architectures, only experimental batteries [9,10] and half cells have been made [11]. This field of science is still emerging, but emerging fast. New materials are being introduced, and advanced micro-structures being synthesized at a growing pace.

Experimental work on microbattery, current collectors, electrodes, material and geometry. Then modeling.

Modeling processes taking place in Li-ion batteries is generally carried out using approach proposed in [1] and [2]. In these works, 1D mathematical model is presented, where porous electrode theory is used to model electrodes, and it is assumed, that electrodes are porous and form superposition of active material, binder and electrolyte. To model electrolyte, concentrated solution theory is used. Ionic transport in active material particles is modelled by diffusion. Model presented in these works is very general and is applicable to wide range of Li-ion systems. Model presented by Newman is validated in [3]. Other works [danilov], [mesocale approac], are using Nernst-Plank equation approach and eventually coincide with [2], [mesoscale] or are based on equivalent electronic network [Notten’s works] or molecular dynamics simulations [Anti?, Endel?]. Although, having good agreement between simulations and experimental results, equivalent electronic network model lack ability to describe local processes taking place in battery, necessary to analyse processes in 3D-MB. Molecular dynamics simulations can not be used in whole battery modeling, as it's not possible to simulate systems large enough, to describe whole battery.

Experimental work about electrode materials and geometry?

Building half cells of nanopillars, nanotrences, etc. is complicated task. Even more complicated  or even impossible  is optimizing 3D-MB systems based by experimental work.

All presented models are dedicated to study conventional Li-ion batteries, that are from nature, 2D. Moreover, to study those batteies, mathematical models can be spatially 1D. In current work, mathematical model presented in [2] is extended to 3D battery systems to make it possible to model 3D-MB systems. Aim of this study is to understand basic features of different 3D-MB architectures and at same time, point out ways to optimize battery architectures and test theoretical limits of different geometries.

# Materials and methods

Materials, from which 3D-MB's are constructed  are still under study it is not clear yet, what sort of materials to use. As there is in literature lots of materials about LiCoO2 anode and C6 graphite cathode, we are using in our simulations right now these materials as starting point.

Chemical reactions taking place in battery electrodes are:

|  | (1) |
| --- | --- |
|  | (2) |

In our model, we are describing reactions taking place in battery by Li ion concentrations. When battery is fully discharged, then in anode, Li+ concentration is maximal and Li+ concentration in cathode (C6) is minimal. When battery is fully charged, then Li+ concentration in anode is minimal and in cathode maximal.

## Geometrical model

Basic architectures proposed for 3D-MB are presented in [Dunn's review article] and pointed out on Fig. 2. To simulate processes taking place in whole whole battery, it is necessary to model all battery architectures, based on these geometries, in 3D, with exception of trench model. By using trench model, it is possible to reduce simulations to 2D and expand results from calculations to 3D. Also, by placing a slice through one symmetry axis of a interdigitated model, it we get a 2D approximation, that coincides with trench model. It is desirable to reduce spatial dimensions in geometrical model of the battery as low as possible, to reduce necessary computer resources during simulations. Thus, in calculations, 2D approximation of trench model is used, as it is possible to extend obtained results to several different geometries without any loss of accuracy.

Basic model for simulations – trench model is constructed with electrode plate length L=100e-6m and thickness 10e-6m. Distance between electrodes is 10e-6m. Length of plate is varied during different calculations.

Electrodes in trench model are made completely from active material. Anode consists of LiCoO2 and cathode from C6. Electrolyte is chosen to be 1.5 molar LiPF6. Current collectors on top of electrodes are simulated by boundary conditions. To current collector on positive electrode, charging/discharging current is applied and current collector on negative electrode is grounded, as we are interested in potential differences in battery.

To describe whole battery with optimal usage of computer resources, small cell consisting of one anode and one cathode plate is selected and periodic boundary conditions for concentration and potentials in electrodes and electrolyte on cell sides are applied. Thus, in calculations infinitely large battery is simulated.

## Mathematical models used in study

Modelling only electrolyte

In our studies, two mathematical models were used, to simulate processes, taking place in Lithium-ion battery. First model based on Nernst-Plank equation, proposed in [danilov], second model, based on concentrated solution and porous electrode theories [newman].

Assumptions made for setting up Nernst-Plank equation based model [danilov] are following:

- Diffusion constants and conductivities are considered constant within a respective region in the battery.

- Active material particles and binder forming electrodes are assumed to form one solid elecrode

- Side reactions are neglected in whole cell

- Volume changes in electrodes are neglected

- Electroneutrality is assumed in electrolyte.

- Charge transfer is described by Ohm's law, formation of Helmholz double layer on surface between elecrode and electrolyte is neglected by assuring continuity of current moving from electrode to electrolyte.

- Constant values for transference number are assumed at all times and all points in battery.

- Ions are transported by diffusion and migration in electrolyte. Transport of ions in electrolyte is not described.

Shortcomings of this approach are, that it is not taking into account formation of Helmholz double-layer on surface between electrode-electrolyte and and ability to model only battery with infinite capacity. Althoug, the model lacks the ability to describe Helmholz double layer on electrode-electrolyte interface and uses simplified approach to calculate potential in electrolyte, it is easy to implement and it is not so nonlinear, than equation system archived by  [newman], thus demonstrating considerably better solution convergence capabilities.

According to [danilov] equation describing concentration profile development in the electrolyte of the battery is

| , | (3) |
| --- | --- |

with boundary conditions on surfaces between electrodes and electrolyte

| , | (4) |
| --- | --- |

where D is diffusivity of electrolyte and is calculated by ,  J current density on surface between electrode and electrolyte and is unit normal on on surface between electrode and electrolyte.

It is possible to approximate battery with model, that consists of three resistors – anode, electrolyte and cathode. Electrical current is entering from current collector, attached to anode, moves through battery and leaves through current collector, attached to cathode. Considering it, current density   in battery is calculated by Ohm's law

|  | (5) |
| --- | --- |
|  | (6) |

Where J_0 is current density on current collector and is, depending of region of the battery, electronic conductivity of electrode, or  ionic conductivity of electrolyte.

Modeling whole cell

In current work, we are modeling battery with non-porous electrodes, made from mixture of active material particles and binder. To set up mathematical model, we are using previously published and validated approach[2] as basis. It is modified to take into account that electrodes are made only from active material (how it's modified). According to [book], where porous electrode theory extension is presented, to model thin film batteries made from nonporous active material.

During constructing mathematical model, describing processes taking place in battery, that is basing on  [newman things], we made following assumptions:

- Diffusion constants and conductivities are considered constant within a respective region in the battery.

- Active material particles and binder forming electrodes are assumed to form one solid elecrode, where movement of Li ions is described by diffusion.

- Side reactions are neglected in whole cell

- Volume changes in electrodes are neglected

- Charge transfer processes over the electrode-electrolyte interface are assumed to be described by Butler-Volmer type kinetic expression:

|  | (7) |
| --- | --- |

- To model open circuit potential in electrodes, piecewise polynomials are used [U_oc].  In some other place

- Constant values for transference number are assumed at all times and all points in battery.

- Electroneutrality is assumed in electrolyte.

- Ions are transported by diffusion in active material and by diffusion and migration in electrolyte.

It is not yet known what sort of electrode is more efficient to use  for 3D-MB – porous or nonporous. Recent experimental works show, that nonporous electrode material approach is good starting point [Gabi's experiments, cheah experiments ...]. Also, geometrical dimensions of battery electrodes are in same range as typical active material particles in porous electrodes. Thus we are setting up our battery model for nonporous electrodes. As we are modeling nonporous electrodes, electrochemical reactions are taking place only on surface between electrode and electrolyte. In [newman things], where there was assumption, that electrodes are forming composition of electrolyte, active material and binder, lithium insertion into the electrolyte was described by, so called, source term in differential equation in electrode area in battery. In our case, electrode is nonporous, and thus, electrolyte is not filling electrode making it impossible to describe lithium insertion by source term in differential equation, but by boundary conditions, as electrochemical reaction takes place on boundaries between electrode and electrolyte.  Thus, source term in equations presented in [Newman] disappears and insertion of lithium ions is controlled by boundary conditions [Advances in Li-ion batteries]. To obtain potential distribution in battery, Ohm's law is used for electrode and modified Ohm's law, taking  into account concentrated solution theory, is used for electrolyte. Accordingly, potential in electrolyte, , is calculated by equation

| , | (8) |
| --- | --- |
| , | (9) |

Where J is calculated by Butler-Volmer equation. Potential  in electrode is calculated by

| , | (10) |
| --- | --- |
| , | (11) |

with equation (11) applied to boundaries, that share interface with electrolyte. J is calculated by Butler-Volmer equation, boundary condition, applied to current collector of anode is

| , | (12) |
| --- | --- |

Where  is charging or discharging current, applied to current collector. Potential zero is chosen to be on current collector attached to cathode.

Equations to describe mass transport in electrolyte are

|  | (13) |
| --- | --- |
|  | (14) |

where D is diffusivity of electrolyte. Boundary condition (14) is applied to boundaries between electrode and electrolyte. To other boundaries, insulation boundary condition is applied, by setting flux of concentration to zero. Material balance in electrode is described by equation

|  | (15) |
| --- | --- |
| , | (16) |

Where dis diffusion coefficient of lithium in electrode material. Again, boundary condition (16) is applied to boundaries between electrode and electrolyte regions. At other regions, flux of concentration (or ions) is set to zero.

## Experimental setup

Electrochemically active surface area evalutaion

To achieve maximum capacity, maximum material usage and peak current of a 3D-MB – which is equivalent of optimizing its energy density – we must utilize the surface area of the electrode to a maximum. This is achieved automatically in a 2D-battery, where electrodes are flat. The current distribution in the electrodes and electrolyte is then homogeneous, and does not depend on the conductivity. In a 3D-battery, however, where the shape of the electrodes is more complicated, we must carefully engineer the shape of the electrodes, their conductivity and ionic diffusivity, in order to achieve a situation where the electrochemical activity on electrode surface – and thus also the current distribution in the electrolyte – is as uniform as possible. This task is more or less impossible to complete systematically with conventional experimental methods, but computer modelling and simulations can give significant insights.

Current distribution in 3D-MB battery depends from factors like diffusion coefficient, conductivities, processes taking place on solid-electrolyte interface (SEI), temperature, side reactions in battery, shape of electrodes etc. In current work, we are studying what effects do changing electrode geometry and material properties have on current distribution in battery.

To study electrochemically active surface area in battery, module of concentration gradient is used. According to equations (5, 7, 9, 11), concentration gradient is proportional to diffusion and migration of species in electrolyte. Concentration gradients at charging and discharging processes differ only by sign, thus, it describes both, charging and discharging processes.

To maximize electrochemical activity on electrode surface, we are looking for a electrode configuration, where differences, on surface between electrolyte and electrode, in concentration gradient are minimal. Simulations are carried out by varying electrode conductivities, length and radius of curvature of electrode corners. Initial material properties and electrode measurements are presented in table 1.

Simulations

Calculations to study effects of changing electrode conductivities, length and thickness of a 3D-MB were divided into three sections. In first section, dependence of electrochemical activity from electronic conductivity of the electrode was studied, while geometrical parameters of battery were fixed. In second section, dependence of electrochemical activity from electrode dimensions was studied, while physical parameters of electrode were fixed. Calculations were carried out by using trench model and modified trench model, where plate, forming electrode also included current collector (some figure to describe.).

In first section, during calculations, geometry of the electrodes and conductivity of the anode was fixed according to table .... . Conductivity of the cathode was varied by decreasing it by 25% steps from initial conductivity, in every sequential calculation. In last calculation, conductivity of the electrode was set to 5% of initial conductivity. Initial conductivity in cathode was set equal to the conductivity of the anode.

In second section of simulations, we studied effects of changing electrode geometry, presented on Fig. 6. During calculations, length L of a pillar/plate was varied by decreasing it, compared to initial length, by 25% steps in every sequential calculation, with length of pillar at  5% of initial value, in last calculation. Distance D between electrodes is held at constant value and material properties in all calculations were fixed according to table 1. In calculations, only length of a plate is changed. Changing it from maximum to minimum value, leads from 3D battery to 2D battery. As well, as changing plate thickness from it's minimum value to maximum value, leads again from 3D battery to 2D battery. Also, by decreasing length of a plate and holding distance D between electrodes constant leads to a situation, where relative thickness of a electrode is increasing. Thus during simulations, only electrode length L is changed.

In third section of calculations, effects of changing radius of curvature of electrode corners to electrochemical acitivity on electrode surface were studied. During simulations, radius of curvature of electrodes was changed from 4.9e-6m, to 2.5e-7m, with step 2.5e-7m.  Largest value of radius of curvature rendred top of the plate, forming electrode, round and smallest value made possible to use basically electrode with sharp corners.

### Material and geometry properties and initial values

Everithing according to table 1.

##### Mesh density and solver settings

In our studies, we are carrying out calculations where we are changing length of electrodes, radius of curvature of electrode corners and conductivity of electrodes. By making that kind of changes, in most cases, we need to generate new mesh to carry out calculation, with probable exception at study of conductivity. In every calculation, where we are changing geometry or material parameters, we must ensure, that element size in the mesh is small enough. When we are using too large elements, solution achieved by finite element method may not be correct (solution of our problem), but instead some solution, that is similar to our solution. To avoid that kind of situation, it is necessary to generate meshes, where element size is going sequentially smaller in every next simulation and compare solutions achieved on these meshes. When differences between solutions are small enough, mesh is considered to be dense enough.

To solve mathematical model describe in chapter ..... , we are using Comsol Multiphysics 3.5 and Comsol Script 1.3. In this program adaptive mesh generation algorithms are included, but unfortunately, these are available only for stationary problems. Thus, to ensure that elements of the mesh are with optimal size, we developed a script in Comsol Script, that compared solutions, achieved on sequentially denser meshes, in given reference points at every time step in simulation for concentrations and potentials in electrode and electrolyte by using equation

dsol = abs(sol_i-1 - sol_i)/sol_i-1,

where sol_0=u_sol, u_el, c_sol, c_el, calculated on coarser mesh and sol_1sol_0=u_sol, u_el, c_sol, c_el, calculated on denser mesh and i is mesh number. To calculate and compare quantities sol_0 and sol_1, finite differences reference grid was generated in geometrical model of battery, with distance l=1e-6m between nodes. This reference grid was same for all time moments in simulation. When every element in dsol<0.01, it was considered, that desired density of mesh was achieved.

On figure ... number of nodes and elements from simulations where influence of changing the length of electrode, on figure .... number of nodes and elements from simulations of influence of changing the radius of curvature and on figure .... number of nodes and elements from studies of influence of changing the conductivity of electrode are presented. In all calculations, quadratic Lagrange elements were used.

To solve time dependent matrix equation, achievd by applying finite element method to mathematical model, we were using direct solver umfpack provided by COMSOL Multiphysics, with relative tolerance .... and absolute tolerance ..., with bla-bla solver for time dependent problem.

Experimental validation of mathematical model, is not necessary, as our representation and modification of model presented in [2] does not introduce any principal mathematical changes. Our model coincides with model in [2], in terms of describing electrolyte and active material. Differences are introduced from battery architecture, as battery with porous electrodes, studied in [2] is rejected and replaced with nonporus electrode battery. Thus, Li ion sources, presented as source terms, in equations (......), in paper [2] are now introduced as boundary conditions (eq. ....). Experimental validation for model, used to study 2D porous electrode battery [2] is experimentally validated in [3]

# Results and discussion

Studies of electrode conductivity

Development of concentration profiles and concentration gradient has been calculated, to evaluate electrochemical activity on electrolyte-electrode interface, in first section of calculations (simulations, where conductivity of electrode was under study). In simulations, charging/discharging current applied to cell is equal to 1C current.

Calculated concentration gradient profile on electrode surface is presented on figure …. .  Concentration gradien has been calculated on edges 6, 23, 12, 24, 13, 25, 14, 26, 15, presented on figure … , for positive electrode (… line on fig), on edges 4, 19, 8, 20, 9, 21, 10, 22, 11 (fig …), for negative electrode (--- line on fig) and projected to straight line (horizontal axis at fig ….). At projections, length of edge elements, used in projections, has been normalized to unity, to plot on same figure concentration gradient development in time, or it’s values from different simulation sections, where conductivity of electrodes, length of electrodes etc were changed.

During simulations, conductivity of electrodes was changed, from equal values in electrodes, to conductivity values of the cathode at 5% of conductivity of the anode. changes in concentration profile are small (how small in %) thus, typical concentration gradients (at what time or soc moment) are chosen to illustrate whole charging/discharging process. Simulation results about changing cathode conductivity, by 25% steps from initial conductivity, are presented on Fig. 8, where figures of concentration gradient modules, corresponding to different electrode conductivity values are presented. From figure, we can see, when differences in conductivity of the electrodes are large, electrochemical activity is maximal on top of the electrode, which has better electrical conductivity, as electrical current is moving mostly through the electrode with better conductivity. Surface area usage moves towards to optimal, when difference in anode and cathode conductivity is getting smaller. When conductivities of the anode and the cathode become equal, surface area utilization becomes optimal, as most of the surface of the electrode is participating in electrochemical reactions at same rate. Electrochemical activity is differing then only at electrode corners, as electrical field on sharp corners is high and distance between electrodes is larger at these points. To move further with maximization of electrochemically active surface area, distance between electrodes should be uniform in every point in geometry, this can be achieved by making corners, which are in current model sharp, round.

Surface area utilization is in tolerable limits (what are these limits), when electrode conductivities are differing up to one magnitude. Technologically, it is hard to achieve situation, where conductivities of positive and negative electrodes are egual, as minimum difference between conductivities achievable for electrode materials today, is about two magnitudes. This encourages studying more complicated electrode architectures, where for example, copper current collector is introduced also into centre of positive electrode (fig_1), thus increasing total conductivity of positive electrode.

Studies of electrode dimensions

On figure, results of calculations described in section two, to study effects of changing electrode dimensions are presented as modules of concentration gradients.

From simulations where electrode length was changed, we can see, that decreasing electrode length tends to lead more uniform concentration gradient on electrodes (, with exception in sharp corners). This is caused by potential distribution in battery electrodes becoming more homogeneous, as potential drop in positive electrode decreases, when electrode lehght decreases, eventually reaching at limit, where 3D-MB architecture becomes ordinary 2D battery. Also, we can see, that concentration gradient is becoming high in sharp edges of the electrode, as electrical field there becomes large. Although, by decreasing electrode length, we can achieve more uniform electrochemical activity on electrode, we are also decreasing electrode surface area, thus decreasing capacity of the battery. High concentration gradient at electrode corners shows also, that it is necessary to round sharp corners, low concentration gradient points out, that it is desirable to ensure uniform distance between electrodes in every geometry point in battery.

By comparing results from simulations with different conductivities and electrode dimensions, we can see, it is possible to fine tune electrode surface area usage by changing simultaneously electrode length, radius, conductivity and distance between electrodes. Such- kind of fine tuning must be done carefully, as from one hand, we are winning in battery performance, but from other hand, we are losing in capacity.

Studies of the radius of curvature of the elecrode

Concentration gradient is presented for calculations carried out to study how the radius of curvature of the electrode affects electrochemical activity on electrode surface. From simulation results, we can conclude, that main difference is, when corners are sharp, concentration gradient goes very high on these sharp corner tips. When corners are round, or at extreme case, where top of the pillar is round (last simulation) concentration gradient is evenly high on that round top of the pillar. Concentration gradient is then divided more evenly on electrode. Of course, maximum of concentration gradient is then much lover, than in case of sharp corners. Result of the simulations were as expected.

General discussion

In present study, the parameters varied in our model have been length, electronic conductivity of the electrodes (different for anode and cathode) and radius of curvature of the electrode corners. We have here used parameter values taken from well-known Li-ion battery materials which are possible to synthesize as nano-materials. In order to optimize the micro-battery performance (with respect to both electrode length, thickness, conductivity, porosity, etc.), we need to go beyond our present one-parameter approach, i.e., where these parameters are studied separately. By using a one-parameter approach, we are only receiving a general picture about the nature of changes, parameter causes – e.g., decreasing length of the electrode also result in a decreasing differences in electrochemical activity on the electrode/electrolyte interface. It is therefore necessary to analyse more complex situations, where more than one parameter is changed at the time, for example, length, thickness and shape of the electrode, to find the optimal combination of these parameters.

Since we would like to study how the electrochemical activity on electrode/electrolyte solid interface depends on changing these four variables, we achieve a non-linear and thus mathematically complicated optimization problem, where we need to divide the planned studies into several tasks:

- Optimizing length, thickness and shape of the electrodes, based on what can be achieved experimentally.

- Choosing material combinations for anode, cathode and electrolyte with optimal conductivities of electrodes to generate a uniform current distribution for a specific surface area.

- The global optimization problem, where the variable parameters are conductivities, length and thickness of electrodes.

Conclusions

Mathematical model has been proposed to simulate processes taking place in 3D-MB. Calculations carried out to optimize electrochemically active electrode surface area in battery showed, that primary means to optimize electrode surface area utilization are manipulating with electrode conductivity and measurements.

In our model, processes taking place on solid-electrolyte interface are not modelled. Also, side reactions taking place in electrolyte are not modelled. Introducing these factors to model would be aim for further studies.

# References

- Doyle, M.; Fuller, T. & Newman, J. Modeling of galvanostatic charge and discharge of the lithium/polymer/insertion cell, Journal of the Electrochemical Society, 1993, 140, 1526 - 33

- Fuller,T.;Doyle,M.&Newman,J., Simulation and optimization of the dual lithium ion insertion cell, Journal of the Electrochemical Society, 1994, 141, 1 - 10

- Doyle, M.; Newman, J.; Gozdz, A.; Schmutz, C. & Tarascon, J.-M. Comparison of modeling predictions with experimental data from plastic lithium ion cells,Journal of the Electrochemical Society, 1996, 143, 1890 - 903

- Hart, R. W.; White, H. S.; Dunn, B. & Rolison, D. R. 3-D Microbatteries Electrochemistry Communications, 2003, 5, 120 – 123

- Danilov, D. & Notten, P. Mathematical modelling of ionic transport in the electrolyte of Li-ion batteries Electrochimica Acta, 2008, 53, 5569 – 5578

- Advances in Lithium-Ion Batteries ... book

- Open circuit potential by piecevise polynomials

- Mesoscale modeling of a Li-ion polymer cell Journal of the Electrochemical Society, 2007, 154, 1035 - 47

- Min, H.-S.; Park, B. Y.; Taherabadi, L.; Wang, C.; Yeh, Y.; Zaouk, R.; Madou, M. J. & Dunn, B. Fabrication and properties of a carbon/polypyrrole three-dimensional microbattery Journal of Power Sources, 2008, 178, 795 – 800

- Peled  Three dimensional thin film microbatteries for Autonomous MEMS

- Teixidor, G. T.; Zaouk, R. B.; Park, B. Y. & Madou, M. J. Fabrication and characterization of three-dimensional carbon electrodes for lithium-ion batteries Journal of Power Sources, 2008, 183, 730 - 740

# Tables

| Symbol | Quantity | Value |
| --- | --- | --- |
|  | Diffusion constant of Li ions in electrode |  |
| D | Diffusion constant of electrolyte |  |
|  | Electronic conductivity of anode |  |
|  | Ionic conductivity in electrolyte |  |
|  | Electronic conductivity of cathode |  |
| C_0 | Salt concentration |  |
|  | Initial Li+ concentration in anode |  |
|  | Initial Li+ concentration in cathode |  |
| J_0 | Charging/discharging current |  |
| H | Distance between electrode bases |  |
| L | Lenght of a plate/pillar |  |
| d | Distance between plate/pillar centres |  |
| h | Thickness of plate/pillar base |  |
| r | Thickness of plate / radius of pillar |  |
| D=H-L | Distance between electrodes |  |
|  | Distance between electrodes |  |
| j_o | Exchange current density |  |

Table 1. Material parameters in model.

Fig 1 Edge element labels in trench model

Fig 2Pojection of Concentration gradient development in time on positive electrode. Nubers on horizontal axis represent edge elements on positive electrode.

# Text boxes

Fig. 1 Difference between 2D and  3D battery.

Fig. 2 Possible 3D-MB architectures

Fig. 3 Trench model geometry used in calculations

Fig. 6 Varied geometrical parameters in simulations

Fig. 9 Cell voltage during discharge/charge

Fig. 7 Effects of changing electrode lenght

Fig. 8 Effects of changing electrode conductivity

Fig. 4: 3D-interdigitated battery architecture

Fig. 5 Trench model in 3D

###### Time /s